Input paper:   ENG10-3.1.11

Input paper for the following Committee(s): 	check as appropriate		Purpose of paper:

□  ARM	X  ENG		□  PAP					X  Input

□  ENAV	□  VTS							□  Information

Agenda item 			Report ENG9 9.14

Technical Domain / Task Number 2	2.2.7

Author(s) / Submitter(s)			Jörg Unterderweide, Traffic Technologies Centre TTC, Koblenz

# Colour fading

# Summary

Gathering experience from the natural weathering of colours is time-consuming.  Rapid weathering methods promise a remedy.  However, the choice of "good" surface colours depends on a wide variety of factors.  In this paper some experiences of the Traffic Technology Centre (TTC) at Koblenz/Germany are described.

## Purpose of the document

The report of ENG9 requests under 9.14 participants to submit input papers on Colour fading of AtoN (plastic and painted) methods to measure and assess to ENG10. With this input paper I would like to report on our experiences and to support the work of Working Group 1.

# Background

Colour fading is an important topic in the work of the German Federal Waterways and Shipping Administration.  The research methods and work were already presented to the participants of the last IALA workshop on “Sustainable Light and Power for the next Generation (IALABATT / IALALITE)” held at 20 to 24 March 2017 at Koblenz.

Measurement devices are already described in GL 1134 [1] and are not considered in this input paper.  Chromaticity coordinates, Luminance factor, glossiness and coating thickness are measured and analysed.  Measurements are done at AtoN in situ, at the outdoor weathering area (both natural weathering) and at the laboratory.

In situ, all actually influencing factors are taken into account.  But the factors can vary considerably.  Moreover measurements can be very time-consuming, e.g. you have to go out by ship to each site.  This type of test lasts the longest.

influencing factors

At the outdoor weathering area influencing factors are comparable for all simultaneously weathered samples, access and measurements are easier, but testing takes just as long as the in situ.

Outdoor weathering area

In case of a laboratory-based artificial weathering influences can be controlled and modified.  Therefore, results are comparable for all measurements.  However, the testing is limited to a few influencing factors, others remain unconsidered.  TTC considers only radiation, moisture and heat as the most important ones.  Air pollution, chemical processes, salt, bird droppings etc. are not considered.

Since natural weathering lasts for many years, TTC will establish the first correlations between natural and artificial weathering in the near future. Then the results of artificial weathering can be interpreted in the context of natural weathering. In best-case scenario, a simple factor between the lifetime of artificial and natural weathering can be established.  Colours on diverse materials are tested, such as

Steel;

Aluminium;

Polyethylene;

Films;

Reflective films.

In addition to the influencing factors mentioned above there are of course other factors with regard to the efficient use of AtoN, such as

Corrosion protection;

Maintenance, cleaning of the surfaces;

Paint application process, surface preparation;

Work safety;

Hazardous substances;

Shelf life of the paints;

long-term market availability;

Cost.

# artificial weathering Equiment

TTC uses a UV-Light Tester that is described by the manufacturer as follows:

“The QUV accelerated weathering tester reproduces the damage caused by sunlight, rain and dew. In a few days or weeks, the QUV UV tester can reproduce the damage that occurs over months or years outdoors. To simulate outdoor weathering, the QUV accelerated tester exposes materials to alternating cycles of UV light and moisture at controlled, elevated temperatures. It simulates the effects of sunlight using special fluorescent UV lamps. It simulates dew and rain with condensing humidity and/or water spray. The QUV accelerated weathering tester is the simplest, most reliable, and easiest to use weathering tester available. With thousands of testers in use worldwide, it is the world's most widely used weathering tester.”  [2]

UV Light Tester

Furthermore TTC uses a Xenon light tester that is described by the manufacturer as follows:

“The Q-SUN Xe-1 tester’s xenon arc lamps provide the best match to the full spectrum of sunlight.  Near-horizontal specimen mounting and optional water spray provide the most realistic moisture simulation available in a compact xenon arc tester.”[3]

Xenon Light Tester

Both test devices differ considerably, e.g. with regard to the number of sample places, the light spectrum used, etc. and finally also in the initial and operating costs.

# Results

Time series of the measurements show that colours have different lifetimes and "age in different ways".

Time series of the measurements

It is also not predictable which of the two factors (Chromaticity coordinates or Luminance factor) will fall short of the specifications first.  Sometimes it takes years before the reference measurements from natural weathering (e.g. according to artificial weathering results in Figure 6 “Evaluation”) are available. In some cases the colours are no longer available at the market.

Evaluation

Samples also occasionally show damages that affect testing and comparability.

Test samples

Despite the still missing correlation of the results artificial weathering has a high benefit. Results allow to compare different products with each other. Although it is not possible to determine how long a product remains stable in the specified colour regions, it is possible to determine whether a product has a high, medium or low colour stability compared to others. Knowing this gives an advice to distinguish good products from poor ones.

# References

IALA G1134 Surface Colours used as Visual Signals on AtoN 
https://www.iala-aism.org/product/g1134-surface-colours-used-visual-signals-aton/?download=true

QUV Accelerated Weathering Tester
https://q-lab.com/products/quv-weathering-tester/quv

Q-SUN Xe-1 Xenon Test Chamber
https://q-lab.com/products/q-sun-xenon-arc-test-chambers/q-sun-xe-1

# Action requested of the Committee

The Committee is requested to:

- Note the information provided in this paper and take action as appropriate.

Input document number, to be assigned by the Committee Secretary

Leave open if uncertain