Guideline

G1134

Surface Colours Used as Visual Signals on AtoN

Edition 2.0

December 2017

Revisions to this IALA document are to be noted in the table prior to the issue of a revised document.

| Date | Details | Approval |
| --- | --- | --- |
| December 2017 | 1st Issue | Council 65 |
| 2021 | working paper / intersessional / ENG 12 -> ENG 13 |  |

1	INTRODUCTION	6

2	SPECIFICATION AND MEASUREMENT OF THE COLOURS	6

2.1	Standard illuminant	7

2.2	Measurement Geometry	7

2.3	Standard Observer	7

2.4	Glossiness of the surface	7

2.5	Fluorescence	7

2.6	Additional Considerations	8

3	Measurement Devices	8

3.1	Light Source	8

3.1.1	Geometry	8

3.1.2	Spectrum	9

3.2	Light Receptor and Evaluation	9

3.2.1	Spectrophotometry – Absolute measurements	9

3.2.1.1 Charge Coupled Device (CCD) Spectrophotometer	9

3.2.1.2 Scanning Monochromator	10

3.2.2	Colorimetry - Relative measurement	10

4	Measurement Method and Requirements	10

4.1	Selection of Sampling Points	10

4.2	Laboratory Measurement	10

4.3	On-site-Measurement	11

5	CONSIDERATIONS OF PARTICULAR COLOURS	12

5.1	Red	12

5.2	Orange	12

5.3	Yellow and White	12

5.4	Green	13

5.5	Blue	13

5.6	Black	13

6	Persistence of colour appearance	13

6.1	Dirt covering the surface	13

6.2	Mechanical Abrasion	13

6.3	Mechanical Stress	14

6.4	Pigment Degradation	14

7	Coloured AtoNs in practice	14

8	Monitoring Colour Status During Service	15

9	Weathering Test	19

9.1	In situ weathering	19

9.2	Outdoor weathering test field	20

9.3	Artificial weathering in laboratory	22

9.3.1	Method	22

9.3.2	Fluorescent UV-Lamp Method	22

9.3.3	Xenon lamp Method	23

9.3.4	Results from artificial weathering tests	23

10	SYMBOLS AND ALPHANUMERIC CHARACTERS	25

11	COLOURS OF RETROREflECTING MATERIALS	25

12	COLOUR COLLECTIONS	25

12.1	RAL Classic Colour Collection	25

12.1.1	Ordinary Colours	26

12.1.2	Fluorescent Colours	26

12.2	Recommended Natural Colour System (NCS) Colour Numbers	26

13	DEFINITIONS	27

14	ACRONYMS	27

15	REFERENCES	27

List of Tables

Table 1	Matrix for registration and calculation of average values of Y, x and y of a buoy	17

Table 2	Matrix for registration and calculation of average values of Y, x and y of a day board	18

Table 3	RAL colours that meet the specifications for ordinary colours	24

Table 4	RAL colours that meet the specifications for fluorescent colours	24

Table 5	NCS colours that meet the specifications for ordinary colours	24

List of Figures

Figure 1	: 45° Illumination / 0° Measurement	8

Figure 2	Component Parts of a Spectrophotometer	9

Figure 3	Component Parts of a Colorimeter	10

Figure 4	Coloured part with marine growth should be avoided when evaluating the fading of the colour but included when evaluating the visual day mark colour of the AtoN.	15

Figure 5	Vertical Measurement Points and Datum Line	16

Figure 6	Top view of buoy with Datum Point and Measurement Points	16

Figure 7	An example to use ID number of the buoy as a reference point (Datum)	17

Figure 8	Day Board with measurement points	18

Figure 9	Influencing factors	19

Figure 10	In situ testing is time consuming, expensive and difficult	20

Figure 11	Outdoor weathering test field	20

Figure 12	Principle in an artificial weathering tester	21

Figure 13	CIE chromaticity diagram with measurements versus time	22

Figure 14	Test samples	23

INTRODUCTION

This document is intended for the provision of guidance to the technical aspects of selecting surface colours as defined in Recommendation R0108 (Surface Colours Used as Visual Signals on Marine Aids to Navigation [1]). It includes specification of colours, measurement, weathering and colour collections.

A surface colour is a colour perceived to belong to a surface. The colour of an ordinary surface, such as an ordinary paint or an opaque plastic material, is the most common kind of surface colour and is known as an ordinary colour. Other kinds of colours include fluorescent (or luminescent) colours, transilluminated colours (for example, the colours of internally illuminated panels) and the colours of retro-reflecting materials.

A surface colour can be specified in terms of its chromaticity and its luminance factor. Chromaticity co-ordinates, which may be plotted on a chromaticity diagram, define the chromaticity and the luminance factor is a measure of the lightness of the colour relative to a pure white diffusing surface under the same illumination. As a specification must be made with respect to some type of illumination, the International Commission on Illumination (CIE) has precisely defined several standard illuminants. The results of the measurement of a colour can depend significantly on the degree of gloss on the surface, and the CIE has also recommended various geometries of illumination and measurement.

Two colours may be measured as having the same chromaticity and luminance factor under one illuminant, but dissimilar ones under a different illuminant. This phenomenon is known as metamerism, and its effect can be very significant.  It is advisable to check that the appearance of a signal colour will remain reasonably constant under the various types of illumination by which the colour is expected to be seen.

A surface colour is usually seen in relation to other surface colours, and the perception of the colour can be quite markedly influenced by the presence of the other colours. Hence, a signal colour should always be checked, especially at a distance, for its appearance among the surrounding colours.

Deterioration of surface colours in use is a common occurrence, and care must be taken that signal colours always remain in compliance with their specifications.  Particular attention should be given to fluorescent colours, as they are liable to undergo rapid changes of chromaticity and luminance factor on exposure to radiation and wear if they are not provided with special protective surfaces.  Frequent inspections of fluorescent colours are advised until the normal useful life has been confidently ascertained for each typical situation where these colours are used.  Special care may be needed if fluorescent and non-fluorescent colours of the same chromaticity are chosen to be used together, as different deteriorations might produce dissimilarities of the chromaticity.

SPECIFICATION AND MEASUREMENT OF THE COLOURS

The guidance in this document are based largely on experimental work involving the recognition and naming of colours, but they have also taken account of common practice and the limitations of materials.  The method of specifying the colours is in conformity with the recommendations of the CIE.  The recommended limits of the chromaticity of a colour are specified by means of limiting boundaries that enclose a chromaticity region on a CIE standard chromaticity diagram and can be found in IALA Recommendation R0108(E-108) - Surface Colours Used as Visual Signals on Marine Aids to Navigation.

The luminance factor ß and the chromaticity co-ordinates x, y strongly depend on the measurement principle and the structure of the surface, texture, gloss, patterns etc.  To make colour measurement precise and repeatable various specifications are necessary.  It is stated that the chromaticity regions and the limits of the luminance factor are only valid, when the following specifications are fulfilled.

Standard illuminant

The standard illuminant specified for the measurement of a colour is D65, which represents a typical phase of daylight and has a correlated colour temperature of approximately 6500 Kelvin.  It is a tabulation of values across and beyond the visible spectrum and does not exist as a real light source although fairly close approximations to it can be realized.

Measurement Geometry

To take the effects of the coloured surface into account a 45º annular/normal geometry (45/0) is used for measurements.  The report CIE No. 15 (point 5.1.2) [4] emphasises this geometry as well.   Measurement with a geometry of normal / 45º will usually produce an identical result.

Standard Observer

The 2° standard observer (CIE No. 15, point 6.1) is used for large observation distances and above all to consider the attitudes of the human eye; this is the area with the highest cone density and is therefore relevant for colour perception.  The 2° observer covers the application for Marine Aids to Navigation (AtoN) purposes.

Glossiness of the surface

A glossy surface produces a saturated colour, whereas a matt-finished surface has only a poor saturation even when both surfaces are based on the same colour pigment.

As a result, the recommended IALA chromaticity regions can only be achieved by a surface with enough glossiness.  Therefore, it is recommended to use glossy colours for AtoN.

Fluorescence

Fluorescence is the process by which electromagnetic radiation of one wavelength is absorbed and re-radiated at another wavelength.  Sometimes a fluorescent material will absorb non-visible light and emit it as visible light.  Fluorescence and ordinary reflectance of radiation take place simultaneously and at the same wavelengths.  When the colour of a fluorescent sample is measured, the fluoresced light is added to the reflected light at those wavelengths.  Therefore, reflectance can exceed 100%. The UV contribution from the reference light of the measurement instrument is often not included and can vary from instrument to instrument.  However, instruments that use a Xenon light source as the reference light can give an approximation of UV daylight.

The common methods of colour measurement of fluorescent material in laboratory are polychromatic light irradiation method and monochromatic light excitation method. The characteristic of the polychromatic light irradiation method is that the polychromatic light simulating D65 is directly used. The spectral radiance factor of the fluorescent material under the illuminant is directly measured and then the tristimulus value is calculated. The limitation of this method is that the result is only based on this particular illuminant and could not predict the colour characteristics of the fluorescent material under another illuminant. But the monochromatic light excitation method doesn’t have this limitation and it can get the colour characteristics of the fluorescent material under each illuminant with specific wavelength.

Due to certain UV components in the illuminant during the colour measurement of the fluorescent material, attention shall be paid to the calibration and the reference materials are also different from that of ordinary colours.

The chromaticity region recommended for each fluorescent colour is identical to the region of the corresponding ordinary colour.  The colour of a fluorescent material should be measured with any protective surface that is normally used with the material.

Additional Considerations

The boundary lines of a chromaticity region, and the restrictions that may apply to the appropriate luminance factor, can together be referred to as the colour limits of a colour.  The recommended colour limits are extreme values that should not be transgressed (except as mentioned in sections 5.1, 5.4, 5.5 and 5.6).  More restrictive limits may be defined as appropriate to particular requirements; and they may be desirable for the signal colours used within one signalling system if substantial differences in appearance, either of chromaticity or luminance factor, are to be avoided.  Also, the recommended colour limits of a colour are intended to apply throughout its entire service life, so examination of its condition may be required from time to time.

It should be noted that, with the exception of the purple boundary of Red, the specifications have not been designed to assist people with severely defective colour vision, most of whom will have great difficulty distinguishing between red and green.

Measurement Devices

The measurement device consists of two main components. One is the light source, which illuminates the colour sample and the other is the light receptor. Although it is possible to build up these components on an optical bench, for practical measurements all-in-one devices with the light source, the receptor and a microprocessor to calculate the colour coordinates are offered.

Light Source

Geometry

The light source, the sample and the receptor have to be arranged in a specific geometry called 45/0 or 0/45. Only a small flat part of the sample will be measured. This part will be masked with a circular screen.

The measuring field will be illuminated with light incident under an angle of 45° towards the vertical line. This can be done with a ring illumination (annular), an array of several light sources (circumferential) or at least two lights on both sides of the vertical line (single-plane).

0

45

annular

circumferential

0

45

single-plane

0

45

: 45° Illumination / 0° Measurement

With 45/0 (0/45) annular, circumferential or single-plane geometry, the measurement results may be different, which is also related to the surface properties of the sample. Therefore, the comparison of surface colour measurement results shall be based on the same measurement geometry. If 45/0(0/45) single plane geometry is adopted, the measured result shall be produced according to the average value of rotation measurement result, 4 times or more rotation measurement is done until there is no obvious difference between the two measurements adjacent. Then the average value is taken as the final result. It is not recommended to use the single-plane geometry for on-site measurement, but annular or circumferential geometry is recommended.

Spectrum

The spectrum of the light source should have a continuous and stable spectrum of at least 400 nm - 700 nm for ordinary colours or retroreflective sheets of day-time conditions. For better results an interval from 380 nm to 780 nm is recommended.

Special care should be taken for fluorescent colours, which definitely need excitation with wavelength up to 380 nm. The fluorescence depends strongly from the UV and blue light and small changes at these wavelengths may change the colour significantly. Many manufacturers provide filtered xenon lamp illumination which can simulate sun light even at blue and UV.

For even more accuracy the monochromator excitation method should be used.

Light Receptor and Evaluation

The measurement is usually done with a spectrophotometer. For minor accuracy colorimeters may be used which are simpler and cheaper.

Spectrophotometry – Absolute measurements

A spectrophotometer measures the amount of light energy reflected from an object at several intervals along the visible spectrum.  It consists of four main parts; the light source (an approximation of the standard illuminant, usually a xenon light source), the sample (the surface colour), the detector and the output (a display or connected to a PC via software), as shown in Figure 2.  The spectral data are shown as a spectral reflectance curve and can be weighted with a standard illuminant and standard observer.

Component Parts of a Spectrophotometer

3.2.1.1 Charge Coupled Device (CCD) Spectrophotometer

A CCD is a type of image sensor that detects light.  It is an integrated circuit made up of an array of linked/coupled light-sensitive receptors.  The light-sensitive receptors detect the intensity of light received and convert it into an electrical signal.  The CCD detector corresponds to the range of wavelengths on a spectrophotometer.  Each pixel on the CCD represents a specific wavelength of light, and the more photons absorbed, the more electrical signal generated.  Therefore, the electrical signal output by the CCD at each pixel is proportional to the light intensity at each corresponding wavelength.  The resultant output is a reflectance curve, which can then be weighted against an illuminant and observer.  Further conversions to alternative units can then be performed.

This type of instrument is often used for in-situ (outdoor) measurements.  However, there are some limitations in wavelength accuracy (<10 nm).

3.2.1.2 Scanning Monochromator

A scanning monochromator uses a diffraction grating that ‘steps’ through the visual spectrum to separate the individual wavelengths (1-5 nm). These instruments are generally quite large and heavy and are more suited to laboratory measurements due to the time it takes to perform the measurement.  However, they are very accurate (~1 nm).

Colorimetry - Relative measurement

Colorimeters are tristimulus (three-filtered) devices that make use of red, green, and blue filters to emulate the response of the human eye to light and colour as shown in Figure 3.  Due to filter imperfections and not recording the spectral reflectance of the sample, tristimulus colorimeters are not suitable for assessing IALA’s surface colour requirements.

Component Parts of a Colorimeter

However, colorimeters used as colour difference meters do provide reasonable results.

Measurement Method and Requirements

Due to material selection, quality control and maintenance of visual AtoN, different measurement environments require different measurement accuracy. On the basis of different measurement environments, measurement methods can be divided into laboratory measurement and on-site measurement. Compared with on-site measurement, laboratory measurement has higher requirements on measurement conditions and measurement instruments, and sample preparation and selection will be different.

Selection of Sampling Points

For the submitted samples or AtoN to be measured, 3 to 5 testing points shall be selected for each colour and be scattered. And for on site measurement, the points shall also be selected in the direction of the sailing observation.

Laboratory Measurement

a. Environmental Conditions

Temperature: 25℃±5℃.

Humidity：relative humidity ≤(85±5%)，no condensation.

The working environment of the instrument shall be free from direct light, corrosive gas, strong vibration or strong electromagnetic interference indoors.

b. Measurement Samples

The measurement samples shall be made of similar substrates and the same coatings as the measurement visual AtoN.

c. Instrument Requirements

In addition to meeting the CIE 45°/0° (0°/45°) geometry, the measurement instrument shall also meet the following requirements:

(1). Light Source: Select the stable light source with continuous spectrum in 380 nm ~ 780 nm for the measurement of ordinary surface colours and the surface colours of retro-reflecting materials of day-time conditions. For fluorescent materials, use the polychromatic light simulating the standard illuminant D65 (the category is evaluated according to CIE 51.2 and shall not be lower than category BC) if polychromatic light irradiation method is selected. The tunable monochromatic light source in 250 nm ~ 800 nm can also be used if monochromatic light excitation method is selected.

(2). Spectrum Measurement: The required wavelength range is 400 nm ~ 700 nm. For higher accuracy a range  380 nm ~ 780 nm is recommended. The spectral resolution is not greater than 3 nm. The wavelength accuracy is better than ±1nm. The reporting interval is ≤ 10 nm.

(3). Sampling Aperture: It is recommended that the ratio of instrument’s sampling aperture to the radius of the sample is less than 0.04 m, and the measurement surface shall be filled with the entire sampling aperture.

(4). Equipped with standard white standard plate and zero calibration device for instrument calibration.

d. White Standard Plate

Use spectral reflectance data of 380 nm ~ 780 nm of the white standard plate under CIE45/0 or 0/45 geometry for calibration for the measurement of ordinary colours and retro-reflecting materials of day-time conditions.

Use spectral radiance data or chroma data under CIE45/0 or 0/45 or CIE BC grade D65 illumination conditions, which is similar to the measured samples. For the measurement of fluorescent materials using polychromatic light irradiation method.

On-site-Measurement

a. Environmental Conditions

The surface of measurement AtoN shall be clean and dry.

There shall be no corrosive gas or strong electromagnetic interference in the surrounding environment.

b. Measurement Instrument

It is recommended to use integrated measurement instruments that can be self-calibrated for on-site measurement. It is also recommended to adopt the 45/0(0/45) annular or circumferential illuminance /observation geometry, and the following requirements shall be met:

(1). Light Source: Select the stable light source with continuous spectrum in 380 nm ~ 780 nm for the measurement of ordinary colours and the colours of retro-reflecting materials of day-time conditions. Use the light source with continuous spectrum in 380 nm ~ 780 nm for the fluorescent materials with the adjustment of  its UV component.

(2). Spectral Measurement: The wavelength range is at least 400 nm ~ 700 nm. The spectrum resolution is not greater than 10 nm. The wavelength accuracy is better than ±2 nm. The reporting interval is ≤ 10 nm.

(3). Sampling Aperture: it is recommended that the ratio of instrument’s sampling aperture to the radius of the sample is less than 0.04 m, and the tested surface shall be filled with the entire sampling aperture.

(4). Equipped with a white standard plate and a zero calibration device.

c. White Standard Plate

Use spectral reflectance data of 380 nm ~ 780 nm of the white standard plate under CIE45°/0°(0°/45°) geometry for calibration for the measurement of ordinary colours and retro-reflecting materials of day-time conditions.

Use the fluorescent standard plate for the measurement of fluorescent materials, in addition to using the same white standard plate for the measurement of ordinary colours and retro-reflecting materials.

CONSIDERATIONS OF PARTICULAR COLOURS

Red

A minimum value of 0.07 is specified in R0108 Table 1 for the luminance factor of ordinary red, but significantly higher values can usually be realized and, in most circumstances, a value greater than 0.10 should be maintained.

The chromaticity region of red, which is identical for both ordinary and fluorescent colours, has been defined on the basis of achieving a very high probability of correct recognition for the colour, and it should prove to be quite practicable for ordinary reds with glossy surfaces and for fluorescent reds. There is doubt though, if their surfaces are matt or even semi-matt, whether serviceable materials of various kinds can always be manufactured in compliance with the restriction imposed by the white boundary of the chromaticity region for ordinary red. Also, it is not yet certain that serviceable materials, with glossy surfaces when new, can necessarily be manufactured so that their compliance continues throughout a reasonable service life if considerable loss of gloss occurs. Therefore, it is proposed that the chromaticity region for ordinary Red may be extended, but only for materials with matt or semi-matt surfaces, to a revised white boundary of y=0.840 – x. This provision for ordinary red colours should not be used unless it is necessary, and then only with the understanding that the probability of correct recognition of the colour will be significantly reduced. The problem discussed here is not expected to arise with any of the other chromatic colours.

Orange

The probability of correct recognition of orange is usually not as high as that of red or yellow; moreover, when these colours subtend very small visual angles, orange and red, or orange and yellow, are very likely to be confused. Hence, in considering signal colours that need to be recognized at a distance, orange does not provide a satisfactory additional colour to a system that includes red and yellow. If orange is completely excluded from a system of signal colours for AtoN, the adjacent hue boundaries of red and yellow should remain as recommended in the Tables, since, otherwise, correct identification may not be made even at close ranges and the colours will not exhibit a reasonably consistent appearance world-wide.

Nevertheless, orange is probably the best ordinary colour for conspicuity against the sea, and it should preferably be reserved for those objects for which detection in the water is more important than recognition of their colours. The objects that require this consideration are items of emergency equipment, such as life-jackets and life rafts. The highest conspicuity will be obtained with fluorescent colours, and then fluorescent red-orange may be used and may, in some situations, be more conspicuous than fluorescent orange, but fluorescent red-orange is not likely to be seen as distinct from fluorescent red.

Yellow and White

Discrimination between yellow and white is not practicable when they subtend very small visual angles, so they should not be considered as separate colours except for close viewing. In particular, it would be inadvisable to create any circumstances that required unequivocal distinction between yellow and white in retroreflecting materials, whether by day or by night.

At sea, the probability of recognizing, or even detecting, white on its own will often be low.

Green

As an ordinary colour, green does not usually show well at sea. However, colours of fluorescent green can be obtained with exceptionally high purities, and they will be very much more recognizable in most conditions.

It may be desirable, if green is required as a background colour on a sign with symbols or alphanumeric characters, to use a special dark colour – for example, one having a value of luminance factor lower than the minimum value recommended in R0108 Table 1. There is a possibility of confusing green with blue at the blue boundary of the green colour. To avoid this, IALA has introduced an IALA preferred green zone. This is shown on the chromaticity regions graph and associated tables in R0108.

Blue

On inland waterways, and in estuaries and harbours, where colours may be seen at close range, blue may prove to be a useful signal colour; but, at a distance, particularly at sea, it is unlikely to be easily recognized.

Although the recommended value of minimum luminance factor in R0108 Table 1 is 0.07, values significantly higher are attainable, and they should be required whenever possible if blue is to be seen alone.

It may be desirable, if blue is required as a background colour on signs with symbols or alphanumeric characters, to use a special dark colour, that is, one having a value of luminance factor lower than the minimum value recommended in R0108 Table 1. In such circumstances, a value as low as 0.05 may be considered for this special dark blue, which should anyway have a chromaticity conforming with the specification for ordinary blue, and which should never be used alone anywhere as signal colour.

Black

A maximum value of 0.03, as specified in R0108 Table 1, is recommended for the luminance factor of ordinary black if surfaces are glossy, but, if surfaces are matt or semi-matt, then it may be necessary to allow a maximum value of 0.04 although the probability of correct recognition will thereby be lowered.

Persistence of colour appearance

During operational use, the coloured surface of a Marine AtoN is effected by several factors which can have more and less influence on the visual performance.

Dirt covering the surface

Marine fouling and bird lime are well-known dirt covering issues on buoys but salt deposits from sea water and industrial air bourn pollutions can also have impacts on the visual performance of the AtoN to the point of causing the risk of misidentification by the mariner.

Use of anti-fouling paint or anti-fouling chemical compound if possible and regularly use of high pressure cleaners are recommended.

Mechanical Abrasion

Mechanical abrasion occurs often on painted buoys when vessels passing too close to the AtoN and make scratches and dents in the surface. It could also occur over the AtoN expected lifetime due to sand or other solid particles airborne such as cement.

The surface of plastic buoys are more resilient against mechanical abrasions due to the fact that the material of the buoy is dyed by the same colour as the surface.

Mechanical Stress

Mechanical stress which effecting colour fading is mainly seen in material of plastic buoys where loss of ductility of the materiel due to whitening of the material resulting in colour fading of the surface.

On steel buoys these changes in the surface are not seen but the difference in the coefficient of expansions between steel and the painted cover of surface can perform cracks in the surface which affect fading and degradation of the surface colour.

Pigment Degradation

Degradation of plastics due to ultraviolet (UV) light is inevitable and must be considered even from the manufacturing process. The type of plastic material selected and the addition of UV inhibitors and stabilizers used to protect the plastic will impact the design life of the coloured surface.

Degradation of plastic strength and loss of ductility is accelerated in latitudes with greater exposure to UV energy.

This process could be slowed down if the appropriate combination of inhibitors and stabilizers is used to guarantee the surface colour stability required for the life time expectancy of the plastic material selected, also considering the operational environment.

Degeneration of the painted surface colours of steel buoys depending very of the strength and quality of the paint.

A very rapid degradation is seen at AtoN painted with fluorescent colours where the degradation speed is commonly reduced by a final and covering clear UV varnish on the coloured surface.

Coloured AtoNs in practice

It should also be recognized that as soon as a coloured surface is exposed to the atmosphere the colour will begin to change. This is due to the degradation of pigments and dyes in sunlight, the breakdown of the glossy surface film, and the production of light coloured particles due to the breakdown of the coloured surface. Bright colours (particularly fluorescent colours) breakdown most rapidly while darker colours last the longest.

Coloured surfaces on buoys and other structures close to the water are also subject to salt deposits, marine growth, bird fouling, etc. Effective colour retention will depend on regular maintenance cleaning which will be simplified by utilising paint with a hard and high gloss surface.

It is important to remember that signal colours should be clearly recognisable in the conditions in which the mariner will view them. The perception of a colour will vary depending on the ambient lighting conditions, the background colour against which the colour is viewed and the surface finish of the colour (the gloss in the case of a paint finish).

They should contrast sufficiently with the local background and watercolour for them to be easily recognised. Dark green colour should be used on buoys on inland waterways where they are viewed against a predominantly light green background. For example, in Nordic countries, light colours are more easily visible in twilight and also against background luminance.

ln recent years, health and safety regulations have prohibited the use of many traditional pigments and alternatives may not have the long-term stability of those used in the past.

Monitoring Colour Status During Service

As described in Section 5, the colour of the surface will change over time. It is important to monitor the status of the colour to ensure it is in compliance with IALA Recommendation R0108 for the present Marine Aids to Navigation.

The colour may not degrade consistently across the surface so it is necessary to have a representative number of measurement points compared of the surface area.

A measurement should be taken at least every 1 m2, and the average x, y, Y coordinates are then calculated. The average of the readings should be used to compare the results to the CIE 1931 Standard Colorimetric System with the IALA coordinates as outlined in R0108.

For evaluation fading of the colour surface measurement points which are obvious not in compliance with the colour e.g. close to the waterline where marine growth is on the coloured surface. This part should be avoided when calculating the average value of the colour for assessment of the specific colour.

For evaluation of the general performance of a day mark or visual part of a buoy structure the surface of the entire surface should be included in measurements – also measurement points where the colour obvious not are in compliance with the genuine colour.

Coloured part with marine growth should be avoided when evaluating the fading of the colour but included when evaluating the visual day mark colour of the AtoN.

Instrumentation for measurement is outlined in Section 3.0. Consideration on which type of instrument used will depend on the environment where the measurements are carried out. For practical field use, a robust handheld instrument is recommended. Available instruments have commonly a wide range of functionalities e.g. to perform average values, acceptance criteria etc.

Visual comparisons using a colour swatch is acceptable if a measurement device is not available or impractical use. The use of swatches should not be used for higher accurate compliance testing. An example of a swatch test kit is shown in Annex A.

Below is examples of measurement methodology for different types of AtoNs:

Vertical Measurement Points and Datum Line

Top view of buoy with Datum Point and Measurement Points

An example to use ID number of the buoy as a reference point (Datum)

Matrix for registration and calculation of average values of Y, x and y of a buoy

| Measure Point/Degree | Y | x | y |
| --- | --- | --- | --- |
| 1/0 |  |  |  |
| 2/0 |  |  |  |
| 3/0 |  |  |  |
| 1/90 |  |  |  |
| 2/90 |  |  |  |
| 3/90 |  |  |  |
| 1/180 |  |  |  |
| 2/180 |  |  |  |
| 3/180 |  |  |  |
| 1/270 |  |  |  |
| 2/270 |  |  |  |
| 3/270 |  |  |  |
| Average values |  |  |  |

Day Board with measurement points

Matrix for registration and calculation of average values of Y, x and y of a day board

| Measure Point | Y | x | y |
| --- | --- | --- | --- |
| a1 |  |  |  |
| a2 |  |  |  |
| a3 |  |  |  |
| a4 |  |  |  |
| a5 |  |  |  |
| b1 |  |  |  |
| b2 |  |  |  |
| b3 |  |  |  |
| b4 |  |  |  |
| b5 |  |  |  |
| c1 |  |  |  |
| c2 |  |  |  |
| c3 |  |  |  |
| c4 |  |  |  |
| c5 |  |  |  |
| d1 |  |  |  |
| d2 |  |  |  |
| d3 |  |  |  |
| d4 |  |  |  |
| d5 |  |  |  |
| e1 |  |  |  |
| e2 |  |  |  |
| e3 |  |  |  |
| e4 |  |  |  |
| e5 |  |  |  |
| Average values |  |  |  |

Weathering Test

The durability of the surface of marine aids to navigation is important for the signalling purpose and for the operational cost in general.

A buoy during operational lifetime is effected by different influencing factors such as temperature change, moisture, radiation, corrosive salts, oxygen, air pollution, biological substances (guano), mechanical stress etc.

Influencing factors

For avoiding too fast degradation of the colour of a painted buoy or the surface of a plastic buoy, it is important to verify the durability of the surface coating and colour before deployment.

In practice, there are three different methods to evaluate how fast a surface colour degrade:

In situ weathering

Outdoor weathering test field

Artificial weathering in laboratory

- Changes during test in chromaticity coordinates, luminance factors, glossiness and coating thickness determined by measurements and analyses.

In situ weathering

In situ weathering is the most comprehensive way to conduct trials on AtoN due to fact that the test object is situated exactly in the specific environment the object are intended to be used into. The actual environment represent all influencing factors and the trial performs a complete result of the durability and robustness of the tested object at the specific location. Influencing factors varying considerable from locations to location accordingly observations differ from one location to another.

In situ testing is time consuming and long lasting procedure and the access to the test area e.g. at open sea can be difficult and expensive to reach.

Guidance on monitoring colour status during service given in section 8.0 of this document.

In situ testing is time consuming, expensive and difficult

Outdoor weathering test field

Outdoor weathering tests conducted on shore based test fields where material or specimen of the material arranged on special designed racks. In this arrangement, specimens exposed to direct sunlight and other influencing element but the influencing elements are only as they are at the actual test field.

At outdoor weathering test influencing factors are comparable for all simultaneously weathered samples.

Outdoor weathering tests are easier to conduct compared to in situ tests but the duration of the test takes just as long as in situ test.

Outdoor weathering test field

An outdoor weathering test is usually named as “natural exposure” if samples are placed in a certain location without any intervention other than the measurement of parameters previously declared on test protocols. On coloured polyethylene those natural exposure protocols may be aimed to assess the influence, in a non-accurately controlled atmosphere and for a certain period of time, of:

- salt spray, usually using a sodium chloride solution at a certain concentration, density and pH,

- humidity and temperature with condensation on the testing samples,

- UV radiation, most likely by placing the samples to the specific angle where there is the most perpendicular and persistent sunlight.

The usual parameters to be determined from these test protocols are the variation of luminance and colour during the test period. It is advisable that the time period to be considered for these test protocols is at least a calendar year, as this would include all the yearly variations of solar radiation and meteorological conditions, also acknowledging those conditions in general terms as they may vary according to climate changes.

The results may be delivered as tables or charts, as shown in the following figures:

Example of chart showing the variation of colour in 12 months

Example of chart showing the variation of illuminance in 12 months

Artificial weathering in laboratory

Method

A laboratorial artificial weathering test is an indoor test where the influencing elements can be controlled and modified for the accurate test specification. Therefore, results are comparable for all measurements carried out in that way. However, test facilities only involving limited influencing factors and others remain unconsidered.

The most common and important influencing factors considered during artificial weathering test are radiation, moisture and heat. Air pollution, chemical processes, salt, bird droppings etc. are not considered.

Accelerated weathering tester reproduces the damage caused by sunlight, rain and dew. In a few days or weeks, the tester can reproduce the damage that occurs over months or years outdoors. To simulate outdoor weathering, the tester exposes materials to alternating cycles of simulated sunlight or UV light and moisture at controlled, elevated temperatures.

For artificial weathering tests, two different methods are standardized and therefore worldwide accepted.

Fluorescent UV-Lamp Method,

Xenon lamp method.

Because of standardization, many test laboratories offer these tests as a commercially available service.

Fluorescent UV-Lamp Method

This method uses UV light from fluorescent lamps, so the colour degradation comes mainly from UV. In addition the sample is exposed to heat and dew. Special programs are defined witch describe heating, illumination and dew periods.

For paintings the methods are described in ISO 16474-3 [10] and for plastic in ISO 4892-3 [11].

The standards contain information about the UV-spectrum used, the required irradiance, temperature, condensation, measurement devices and the design of the test chamber.

Principle of an artificial weathering tester (side view)

Figure 12 shows an artificial weathering tester, but testers are available in different designs and cost levels.

The tester consists of a weathering chamber. The fluorescent lamps are positioned inside the chamber. The colour sample are at the side of the chamber and the surface to be weathered is inward-looking. The fluorescent lamps irradiate the colour samples.

At the bottom is a water reservoir with a heating unit. The water is heated so that the chamber is filled with water vapour. The vapour condenses on the colour sample. To improve condensation the samples slope down.

The lamps and the heating are switched on and off due to the weathering program chosen.

Xenon lamp Method

In this method the lamps are xenon arc lamps. The main difference to the fluorescent lamp method is that with filtered xenon light the radiation used is very similar to daylight. For the spectral adjustment special optical filters may be used. The exposure to heat and dew is the same as for the fluorescent method.

The standards behind this method are ISO 16474-2 [12] for paintings and ISO 4892-2 for plastic [13].

Results from artificial weathering tests

Chromaticity details plotted into CIE chromaticity diagram combined with time series indicates the durability of the colour of tested material.

Figure 13 shows a CIE chromaticity diagram plotted with measurement details versus exposure time for two greencolour samples. Embracing continuous lines of green, red and yellow representing the accepted area of the competent authority before testing (delivery status). Dotted lines represent the accepted level of chromaticity of the colour and the material when in use.

Small blue dots on the diagram indicates every single measurement. When in delivery status the colours are very saturated (s: starting colour, high y-value, uppermost dots of both samples). When the sample are exposed to the weathering test, the colour will fade and gets less saturated. The corresponding exposure times of each measurement are listed in the table.

In the example of Figure 13 the colour of both green samples moved towards white or grey with an inline development. Other green samples may move to blue or yellow instead but they always become desaturated.

Sample 1 on the left side lasts longer then sample 2 on the right. After an exposure time of 5655 hours (measurement 12) it is still in the accepted region of the competent authority. A mathematical extrapolation shows that it is expected to leave the region at about 7800 h (red dot 'e').

Sample 2 on the right side left the accepted region already between measurement 6 and 7. The interpolated exposure time is about 2300 (red dot 'e').

From this example it can be derived that the colour of sample 1 will last more then 3 times longer than the colour of sample 2. However, these results can only be used to compare the fading of different colours. As it is an accelerated weathering test the colours will last much longer in practice than the exposure time.

CIE chromaticity diagram with measurements versus time

Samples also occasionally show damages that affect testing and comparability (see Figure 14)

Test samples

The main result of artificial weathering test allows comparing product according to maximum exposure time the sample stays in accepted colour region.

The maximum exposure time of artificial weathering test has correlation to real exposure at location.

The correlation factor may take a value factor 5 to 20 depending on test parameters.

To find out the suitable factor require much work, see references [14 and 15]

SYMBOLS AND ALPHANUMERIC CHARACTERS

Good legibility requires that symbols and alphanumeric characters should have a sufficient contrast with the colours against which they are seen. A contrast of luminance factors is usually of more advantage than one of hues, and the ratio of the luminance factors should be made as large as is possible. Thus black should be applied on yellow, and, in general, white should be used on red, green or blue. However, if the luminance factors of red or green are particularly high, as they may be if these colours are fluorescent, then a contrast of black may be more satisfactory. Sometimes a symbol or an alphanumeric character may be clearer if it is outlined in a contrasting colour or is shown on a distinct panel of contrasting colour.

COLOURS OF RETROREflECTING MATERIALS

Two different specifications for the colours of retro-reflecting materials are required if the colours are to be defined adequately for the purposes of this document. The specifications need to define the colours for conditions of illumination that are representative of those occurring both by day and by night. With regard to this document, a specification of the colours for night-time conditions is unquestionably the more useful, but the methods of measurement have not yet been internationally resolved. A specification of the colours for daytime conditions has been undertaken by the CIE. A particular problem with a specification for daytime conditions relates to the geometry of measurement and the limits of the luminance factors. IALA Recommendation R0106 (E-106) - The Use of Retro-reflecting Material on Aids to Navigation Marks within the IALA Maritime Buoyage System refers [5].

COLOUR COLLECTIONS

This guideline uses the CIE 1931 Standard Colorimetric System [1] to specify ranges of colours by their chromaticity and luminance factors. This provides a scientifically correct method of defining colour. Although the use of chromaticity coordinates and luminance factor is well established, there are practical reasons to choose different methods to describe a colour. One of the reasons is that paint manufacturers can more easily work with colour collections.

A collection contains a number of colours and gives a name to them. Behind the collections stands an exact procedure to reproduce the surface colours.

A colour ‘swatch’ can often be obtained for each colour in a colour collection. These can be used to compare the colour of a surface to the ‘swatch’. However, this is a subjective method and should only be used under natural light, to give an indication of how different a colour appears compared to its original state. Swatches should be stored in darkness when not in use.

The use of a colour collection simplifies the definition of a colour and produces a number of colours that lie within the colour regions. However, because of the strong influence of gloss on the saturation of colour, there may not be a single chromaticity co-ordinate for each colour.

Throughout the world different types of colours are used depending on local circumstances. Some countries use darker colours because of light backgrounds; others need lighter colours in twilight to make the object more visible.

RAL Classic Colour Collection

The IALA regions can be achieved with the RAL CLASSIC Colour collection for glossy colour shades RAL 841-GL [6].

The following numbers are a subset of the RAL collection. They were chosen to ensure a high distance of recognition and good conspicuity and so the colours have a high saturation and luminance factor.

Ordinary Colours

RAL colours that meet the specifications for ordinary colours

| Number | Name | Luminance factor ß |
| --- | --- | --- |
| RAL 3028 | Pure Red | > 13% |
| RAL 6037 | Pure Green | > 15% |
| RAL 1023 | Traffic Yellow | > 50% |
| RAL 2008 | Bright Red Orange | > 25 % |
| RAL 5019 | Capri Blue | > 7% |
| RAL 9016 | Traffic White | > 80% |
| RAL 9017 | Traffic Black | < 1% |

There are other RAL-Colours that meet the specifications but are not as saturated as the colours shown in Table 5.

Fluorescent Colours

RAL colours that meet the specifications for fluorescent colours

| Number | Name | Luminance factor ß |
| --- | --- | --- |
| RAL 3024 | Luminous Red | > 25% |
| RAL 6038 | Luminous Green | > 25% |

For the fluorescent colours orange and yellow there are no RAL numbers that meet the specifications of this recommendation.

Recommended Natural Colour System (NCS) Colour Numbers

NCS is a system with the help of which all conceivable surface colours (not fluorescent or metallic colours) can be described [7].

NCS colours that meet the specifications for ordinary colours

| NCS-Code | Name | Equivalent RAL |
| --- | --- | --- |
| S 1085-Y80R | Red | --- |
| S 2070-G10Y | Green | --- |
| S 1080-Y | Yellow | RAL 1023 |
| S 0585-Y40R | Orange | RAL 2008 |
| S 4050-R90B | Blue | RAL 5019 |
| S 0500-N | White | RAL 9016 |
| S 9000-N | Black | RAL 9017 |

DEFINITIONS

The definitions of terms used in this IALA guideline can be found in the International Dictionary of Marine Aids to Navigation (IALA Dictionary) at http://www.iala-aism.org/wiki/dictionary and were checked as correct at the time of going to print. Where conflict arises, the IALA Dictionary should be considered as the authoritative source of definitions used in IALA documents.

ACRONYMS

CCD	Charge Coupled Device

CIE	Commission Internationale de l'Eclairage (International Commission on Illumination)

IALA	International Association of Marine Aids to Navigation and Lighthouse Authorities - AISM

NCS	Natural Colour System (Sweden)

nm	nanometre

RAL	RAL colour system (Reichs-Ausschuß für Lieferbedingungen und Gütesicherung)

UV	Ultra Violet (light) (10 – 380 nm)

REFERENCES

IALA RecommendationR0108(E-108) - Surface Colours Used as Visual Signals on Marine Aids to Navigation

CIE 1931 Standard Colorimetric System has become a Joint ISO/CIE Standard On Colorimetry: ISO 11664-1 / CIE S014 (series of standards).

CIE No. 39.2, Recommendations for Surface Colours for Visual Signalling (2nd ed.), 1983.

CIE No. 15,Technical Report: Colorimetry, 2004.

IALA Recommendation R0106(E-106) (June 2017) - The Use of Retroreflecting Material on Aids to Navigation Marks within the IALA Maritime Buoyage System.

RAL-Colour Collections: www.ral-farben.de, RAL Gemeinnützige GmbH, St. Augustin, Germany.

NCS Natural Colour System: www.ncscolour.com, NCS Colour AB, Stockholm, Sweden.

NCS Translation Key NCS RAL, July 2007 (with English, French, Swedish and German translation).

ASTM E2152 Standard Practice for Computing the Colors of Fluorescent Objects from Bispectral Photometric Data, American Society for Testing and Materials, United States of America

EN ISO 16474 - Paints and varnishes - Methods of exposure to laboratory light - Part 3: Fluorescent UV lamps

EN ISO 4892 - Plastics - Methods of exposure to laboratory light - Part 3: Fluorescent UV lamps

EN ISO 16474 - Paints and varnishes - Methods of exposure to laboratory light - Part 2: Xenon arc lamps

EN ISO 4892 - Plastics - Methods of exposure to laboratory light - Part 2: Xenon arc lamps

Sealite ‘Hot Climate Presentation´ by John Corio

SeaHow Report ‘Colour Stability of Navigation Buoys’ by Solar Simulator, Finland, 2016

An example of a swatch test kit (Finnish transport agency)

Laboratory Measurement

B.1  Selection of Measurement Points

a. Select 3~5 measurement points of each colour for the same sample to be measured;

b. Scatter the measurement points selected.

B.2  Measurement Procedures

a. Mesurement of Ordinary Colours and Retro-reflecting Materials of day-time conditions：

(1) Calibrate the measurement instrument with the zero calibration device;

(2) Use the white standard plate to calibrate the instrument after the zero calibration of the instrument is accomplished;

(3) Place the sample to be measured, measure and obtain the spectral reflectance of the measured points of the sample after the white standard calibration.

b. Colours Mesurement of Fluorescent Materials

-- Polychromatic Light Irradiation Method

- Calibrate the measurement instrument with the zero calibration device;

- Use the white standard plate and the fluorescent standard plate to calibrate the instrument after the zero calibration of the instrument is accomplished;

- Place the sample to be measured, measure and obtain the spectral reflectance of the measured points of the sample after the calibration is completed.

-- Monochromatic Light Excitation Method

(1) Place the sample to be measured,  and obtain the Donaldson Matrix for the measured points of the sample with the 10nm wavelength interval( including the reflecting component and fluorescent component of the sample, according to Standard ASTM E2153);

(2) Calculate the total spectral radiance factor of the measured sample, i.e., the final value for subsequent color parameter calculation.

On-site Measurement

C.1  Selection of Measurement Points

a. Select 3~5 measurement points of each colour for the same sample to be measured;

b. Select the measurement points in the direction of navigation observation;

c. Scatter the measurement points selected.

C.2  Measurement Procedures

a. Measurement of Ordinary Colours and Retro-reflecting Materials of day-time conditions:

(1) Calibrate the measurement instrument with the zero calibration device;

(2) Use the white standard plate to calibrate the instrument after the zero calibration of the instrument is accomplished;

(3) Place the sample to be measured, measure and obtain the spectral reflectance of the measured points of the sample after the white standard calibration.

b. Colours Measurement of Fluorescent Materials:

(1) Calibrate the measurement instrument with the zero calibration device;

(2) Use the white standard plate to calibrate the instrument after the zero calibration of the instrument is accomplished;

(3) Use the fluorescent standard plate to calibrate the instrument after the calibration of the white standard plate is accomplished;

(4) Measure the AtoN and obtain the spectral reflectance of the measured points after the calibration;

(5) Obtain the measurement result of different UV radiation components through the adjustment of UV components of light source.

monochromatic light  excitation method

The monochromatic light excitation method is the most precise method for measuring fluorescent colour. The measurement equipment consists of two separate monochromators (figure D.1). The irradiation monochromator produces monochromatic light to illuminate the sample. The viewing monochromator analyzes the radiation leaving the colour sample.With this method the radiation-transfer properties of fluorescent material become independent of the specific illuminant spectrum.

The result of the measurement is a two-dimensional array of bispectral photometric values. It is obtained by setting the irradiation monochromator at a series of fixed wavelengths () in the ultraviolet and visible range, and for each , using the viewing monochromator to record readings for each wavelength () in the visible range.

The resulting array is called 'Donaldson Matrix'. The value of each element () of this array is described as the Donaldson radiance factor (). It is an instrument and illuminant-independent photometric property of the sample.

To get the emitted spectrum of a colour sample with a specific light source it is necessary to calculate the stimulus function according to Equation D.1. From the calculated stimulus function the Tristimulus Values are derived in the usual way (Equation D.2).

The advantage of this method and the Donaldson matrix is that they provide a characterization of the sample’s radiation-transfer properties, without the inaccuracies associated with source simulation and various methods of approximation.

Sample

Irradiation

Monochromator

Viewing

Monochromator

Photoelectric

Detector

Illuminant

Figture D.1  Component Parts of a two-monochromator system

The calculation of tristimulus values with the Donaldson radiance factor () are as follows:

Equation D.1 Stimulus Function

Where:

is the sample’s stimulus function (relative spectral radiance),

is the relative spectral power of the standard illuminant  at the element’s irradiation wavelength().

Equation D.2 CIE1931 Tristimulus Values

Where:

is the normalization constant,  ,

, , are CIE 1931 standard observer.

For further information see ASTM E2152 Standard Practice for Computing the Colors of Fluorescent Objects from Bispectral Photometric Data, American Society for Testing and Materials, United States of America.

Spectral Mismatching of Colour Measurement by photoelectric Integration Method (Colorimeter)

Photoelectric integration method (with Colorimeters) performs integrating on the measured spectral power by matching the spectral response of the detector to the CIE standard colorimetric observer、、, to get the related colour parameters of the samples, as shown in figure E.1.

Figure E.1 The principle of photoelectric integration method

In fact, there is always a spectral mismatching problem in this method with the limitation of technology. The relative spectral sensitivity of the detector cannot match perfectly with the curve corresponding to the standard observer 、、, and there is somewhat deviation. Generally, ,,   are used to evaluate the spectral mismatching degree of the detector. The larger the value is, the worse the matching degree is, the greater the error of the measurement result will be, especially for the red, blue and other color visual AtoN samples.

(C.1)

，，is relative spectral power distribution of standard source A， is spectral sensitivity curve of detector.

Figure E.2  Simulation of detector with 5% of , and

Figure E.3  Typical red, green and yellow colour samples (left) and their spectral distribution (right)

In the research process, the detector system with,and   as shown in Figure E.2 is simulated to measure the chromaticity coordinates of typical red, green and yellow color samples as shown in Figure E.3. The measurement results are shown in Table 1. When =,== 5%, the chromaticity coordinate error is as high as 0.0031. While in the market, there are more detector systems with =,=≥ 7%. In addition, if there is a narrow-band spectrum in the spectrum of the sample to be measured, the detection error will be greater. Therefore, spectrophotometry method is recommended for high-precision color measurement.

Table 1 Measurement results of detector spectral mismatch

| Mismatch error Chromaticity coordinates |  | Red |  | Yellow |  | Green |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | x | y | x | y | x | y |
| 0% |  | 0.3466 | 0.3101 | 0.2632 | 0.4733 | 0.2903 | 0.4127 |
| 5% | Result | 0.3471 | 0.3089 | 0.2638 | 0.4741 | 0.2894 | 0.4158 |
|  | Deviation | -0.0005 | 0.0012 | -0.0006 | -0.0007 | 0.0009 | -0.0031 |

The recommended colours for NCS for green and red are not equivalent to the recommended RAL Colours

The recommended colours for NCS for green and red are not equivalent to the recommended RAL Colours