IALA Guideline

G1???

Properties of a good marine solar Module

Edition 1.0

Document date

Revisions to this IALA Document are to be noted in the table prior to the issue of a revised document.

| Date | Page / Section Revised | Requirement for Revision |
| --- | --- | --- |
| Mar 21 | All | New guideline |

1	Introduction	7

2	Scope	7

3	Use of solar panels as power source for aton – Peter D	7

4	Technology	8

4.1	Monocrystalline	8

4.2	Polycrystalline	8

4.3	Thin film / flexible modules	9

4.4	Solar panel technologies – Monocrystalline vs Polycrystalline panels	9

5	Design	10

5.1	Number of cells	10

5.2	Intercell connection	10

5.3	Colour	11

5.4	Shock and vibration	12

5.5	Panel Efficiency	13

5.6	Diodes	13

5.7	Construction of modules	13

5.7.1	Glazing material	14

5.7.2	Backing material	14

5.8	Quality	14

5.9	Ingress protection	14

5.10	Wind loading	14

5.11	Performance	14

6	Developments	14

7	Operation	15

7.1	MPPT	15

7.2	PWM	15

7.3	Impact of solar regulation	15

7.4	Operating conditions – Part of environmental factors?	15

8	Application – is this need or should it be combined with installation?	15

8.1	Self-contained	15

8.2	BuoY	15

8.3	Other platforms – Smart buoys	15

8.4	Lighthouse	15

8.4.1	Grid connected systems	15

8.4.2	Islanding system	15

8.4.3	DC floating system	15

9	Environmental factors	15

9.1	Materials used in production	15

9.2	Deposits	15

9.2.1	Bird Foul (Guano)	15

9.2.2	Salt	15

9.2.3	Dust	16

10	Temperature	16

10.1	Humidity	17

10.2	Irradiance	17

10.3	Atmospheric Effect	17

10.4	Poor levels of visibility	17

10.5	EMC impact (Lightning)	17

10.6	climate change impacts	17

11	Installation	18

11.1	Mounting methods	18

11.1.1	Self contained	18

11.1.2	Buoys	18

11.2	Orientation	18

11.3	Shadowing/Shading	18

11.4	AC connected – IS this used in a marine environment?	19

11.5	Identification of modules	19

12	Problems / failures	20

12.1.1	If lightning strikes :	20

12.2	Poor connection between cells	21

12.3	Hot spots	21

12.4	Micro cracking – wind pressure	21

12.5	Physical Stresses	22

12.6	Water ingress	22

12.7	Sealant failure	22

12.8	Delamination	23

12.9	Cell corrosion	23

12.10	Metal corrosion	23

12.11	Poor insulation	24

12.12	Mechanical impacts caused by handling and shock/vibration	24

12.13	Ice	24

12.14	Theft of modules and ways to prevent it	25

12.15	Connector failure and use of connectors and types	25

13	Maintenance and testing	25

13.1	Equipment and measurement devices – Some info from Peter S	25

13.2	Life / aging	27

14	Procurement	27

14.1	Assessment	27

14.1.1	The guarantee:	27

14.1.2	Price list :	27

14.1.3	Manufacturer	27

15	Recycling and repurposing	28

16	Standards	28

17	DEFINITIONS	28

18	ACRONYMS	28

19	REFERENCES	28

20	documentation	29

20.1	proofs	29

20.2	references	29

20.3	datasheet	29

20.4	(Example Heading level 2)	29

20.5	(Example Heading level 2)	29

21	AIMS AND OBJECTIVES (Example Heading level 1)	29

22	Example Heading level 1	29

22.1	(Example Heading level 2)	31

22.1.1	(Example heading level 3)	31

23	Example Heading level 1	31

23.1	TABLES	31

24	FIGURES	32

25	DEFINITIONS	33

26	ACRONYMS	33

27	REFERENCES	33

ANNEX A	EXAMPLE OF AN ANNEX - LANDSCAPE	34

APPENDIX 1	EXAMPLE OF AN APPENDIX TITLE	35

ANNEX B	(EXAMPLE ANNEX TITLE)	36

ANNEX C	PERMITTED COLOUR PALETTE	37

List of Tables

Table 1	Example of a table caption; table with the significant information in the first column	20

Table 2	Example of a table caption; table with the significant information in the first row	21

Table 3	Example of a table caption; table with coloured rows	21

Table 4	Example table caption	23

List of Figures

Figure 1	Component of a solar system by Rfassbind - Own work, Public Domain,	7

Figure 2	Diagram of atmospheric effects.	11

Figure 3	Example figure caption	21

Figure 4	Another example figure caption	22

List of Equations

Equation 1	Geographical range	20

Equation 2	Theory of Special Relativity	20

# Introduction

The use of solar panels on marine aids to navigation (AtoN) dates back to the mid 1980s, where the goal was to adopt a clean renewable energy source. This source of energy allowed the powering of remote and afloat AtoN, removing the need for gases such as Acetylene powered light sources. This also eliminated the requirement for periodic exchange of gas holders, at a significant number of locations.

Since these early days, the development of solar modules has made significant strides, moving from niche areas as small off grid systems, to the mainstream power production, in the form of grid connected “solar farms”. This has delivered great enhancement in solar cell efficiency and a reduction in manufacturing costs, but it has resulted in manufacturers focussing their products toward this high-volume market.

Naturally, the demands and requirements for such high volume “solar farm” panels differ to that required in a remote location marine environment. This has resulted in the challenge of trying to identify the qualities that make a good marine solar panel from that presented in a data sheet of the more mainstream panel. This guideline hopes to identify the area that are important to a survivable marine solar panel.

# Scope

This guideline has been developed to assist marine aids to navigation (AtoN) manufacturers and authorities when selecting and applying solar modules to power systems in a marine environment. It is intended to inform the reader about factors influencing performance and reliability, as well as considering aspect of selection and purchasing.

# Use of solar panels as power source for aton – Peter D

Although the first solar panel was created in 1881 by Charles Fritts, it was not until 1957 that the first commercial solar cells became available. This technology was fist adopted on aids to navigation (AtoN) in the mid 1980, generally as trials, leading to adoption in the mainstream as a source of power in the mid 1990. This technology initially allowed the replacement of small acetylene gas AtoN such as that used on buoys.

As the efficiency of solar cells has developed through the expansion of commercial mainstream solar modules for such things as housing and solar farms. This has allowed solar to be adopted for significantly higher demand system at one end of the power spectrum and the development of small self-contained AtoN often referred to as Integrated power systems (IPS) at the. other.

As the power demand of a solar system expands so the number cells need expands. How these expanding systems refer to different components is captured in figure 1, starting from solar cells used on an IPS to solar arrays used on a larger lighthouse installation.

When considering designing a photovoltaic power system, IALA provide a guideline G1067 on how to design a photovoltaic power system.

Purpose of solar modules

Component of a solar system by Rfassbind - Own work, Public Domain,

How to recognize the best photovoltaic panels on the market?

It is difficult for a neophyte to verify the quality of a solar panel only by checking the visual aspect. Indeed, several criteria such as standards and technical specifications will have to be checked to ensure the reliability of his photovoltaic solar panel.

# Technology

## Monocrystalline

It is made from the mineral "silicon", which is found in abundance in sand. A single "grown" crystal is gradually formed into a block. The cells are then cut into thin slices from 250 to 350 μm. The efficiency limit of the crystalline cell is around 35%. Currently this type of cell achieves efficiencies of 21%.

## Polycrystalline

It is made from molten silicon glass that is formed in a mould. It is cheaper than the monocrystalline cell, but its limit efficiency is 32%. Currently this type of cell achieves efficiencies of 19%. It is recognized because its colour is irregular and clearer than the monocrystalline and has a rectangular shape without cuts at the edges.

Polycrystalline cells are somewhat less efficient than monocrystalline cells but are more efficient when the sun reaches low incidence angles on the solar cell.

## Thin film / flexible modules

It uses a new technology consisting of a thin film of pure silicon glass on a glass or ceramic substrate. This layer does not exceed 20 μm. The thickness of the entire cell is 300 to 800 μm. The substrate may also be plastic which allows the production of flexible modules.

Currently the efficiency of these cells is around 13% although in laboratories efficiency levels of 15% have been reached. The advantage of this technology is that it is much cheaper than the crystalline cells, it allows the formation of flexible modules and in the manufacturing process no polluting elements are used. They have a performance less than half that of crystalline type cells.

Types of solar cells

## Solar panel technologies – Monocrystalline vs Polycrystalline panels

Crystalline silicon PV cells are the most popular solar cells on the market today and provide the highest energy conversion efficiencies of all commercial solar cells and modules. Silicon is safe for the environment and one of the most abundant resources on Earth. Monocrystalline and Polycrystalline panels are both types of solar cells that are made from crystalline silicon and the most commonly used crystalline silicon solar cells. Monocrystalline panels, as the name suggests, are created from a single continuous crystal structure. Monocrystalline solar panels typically have the higher efficiency rates since they are made out of a higher-grade silicon and their single-cell structure creates minimal resistance to the flow of electricity once the electrons are excited by the sun. Solar panels are constructed using a collection of each of these types of cells. It was once the case that polycrystalline solar panels were 20-30% cheaper than monocrystalline solar panels because producing monocrystalline cells was a more expensive process than producing polycrystalline cells, this however is no longer the case with the price difference between the technologies being negligible. With all solar cells, electricity production falls as temperature goes up. Studies have shown that in the summer months with high temperature, polycrystalline and monocrystalline modules perform similar however, in non-summer months, even with similar irradiance, monocrystalline modules perform better then polycrystalline modules. The choice between monocrystalline and polycrystalline solar panels is not considered a critical factor when purchasing solar panels unless modules are susceptible to long periods of low irradiance in which case monocrystalline panels would be recommend over polycrystalline.Construction of modules

Polycrystalline, Monocrystalline or Amorphous? Which solar cell technology did you choose and why? Make sure that the solar panel technologist meets your needs and expectations and that it is adapted to the production context of your solar power plant.

# Design

This section looks at some of the important factor in the design of reliable marine solar modules.  When considering design a solar system then also see guideline G1039 designing solar power systems for marine aids to navigation (Solar sizing tool).

## Number of cells

Each solar cell within a solar module produces about 0.5V as 25°C under standard test condition. This mean the solar cells within a module are interconnected in a series and parallel arrangement to achieve the desired output voltage and power. Typically for a 12V modules this is 36 cells in series to allow a suitable output for the charging range of a 12V battery system at different operating temperatures.

Modules designed for domestic and grid connected purposes will have a higher output voltage and more solar cells in series, typically 72, as the drive is to maximise the voltage and efficiency of the modules.

## Intercell connection

The series / parallel connectivity of the solar cells within a module can impact on how well your solar systems perform. On paper, it looks as if striving for modules with the greatest efficiency is best, but in a marine environment, these modules are often fitted where small amounts of shading may occur due to supporting structures or hand railing within in the vicinity.

| The above example of shadowing could result in a 90% reduction in power output. |  |  |  |
| --- | --- | --- | --- |
| The above example of shadowing could result in a 75% reduction in power output. |  |

Examples of shadowing on solar modules

Shading can therefore lead to a period of reduce or no output from a module or part of a module. Given this, it is worth considering a less efficient module overall, but one with greater parallel sections. This will then ensure some output from a module during periods of partial shade, probably leading to a more effective solar system as a whole. When fitting the modules consideration should be given to orientating the parallel section in line with the possible source of shading to minimise any impact.

An example of a module with 6 parallel sections

## Colour

The colour of solar modules is generally a dark blue or black to maximise the energy capture, see figure 1. This however can have a detrimental impact on the look of the daymark, such that the solar modules need to be located with the daymark in mind. See Figure.

Example from WSV showing the solar modules within dark sections on the daymark

The use of coloured solar modules on AtoN is a new area of development, predominantly driven by architectural building pressures, but is slowly becoming more readily available. This option has not generally been considered as an option on AtoN, but the efficiency of conventional AtoN and solar modules having improved, there is now not the need to maximise the available space for energy generation. This potentially allows the option to adopt coloured module of a lesser efficiency to improve the daymark. An example of this has be tried on the Norwegian lighthouse of Domberskjera as can be seen in figure 2

Domberskjera lighthouse with white solar modules

There are a number of approached to achieving a colours module, including colouring the solar cells, colouring the glass, but one of the most effective method is through the uses digital, ceramic printing of small coloured dots on the glass. This option provides the highest number of colour option along with a stable colour for a >20 year life, but with approximately 20% reduction in the solar module performance.

An example of digital, ceramic printing on glass (Left) and solar cell colouring in yellow (right)

## Shock and vibration

The impact of shock and vibration is generally not an issue for the design of the solar modules, and can generally be mitigated by the design of the structure it is fitted to. The design does need to consider the handling and environmental condition and as such should be consider “rugged” for this application.

“Each module shall be ruggedly constructed to withstand the shock and vibration incident to service on lighted buoys and fixed ATON structures.”

## Panel Efficiency

Panel efficiency is the portion of sunlight energy that can be converted into electricity via the photovoltaics solar cell. For example: a solar panel with 15% efficiency and an area of 1 m² will only produce 150W at Standard Test Conditions (STC).

It is a factor to be considered according to your context of installation, the rate expressed as a percentage will indicate you the ratio between the power produced and the power of the radiation absorbed by the solar panels. The efficiency of photovoltaic solar panels varies according to several determining factors, but generally it is between 12 and 20%. There are very good solar panels with yields at 12%, the yield is not to be considered to determine the quality of the equipment but rather to help you in the choice of photovoltaic modules according to your solar installation configuration.

## Diodes

By pass diodes limit impact of module shading – these are physically fitted within the panel but can be fitted in a junction box attached to the solar models

Blocking diode to prevent a shaded module acting as a load when modules are in parallel. These are usually in junction boxes on the back of the panel. For buoys in more temperate climates this is not always adopted and there is generally illumination all around – think about the voltage being produced on the shaded side. An alternative approach is to have a regulator on each module so a blocking diode is not necessary.

Need a photo of the electrical circuit showing both diodes. ideally needs to show cells not modules.

## Construction of modules

The construction of all solar modules is made from a three part laminate essentially sealing the selected solar cell technology between two other supporting materials and using Ethylene-vinyl acetate (EVA) sheet as a waterproof bond layer for the laminate. For flexible solar modules, thin film solar cells are used within a flexible plastic laminate, but for rigid solar modules, the monocrystalline and polycrystalline cells can be used with supporting stiff materials as part of the laminate as show in Figure 7.

Generally it has been found that rigid structure modules have proven last better than flexible solar modules. Although flexible modules have been used on AtoN, with the advantage of lightness, it had been found that they have less output and are more susceptible to water ingress in the harsh environment.

Add photo of the swale buoy Peter D

Figure showing the construction of a solar module from www.sunnectsolar.com

### Glazing material

Both toughened glass and acrylic can be used as the glazing section. The use of acrylic allow a small degree of flexing during impact, without loss of the module. It also reduces the weight which benefits handling. The transmissivity of acrylic can also be better than toughened glass.

### Backing material

Various types of backing materials have proven to be successful in a marine environment. These being Polyvinylfluorid foil as a frameless arrangement where it is supported within a structure, marine grade aluminium where structural support is needed and stainless steel for standalone arrangement. A glass / glass structure within a frame is also used when the solar modules are land based and protected from direct action from the sea.

## Quality

The quality of photovoltaic solar panels:

The quality of the photovoltaic solar panels is an important factor to consider for any rooftop or ground-mounted solar power plant project. Indeed, the quality of the chosen photovoltaic modules will determine the payback time of your solar power plant by guaranteeing you an optimum production of solar energy in the long term.

Specification

EN61215

EN61140

503 from join research centre ISPRA – useful content but may not be current

Materials

## Ingress protection

EN60529 – IP67

# Wind loading

40m/s need some word about this

## Performance

After 10 years 90% and after 15 years 80% as a minimum

Corrosion resistance when used in a marine environment

# Developments

Perovskite cell

Double sides solar cells

# Operation

## MPPT

## PWM

## Impact of solar regulation

Poor regulation

## Operating conditions – Part of environmental factors?

# Application – is this need or should it be combined with installation?

## Self-contained

## BuoY

## Other platforms – Smart buoys

## Lighthouse

### Grid connected systems

### Islanding system

### DC floating system

# Environmental factors

Although solar panels appear to be an inert object with a glass surface, no moving parts all held together in a frame, it is influence by its operating environment for both performance and operational longevity. This section outlines the key factor to consider.

Two major factors that affect solar panel performance under normal circumstances are Irradiance and Temperature. There are also other factors that are area dependent like Shadowing and environmental factors like Salt film, Dust and Bird Foul (Guano).

## Materials used in production

## Deposits

These factors impact on the maintenance frequency and sizing of solar system.

Snow, sand, pollution deposits

### Bird Foul (Guano)

While it is possible to prevent birds from landing on the solar panels using bird deterrent i.e. bird spikes, etc, they can still drop their droppings while flying. Over time if not rid of, it will become harden and form a similar shading effect that can drastically affect the panel’s efficiency.

### Salt

To prevent a salt film and dusts from forming on the panel’s surface, it is recommended to install the panels at an angle to induce a natural washing effect when the rain comes. This will help wash away the salt that is gathered on the surface.

### Dust

Dust is an issue in certain extremely hot environments and can cause several issues.

Dust can cover lanterns and day marks, severely impacting the range, can cover solar panels thereby reducing the ability to charge batteries and its abrasive nature can accelerate deterioration of AtoN components.

Dust can be of different physical properties, both industrial and natural, can cause different issues and require different controls and cleaning methods.

Excessive dust also poses health and safety related risks to AtoN personnel. refer to IALA G116 / 2.2.7. DUST

# Temperature

One of the factors affecting solar panels is temperature that is generally caused by the environmental effects. Depending on the location, those at the north and south generally get colder climate at the expense of the daily available sun hours. This means that the solar panels perform at optimum efficiency due to the lower operating temperature. However, those panels that are installed nearer to the equator generally get hot all year round which translate to a drop in the panel’s efficiency.

The output voltage of a module is affected by the cell temperature and changes in a similar way as the output power. Therefore, every solar panel has its own thermal characteristics derived under Standard Testing Condition to measure the loss known as the “temperature coefficient”. Generally, it is given as -0.45%/°C for Monocrystalline and -0.50%/°C for Polycrystalline panel. Refer to IALA G1136 / 5.1.3. SOLAR PANEL PERFORMANCE for more info.

Temperature: refer to G1039 / 1.1.4 TEMPERATURE INFLUENCE and 1.1.5 THERMAL CHARACTERISTICS

7 - Temperature coefficient :

The temperature coefficient indicates the electrical behaviour of your solar panel from a standard operating temperature of 25°. The units of this coefficient are expressed in "% per ° C", so the lower the coefficient, the more efficient the solar panel is. Conversely, the higher the number, the less the photovoltaic module will produce in case of strong heat or early afternoon.

A high temperature coefficient is the sign of a solar panel of lower quality. A reasonable number is around 0.5%, so the best solar panels go down to 0.3%, while 0.7% indicates a poor coefficient in terms of performance and therefore a photovoltaic equipment not very reliable.

Hot and cold impacts efficiency. Higher temperatures result in  ADD diagram of what this means

Colder temperatures enhance efficiency, but battery storage reduces??

High levels of UV- does this have an impact on life through breakdown of PN junction?

## Humidity

## Irradiance

Irradiance is known as the amount of solar power available per unit area. Symbol = I. Its units are represented by kW/m² or mW/m². It is one of the major factors that affects the performance of solar panels. How we install each panel to face the sun is very important. Due to geometric effects, it is always recommended that each panel is facing 90° perpendicular to the sun’s altitude angle (when it is at the highest point in the sky) to ensure that the panel can capture all the sun’s radiation.

## Atmospheric Effect

Atmospheric Effects consists of two categories, Direct and Diffuse Radiation. The photo below to illustrate the concept easier.

Solar constant = 1.36kW/m²

solar radiation at surface = 1kW/m²

Sun

Reflected solar radiation (albedo) from atmosphere

Dust particles

Clouds

Direct solar radiation

Diffused solar radiation

Atmosphere entry point

Earth’s surface

Diagram of atmospheric effects.

## Poor levels of visibility

Pollutants can have the same impact, less of an issue offshore, but could be on inland waterways through built up areas

Performance factors

## EMC impact (Lightning)

Damage can occur to your photovoltaic system due to a direct lightning strike or nearby. Investing in protection is all the more advisable if your installation is expensive. Lightning protection will be prioritized at lighthouse sites located in areas where the risk of lightning strikes is highest. In order to know the probability of lightning strikes, it is advisable to use a kerunic level map of the place in order to define the level of protection that will be adapted

## climate change impacts

- Refer to Guideline GYYYY

# Installation

When selecting a suitable module for a marine environment, there will be a balance between the need to generate the power and the number and size of the solar modules.

What sizes are used on  buoys and what sizes used on lighthouse and why?

Size, weight, power, efficiency, performance

- Self contained Vs  discrete panels

Safety and handling

## Mounting methods

### Self contained

With self contained units are designed with the solar module integrated into the moulded in – replace whole unit on failure (less stressful environments??

### Buoys

The fitting of solar modules to buoys is generally achieve through direct fixing arrangement for security purposes, yet there is still a need to be able to simply remove and replace the modules following failure.

Add photo of rubber nuts Peter D

Consideration of physical protection to the modules

Buoy – removable and replaceable – Photo from Peter.

Lighthouse based – can be as stressed but are on a dedicated frame. Can be glass/glass in a frame

Photo from Ronan

## Orientation

- Refer to G1039 / 1.1.6 SOLAR PANEL ORIENTATIONDisposal/ recycling

## Shadowing/Shading

It is always recommended to install arrays that have clear line of sight to the sun. Any shadowing caused by nearby buildings or trees can cause a significant reduction in maximum power point voltage therefore a reduction in the maximum power available from the array. Although temporary, meteorological factors like passing clouds caused during overcast days also affects the panels efficiency.

Solar panels should be usually oriented toward the equator to maximise power output. The tilt angle should be chosen with regard to insolation, geographic location, self‐cleaning capabilities, available space, etc.

In the case of floating Marine Aids to Navigation it is not possible to guarantee the orientation of the modules, so a reduction factor must be applied.

It should also be considered that solar modules are sensitive to the presence of small shadows, even a narrow shadow can significantly decrease the output power. For example shadows generated by vegetation, buildings, daymarks and handrails can cause problems and should be avoided.

In some locations, fouling of the surface may be an issue. In these locations, it is recommended to avoid horizontal placement and that solar panels are installed with an inclination that promotes self‐cleaning. refer to IALA G1039 / 1.1.6 SOLAR PANEL ORIENTATION

## AC connected – IS this used in a marine environment?

Refer to G1039 / 1.1.3 CURRENT ‐ VOLTAGE CURVE

6 - Power tolerance:

This is the amount of power in real output of your solar panel. For example a 165W module with a +/- 5% tolerance could actually produce from 156.75W up to 173.25W.

The best photovoltaic solar panels have a "positive only" power tolerance, which means that you are guaranteed to get at least the specified output power from the panel.

For example: a 200W solar panel with a tolerance of +5% / - 0% will produce a minimum of 200W and a maximum of 210W.

Resistance to earth

Types and quality of the connection cable

Connectors

IP67/68

Junction box (disadvantages, fixing, tests….)

9 - The Boitier by Pass and the cables :

Turn the module over to inspect the finish of the By pass box. It must be siliconized in the correct way and the appropriate cable diameter. Check the By-pass diodes that will allow the solar panel to continue to produce even if there is shade on part of the solar panel.

- •	Plugs

Connecting the cells

Product history

Cable size from JB

- Construction and material of junction box

## Identification of modules

- Date of manufacturing

- Manufacturer

- Electrical performance

# Problems / failures

Use of commercial modules are now starting to be used on island and shore

Water ingress

Diodes

Lightning protection

### If lightning strikes :

-  less than 500m away, overvoltages are induced by magnetic fields on your entire electrical installation.

-  Indirectly: the installations and the various electrical circuits can suffer serious damage.

-  directly: the high current destroys electrical installations with fire risks.

The external protection is used to protect against the direct impacts of lightning. It consists of a lightning conductor system. The lightning conductors capture the lightning and conduct the current to the earth. Long rods made of conductive metal are used which protrude above the photovoltaic installation to be protected.

Interior protection is the use of devices to protect against currents and magnetic fields that can damage interior installations. The essential device is the earthing system, which prevents discharges from passing through the electrical installations. At the photovoltaic installation level it is necessary to :

If your installation is not directly exposed:

-connect the frame of the modules to the earthing circuit.

-connect the frame of the photovoltaic module to the ground by an electric wire on the outside of the building.

-and of course, lead the grounding circuit to the grounding bar using a low impedance device.

If your installation is directly exposed:

connect the frame of the module to the lightning conductor with a wire capable of withstanding the lightning current direct the discharges to the grounding circuit with a lightning arrester installed before the DC input line of the inverter.

For more information about lightning you can use Guideline 1012 Ed 3.

And specifically, Paragraph 7.6.4 SOLAR PHOTOVOLTAIC ARRAYS:

Photo‐voltaic (PV) arrays are vulnerable to lightning damage, particularly where they are located at a distance from the main building. A separate earth termination should be installed locally, connected to the array mounting frame. This should be bonded to the main lightning earth using a bonding conductor of not less than 50 mm2, which should follow closely the route of the DC cables between the photovoltaic array and the main building. When assessing this requirement, the rolling sphere technique (see Table 1) should be used based on the required lightning protection level and taking account of the location of the photovoltaic array.

All cables should be run either on cable tray, in conduit/trunking or tightly against earthed metalwork/conductor tapes.

## Poor connection between cells

Early solar module from the 90s where the connections failed. New production processes have essentially eliminated this.

## Hot spots

Reduction of about 15%

Need more investigation for an example of a hot spot.

## Micro cracking – wind pressure

## Physical Stresses

## Water ingress

## Sealant failure

## Delamination

## Cell corrosion

## Metal corrosion

Dissimilar material corrosion – example from RD around fixing and dissimilar metal in LV

Cosmetic problems only

Difference between good and bad can be difficult to tell

## Poor insulation

Example of conductivity between the solar cell power and the sea as a battery. Poor insulation can have a very rapid impact on the corrosion of the Aluminium. Example show impact after just 2 years.

## Mechanical impacts caused by handling and shock/vibration

## Ice

Peter S has some photos of  solar panels with ice. Peter to send presentation of panels with damage.

Immersion in water and water jetting for cleaning

Solar modules in ice is not often used as the extreme conditions tend to damage the modules.

Wavewash refer to G1136 / 2.2.4. b EXTREME WEATHER EVENTS

## Theft of modules and ways to prevent it

Although in recent years there has been a considerable reduction in the theft of solar modules due mainly to the sharp decline in the purchase costs of panels, the replacement costs due to logistics for modules located in remote and difficult to access locations remains high and represents a very important consideration in the design of a photovoltaic installation. The risk of theft or unauthorised use of photovoltaic modules installed at AtoN sites warrants consideration of an effective anti-theft solution to protect the photovoltaic panels. The most commonly used method for securing solar panels is the use of security fixing screws in the end and mid clamps of the solar mounting system. The fixings require a special insert bit or key wrench to remove the clamps securing the panels to the mounting frame.

Vandalism

Shooting and theft – plexi glass???

Presentation from Adam Hay on vandalism so if we can find out more on this.

## Connector failure and use of connectors and types

# Maintenance and testing

See model course

Cleaning and surface finishes (self cleaning)

## Equipment and measurement devices – Some info from Peter S

Checking performance

Measurement methods

Measurement of solar generators – an example from HT equipment

The measurement of the open-circuit voltage and the short-circuit current gives a first statement about the function of a solar generator. However, defects caused by shading or cell breakage may remain hidden.

Therefore, a complete current-voltage characteristic curve has the greatest significance for the proper functioning of a solar generator. To record such curves, devices are available on the market that allow on-site measurements and subsequent evaluation of the data by PC.

In the following a simple method is shown, with which a

measurement of the solar generator with "household remedy" is possible.

The open-circuit voltage Uoc and the short-circuit current lsc can be measured directly with an appropriate multimeter (caution when measuring the short-circuit current: When removing the measuring tips, an arc can remain if the system voltage > 50 V) is sufficient!)

To record the characteristic curve, the solar generator must be loaded with different resistances. Of course, these must be able to dissipate the resulting power.

Since the operating point of the solar module is typically in the area around the MPP and partial shading has the greatest effect on the characteristic curve there, a few measuring points should be recorded especially here.

The position of the MPP can either be taken from the data sheet or estimated from the open-circuit voltage and short-circuit current as described:

UMPP (0.75 .. 0.9) UoC

IMPP (0.85 ... 0.95) lsc

On/off site

Frequency

Standards

Certification

You have obtained the certificates, certificates of standards, laboratory tests and the quotation, then it will be wise to go through the documents and data sheet of the photovoltaic module and check the following 10 points:

## Life / aging

Replace on age or performance.

Performance over life 90% after 10 years 80% after 15 years.

Performance testing over the life

Refer to IALA G1039 /1.1.2 LIFESPAN

Operational life

Performance life

# Procurement

- How to specify

## Assessment

### The guarantee:

The manufacturer must at least offer you a solar panel with a minimum 25-year guarantee. What is the procedure for replacing my solar panel in case of failure? It is a good idea to ask the installer or the manufacturer if you have difficulty obtaining information on this subject, then it is a bad sign.

### Price list :

The cost of a photovoltaic solar panel is normally expressed in cost per Wc. Example: 0.85 euros/Wp for a 250 Wp solar panel which indicates a unit price of 212.50 euros.

Beware of very low rates on solar panels, it is generally the sign of a minimum quality equipment with sometimes dubious guarantees. Do not hesitate to ask for several quotes from several distributors or installers in order to compare.

### Manufacturer

Try to find out about the reputation of the solar panel manufacturer in search engines. How long has it been in the photovoltaic field, see the design of the website and the aspects dealing with the guarantee.  It is wise to see the exchanges on the forums concerning the manufacturer's brand, are they positive or negative?A guarantee of reliability:

The standards are a guarantee of reliability for photovoltaic solar modules, so installers and manufacturers are able to provide you with quality certificates for the solar panels they offer. There is also the possibility to download the certificates and test certificates directly from the manufacturer's website, for example the certificates for the manufacturer Qcells.

The TUV certificate ensures that the photovoltaic module has passed the rigorous tests carried out by the German TUV (Technischer Überwachungsverien) laboratory proving its resistance to extreme temperatures, accelerated ageing cycles, violent projections and fire.he quality of photovoltaic solar panels:

The quality of the photovoltaic solar panels is an important factor to consider for any rooftop or ground-mounted solar power plant project. Indeed, the quality of the chosen photovoltaic modules will determine the payback time of your solar power plant by guaranteeing you an optimum production of solar energy in the long term.

# Recycling and repurposing

Use after performance drops below 80% of there output.

# Standards

List of standards

The manufacture of photovoltaic modules is governed by several standards.required by the IEC (International Electrotechnical Commission) in order to be sold on the international market.

These standards are as follows:

The IEC 61215 (crystalline) or IEC 61646 (thin film) standard certifies a guarantee of quality in terms of compliance with electrical parameters and mechanical stability. The requirements of this standard refer to the design qualification and approval of photovoltaic modules for terrestrial application and long-term use.

The IEC 61730 standard specifically deals with the prevention of electric shocks, the risk of fire, and the use of the photovoltaic modules in the field of photovoltaic systems and personal injury accidents due to mechanical and environmental stress.

This standard, which deals specifically with the safety aspects of the modules, complements IEC 61215, which sets the electrical performance.

# DEFINITIONS

Suggested text: The definitions of terms used in this IALA Guideline can be found in the International Dictionary of Marine Aids to Navigation (IALA Dictionary) at http://www.iala-aism.org/wiki/dictionary and were checked as correct at the time of going to print.  Where conflict arises, the IALA Dictionary should be considered as the authoritative source of definitions used in IALA documents.

# ACRONYMS

IMO	International Maritime Organization (Acronym style)

# REFERENCES

Abcd

Efgh

# documentation

## proofs

## references

## datasheet

Body text (To assist in the use of this guideline, the following acronyms and definitions have been used:)

## (Example Heading level 2)

Body text

## (Example Heading level 2)

Body text

# AIMS AND OBJECTIVES (Example Heading level 1)

Body text (left justified)

Body text (left justified)

List 1.

List1.

List 1 text (for subsequent text at the same level).

List 1:

List a.

List a.

List a text (for subsequent text at the same level).

List a:

List i.

List I text (for subsequent text at the same level).

Bullet 1;

Bullet 1 text (for subsequent text for the same bullet).

Bullet 1:

Bullet 2;

Bullet 2 text (for subsequent text for the same level).

Bullet 2:

Bullet 3;

Bullet 3 text (for subsequent text for the same level)

Bullet 3.

# Example Heading level 1

Body text

## (Example Heading level 2)

Body text

Rg=2.03h0+Hm

Geographical range

Where:

Rg is the geographical range (nautical miles) (alternatively NM)

ho is the elevation of observer’s eye (metres) (alternatively m)

Hm is the elevation of the mark (metres) (alternatively m)

### (Example heading level 3)

Body text.

E=mc2

Theory of Special Relativity

Where:

E is the kinetic energy (Joules) (alternatively J)

m is the mass (kilograms) (alternatively Kg)

c is the speed of light (metres/second) (alternatively m/s)

#### (Example heading level 4)

Body text.

# Example Heading level 1

Body text.  Bullets have only one sentence.  Anything further needs to appear in the relevant 'bullet text' style.

Bullet 1:

Bullet 1:

Bullet 1.

## TABLES

Body text

Example of a table caption; table with the significant information in the first column

| Table heading | Table text |
| --- | --- |
| Table heading | Table text |
| Table heading | Table text |
| Table heading | Table text |
| Table heading | Table text |
| Table heading | Table text |

Example of a table caption; table with the significant information in the first row

| Table heading | Table heading | Table heading |
| --- | --- | --- |
| Table text | Table List 11 - Table list a Table list i | Table text |
| Table text | Table text | Table text |
| Table text | Table text | Table text |
| Table text | Table text | Table text |

Example of ‘normal text’ following a Table

Example of a table caption; table with coloured rows

| Table heading | Table heading | Table heading |
| --- | --- | --- |
| Table text | Table text | Table text |
| Table text | Table text | Table text |
| Table text | Table text | Table text |
| Table text | Table text | Table text |
| Table text | Table text | Table text |
| Table text | Table text | Table text |

Note:  Colours for text and cell shading need to be selected from the permitted palette (see ANNEX C)

# FIGURES

Example figure caption

Another example figure caption

# DEFINITIONS

Suggested text: The definitions of terms used in this IALA Guideline can be found in the International Dictionary of Marine Aids to Navigation (IALA Dictionary) at http://www.iala-aism.org/wiki/dictionary and were checked as correct at the time of going to print.  Where conflict arises, the IALA Dictionary should be considered as the authoritative source of definitions used in IALA documents.

# ACRONYMS

IMO	International Maritime Organization (Acronym style)

# REFERENCES

Abcd

Efgh

EXAMPLE OF AN ANNEX - LANDSCAPE

Body text

example of ANNEX heading level 1

Body text

example of annex heading level 2

Body text

Example of annex heading level 3

Body text

Example of Annex heading level 4

Body text

Example table caption

| No | Title/Topic | IMO References | Requirements | Possible Audit Questions | Remarks |
| --- | --- | --- | --- | --- | --- |
| 1 | Table text | Table text | Table text | Table text | Table text |
|  |  | Table text | Table text |  |  |
|  |  | Table text | Table text |  |  |

EXAMPLE OF AN APPENDIX TITLE

APPENDIX HEADING 1

Body text

APPENDIX HEADING 2

Body text

APPENDIX HEADING 3

Body text

Appendix Heading 4

Body text

(EXAMPLE ANNEX TITLE)

Introduction (Example Annex Heading 1)

Body text.

Example of ANNEX HEADING Level 2

Body text

Example of annex heading level 3

Body text

Example of Annex heading level 4

Body text

PERMITTED COLOUR PALETTE

The IALA colour palette is divided in 3 palettes of different level of hierarchy that has to be respected.

Corporate colours (Not shown)

IALA’s corporate colour palette is directly inspired from the colours in our logotype:

- dark blue

- white

- yellow

- gradient blue

Primary & secondary colours

The primary colours are to be applied in complement with the corporate colours.

This second level of colours gives rhythm and helps to segment our publications.

The secondary colours are used to highlight information, titles in a minor proportion only.

These colours can’t be replaced by other tints.

PANTONE PROCESS CYAN C CMYK : C 100

RGB : R 0 - G 159 - B 223

CMYK : 50 % OF THE TONE RGB : R 131 - G 208 - B 245

CMYK : 50 % OF THE TONE RGB : R 148 - G 217 - B 213

CMYK : 50 % OF THE TONE RGB : R171 - G 219 - B 233

CMYK : 50 % OF THE TONE RGB : R 178 - G 193 - B 237

PANTONE 326C CMYK : C 81 - Y 39

RGB : R 0 - G 175 - B 170

PANTONE 7703 C

CMYK : C 79 - M 2 - Y 10 - K 11

RGB : R 0 - G 181 - B 208

PANTONE 660 C CMYK : C 88 - M 50

RGB : R 64 - G 126 - B 201

CMYK : 20 % OF THE TONE RGB : R 212 - G 237 - B 252

CMYK : 20 % OF THE TONE RGB : R 213 - G 240 - B 237

CMYK : 20 % OF THE TONE RGB : R 216 - G238 - B 245

CMYK : 20 % OF THE TONE RGB : R 218 - G 223 - B 246

PANTONE 258 C CMYK : C 51 - M 79

RGB : R 153 - G 80 - B 159

CMYK : 50 % OF THE TONE RGB : R 201 - G 169 - B 208

CMYK : 50 % OF THE TONE RGB : R 183 - G214 - B 155

CMYK : 50 % OF THE TONE RGB : R 246 - G 174- B 135

CMYK : 50 % OF THE TONE RGB : R 157 - G 157 - B 156

PANTONE 739 C

CMYK : C 78- Y 95- K 5

RGB : R82 - G 174 - B 50

PANTONE 2347 C

CMYK :M 88 - Y 100

RGB : R 230 - G 56 - B 17

PANTONE COOL GRAY 11 C CMYK : K 100

RGB : R 87 - G 87 - B 86

CMYK : 20 % OF THE TONE RGB : R 232 - G 221 - B 288

CMYK : 20 % OF THE TONE RGB : R226 - G 238 - B 217

CMYK : 20 % OF THE TONE RGB : R 253 - G 224- B 208

CMYK : 20 % OF THE TONE RGB : R218 - G 218 - B 218

CMYK : 10 % OF THE TONE RGB : R 237 - G 237 - B 237

Guideline

Recommendation

Model Course

PRIMARY COLOURS

SECONDARY COLOURS

Example footnote

Example of footnote