Input paper:	     ENG2-9.8

Input paper for the following Committee(s): 	check as appropriate		Purpose of paper:

□  ARM	X  ENG		□  PAP					□   Input

□  ENAV	□  VTS							X   Information

Agenda item			9

Technical Domain / Task Number	TD#1

Author(s) / Submitter(s)			Dr. Ju-Seop Han / Korea Association of Aids to Navigation

# Analysis of the causes of deterioration to LED lanterns

This paper provides the additional information of research of degradation characteristics of LED lanterns with using time. The details are as follows;

- Red LED Lantern : 32% reduction(initial luminous intensity), pass(regular inspection, 3years)

- Green LED Lantern : 21% reduction(initial luminous intensity), pass(regular inspection, 3years)

- Yellow LED Lantern : 47% reduction(initial luminous intensity), fail(regular inspection, 3years)

- White LED Lantern : 79% reduction(initial luminous intensity), fail(regular inspection, 3years)

The white and yellow LED Lantern were analyzed for optical and electrical properties in KOPTI (KOLAS).

Fig. 1 Photograph of analyzed LED Lanterns

The luminous intensity was measured using a Goniometer (horizontal angle: 0 ~ 360, 16points, vertical angle: 70 ~ 110, 41points). The spectrum was measured using a Spectrometer (horizontal angle: 0 ~ 360, 16points, vertical angle: 85 ~ 95, 11points). Lens transmittance was compared with the transmittance of the lens between the laser light source and the detector. Optical characteristics of the LED Package was measured using an integrating sphere at the rated current.

From the results, the luminous intensity did not meet the regular inspection standards and The horizontal distribution of lanterns is large deviation.

- Yellow LED Lantern : min. luminous intensity 221.3cd, max. luminous intensity 306.6cd

Fig.2 Polar Luminous Intensity Distribution         Fig. 3 Cone Intensity Distribution

- White LED Lantern : min. luminous intensity 78.8cd, max. luminous intensity 111.5cd

Fig.4 Polar Luminous Intensity Distribution         Fig. 5 Cone Intensity Distribution

When the Transmittance after the injection molding of the PMMA material used for the lens is considered to be about 90-94%, the measured Lens transmittance were good.

| Type | Yellow LED Lantern | White LED Lantern | Remark |
| --- | --- | --- | --- |
| Lens transmittance | 86.70% | 92.26% |  |
| Lenz |  |  | Center |

Test samples are LED Package16s(same stage).

| Type | Luminous flux |  | Remark |
| --- | --- | --- | --- |
|  | Yellow LED Lantern | White LED Lantern |  |
| Min. | 1.57 | 0.34 |  |
| Max. | 2.57 | 1.00 |  |
| Avg. | 1.94 | 0.60 |  |
| Deviation(min/max) | 38.6% | 66.3% |  |

Fig. 6 Wavelength of the LED Packages

From the results of the measuring the LED Packages, the deviation of the luminous flux between the LED packages was confirmed to significantly appear. Therefore, the deterioration of the LED Package is considered the cause of reduction to the luminous intensity of the LED Lanterns.