IALA Guideline 1006

On

Plastic Buoys

Edition XX

April  2008

Draft report from Floataid Workshop Brest, 2008

20ter, rue Schnapper, 78100

Saint Germain en Laye, France

Telephone: +33 1 34 51 70 01 Fax: +33 1 34 51 82 05 E-mail - iala-aism@wanadoo.fr	Web site : iala-aism.org

Document Revisions

Revisions to the IALA Document are to be noted in the table prior to the issue of a revised document.

| Date | Page / Section Revised | Requirement for Revision |
| --- | --- | --- |
| December 2005 | Entire document | Reformatted to reflect IALA documentation Hierarchy |
| April 2008 | Entire document except foam buoys | Floataid Brest 2008 |

Table of Contents

Guidelines On Plastic Buoys

# 1 INTRODUCTION

A plastic buoy may be defined as a floating aid with at least the hull being constructed of a plastic material.

Plastic buoys have been in production for over 20 years. They are produced in various materials and designs. Initially they were produced as small sizes, but nowadays there are several manufacturers producing plastic buoys in sizes up to and in excess of 3m diameter.

# 2 BACKGROUND

Many types of plastic buoys are on the market ranging from small harbour or river markers, to large offshore buoys.

It is suggested that plastic buoys have several advantages over conventional steel buoys including; light weight handling, corrosion resistance, low maintenance, and in some cases, lower costs. However, these apparent advantages need careful evaluation.

- Light weight buoys need careful design to avoid having a rapid rolling or pitching motion detracting from their navigational effectiveness in waves, wind and current.

- A well-manufactured buoy using high-quality pigment within IALA chromaticity standards, and virgin material, should retain an acceptable surface colour for the design life of the buoy, which can be in excess of 15 years in most climatic conditions. However, high ultra violet exposure will accelerate the ageing process.

- Some plastic materials may have better resistance to dense marine fouling than other buoy types. Plastic buoys must be sufficiently robust to withstand weed being scraped off, or high pressure water jetted, regularly during the working life of the buoy.

- The purchase cost of plastic buoys is dependent on the technology. Whole of life costs may be less than steel types, however users should carefully assess their requirements with costs factors.

- Plastic buoy technology offers increased flexibility to incorporate new design developments.

- Some plastic spar buoys are particularly adaptable to certain ice conditions

- The mooring eye (or eyes) will usually be metal and must thus be fastened or moulded into the buoy by some means.

- Handling plastic buoys may require different methods. The safe working load on plastic buoys may be less than steel types.

- Major service intervals will be governed by the life expectancy of the metals used in the buoy assembly.

- Sea-based maintenance can be achieved on most plastic buoys, including jet washing and other normal service tasks. Various maintenance procedures are suitable for different plastic materials. A full guideline is available under IALA-1040 – The Maintenance of Buoys and Small Aids to Navigation Structures, April 2008.

- The metal components will require a more intensive maintenance regime (eg mooring eye).

- It may be necessary to incorporate an earthing strap on large plastic buoys to prevent the buildup of static electricity, which may cause shock or damage electronic equipment.

# 3. Buoy Construction-Materials

Plastic buoys may be grouped into 4 basic types which are listed with comments on their design and construction.

## 3.1 POLYETHYLENE (Fiqs 4&5&?),

### 3.1.1 General

This is well-known technique that has been widely used to manufacture many types of buoys, in rotationally moulded or extruded polyethylene. Some manufacturers may then fill the buoy with foam or polystyrene.

The polyethylene material may be linear (low, medium or high-density) or crosslinked. The linear material has the advantage that it can be melted and hence repaired by hot fusion welding. The polyethylene material used in buoy manufacture is usually linear.

The polyethylene provides poor adhesion for conventional paints, but specialized hot plastic spraying processes are available. When colour is moulded-in, pigments must be of the highest quality suitable for marine use and UV exposure.

The rotomoulding process is also used to manufacture buoyancy modules which are attached to a structural core which may be in the form of a buoy or a resilient beacon.

The manufacturing process has been developed in recent years to allow the production of large floats (3m diameter) with wall thickness in the order of 10mm which are now being used as the buoyancy element of substantial buoys. These floats may be manufactured in four segments to simplify handing and transport and allow a reserve of buoyancy should one segment be damaged.

### 3.1.2 Construction

Manufacturers typically construct polyethylene buoys from either 1-piece plastic, modular plastic, or hybrid metal/plastic designs. Generally, small buoys are made in 1-piece, while larger types may be modular or hybrid designs.

Polyethylene material will expand and contract with ambient temperatures. Care should be taken in the design characteristics to ensure compatibility between different materials (ie elongated or oversized clearance holes).

- Filling

To prevent the buoy sinking the buoy may be divided into separate watertight segments, which may be filled with foam or polystyrene. If foam is used it must be of the highest quality closed-cell specification to prevent water absorption. Filling material should be of sufficient quality to survive the expected lifetime of the buoy. Some disadvantages may exist in the use of filling. Some polyurethane foam types may prohibit recycling of the polyethylene.

- Fasteners

In the manufacturing process, care should be taken to ensure the threaded inserts are fixed and aligned correctly in the material, otherwise they should be avoided.

Care must be taken when using threaded inserts to avoid detachment of the insert with the polyethylene.

It is desirable to use non corrosive fasteners including; hot-dipped galvanized steel, marine-grade aluminium, marine grade stainless steel or bronze.

It is important that any high loads are distributed throughout the structure of the buoy and not concentrated in small areas of the skin. One solution to avoid these stresses may be to interconnect the mooring and lifting points.

- Quality Control

The manufacturing materials must be carefully specified and certification obtained from the manufacturer to ensure that correct quality virgin materials and UV stabilizers (in pigment & polyethylene) have been used.

### 3.1.4 Repair & Maintenance

Linear polyethylene can be easily repaired by trained technicians using hot fusion welding equipment in required colours.

Maintenance procedures are outlined in IALA 1040 –

### Health & Safety

Reference to available material datasheets should be made prior to any repairs conducted, in regards to handling of the polyurethane filling material used (disposal, fusion welding etc).

### 3.1.6 Disposal

Linear thermoplastics can be recycled, however it must be possible to separate any metal components and impurities (marine growth / paint etc) from the plastic, and remove any internal filling.

The light weight of the plastic buoy is probably the major advantage for many authorities. If a buoy of a certain size is required the limited lifting capacity of the available servicing vessel may force the authority to use a lightweight plastic buoy.

If a steel buoy can be handled by servicing vessels, either by lifting or by towing to station, then the local availability of long term maintenance facilities must be considered before the whole life costs of equivalent plastic and steel buoys can be investigated.

- For large buoys, the first cost of plastic buoys may, in some areas of the world, maybe equal or less than the cost of a steel buoy however any cost advantage needs to be considered as part of the whole life cost of the buoy. The shorter potential life of the plastic buoy must be compared with the much longer (typically over 40 years) life of a regularly maintained steel buoy.

Small plastic buoys have the advantages when compared with steel of light weight, minimum servicing requirements within their planned life span and ease of handling by the smaller type of service craft with which they are associated.

## 3.2 GRP OR FIBREGLASS (Fiq 4)

### 3.2.1 General

GRP is the usual abbreviation for glass reinforced plastic which in its most common form consists of glass matt bonded by polyester resin. As many commonly available types of glass fibre and polyester resin have limited resistance to extended immersion in water.

### 3.2.2 Construction

Complex shapes can be easily produced by laying-up resin and glass reinforcement into a mould by hand (or spray machine). The cylindrical buoy body is usually formed by joining two half body shapes. It is important to note that the join is often the weakest area of the body.

The strength of GRP is basically dependent of the ratio of glass fibre to resin and thus this is another area which requires definition and quality control. High strength (required in ice conditions) can be achieved by the use of carbon or Kevlar fibres, but their costs may be high. These fibres may be used in specific stress areas of the buoy.

The outer layer of resin, the gel coat, prevents water absorption into the glass reinforcement and must be protected from mechanical damage. This is usually provided by some form of fendering.

- Filling

In the event of a collision, a GRP buoy may well crack from an impact which would only dent a steel buoy. To prevent the buoy sinking the buoy should be divided into separate watertight compartments or filled with foam or polystyrene. If foam is used it must be of the highest quality closed-cell specification. If the foam is porous it may absorb water over a long period of time and increase the weight of the buoy to such an extent that it cannot be lifted by the servicing craft, or the buoy may sink.

- Fasteners

Care must be taken when bonding metal attachment points into GRP due to the considerable difference in expansion rates between metals and plastics, and the inherent flexibility of the GRP. Another option is to use through-bolted fixings with generous backing plates and resilient washers or coatings between the metal and the GRP.

It is desirable to use non corrosive fasteners including; hot-dipped galvanized steel, marine-grade aluminium, marine grade stainless steel or bronze.

Similar problems may exist with the fastening of lifting eyes and tower type superstructures. It is important that any high loads are distributed throughout the structure of the buoy and not concentrated in small areas of the skin. One solution to

this problem is to incorporate a central (usually steel) spine to connect the mooring eyes, lifting eyes and superstructure.

- Quality Control

The manufacturing materials must be carefully specified and certification obtained from the manufacturer to ensure that correct quality materials have been used. Confirmation must also be obtained that laminating and curing has taken place in the correct environment.

### 3.2.3 Repair & Maintenance

GRP buoys will require cleaning and repainting and any necessary repair to the gel coat.

Repair of GRP is usually straightforward but does require standards of cleanliness and recommended working temperatures. Effective drying of damaged laminates or foam cores may also be difficult in cold climates. It may be necessary to use heaters to warm and dry damage areas and to ensure effective curing of the repair.

The final surface colour of GRP buoys can be incorporated into the gel coat, but if not the buoys will require normal painting to achieve required surface colours at the beginning of their service life.

GRP buoys may be cleaned onsite using water jet, however care should be taken to ensure paint flakes and surface materials avoid polluting the surrounding environment.

### 3.2.4 Handling

Care should be taken to avoid damage to the GRP through shock due to its rigidity.

### 3.2.5Recycling / Disposal

GRP is a recyclable material?

### 3.2.6Heath & Safety

The use of laminating resins and solvents is subject to increasing control by health and safety regulations.

## 3.3 URETHANE COATED FOAM (Fiq 5):

### 3.3.1 General

These buoys typically consist of a flexible urethane elastomer skin (up to 10mm) on a flexible closed cell foam core. They have the advantage of overall flexibility and resilience. The flexibility will also be an advantage when the buoy has to be lifted or serviced in rough weather.

### 3.3.2 Construction

The buoys are usually manufactured by spraying the urethane skin material onto a shaped foam core and can thus be made to almost any required shape without the need for an expensive mould.

The points noted regarding mooring eyes on GRP buoys apply equally to these buoys.

The concept of a central structure steel spine between the mooring and lifting eyes is commonly employed.

In the manufacturing process, consideration must be taken into the attachment or the interface between the flexible skin and steel mooring eyes. This requires particularly careful design to prevent water penetration into the foam or tearing of the skin.

The quality of the skin and foam materials is of the utmost importance. The consequences of failure of the skin are self evident but poor quality foam may absorb water through an apparently sound skin or may simply shrink, resulting in a wrinkled buoy with a considerable loss of buoyancy!

- Filling

- Fasteners

- Quality control

### 3.3.3 Repair &maintenance

Urethane may be repaired with two component pouring or trowelling compounds. Correct working conditions are critical (temperature and humidity) and detailed health and safety precautions must be observed.

### 3.3.4 Maintenance

For urethane coated foam buoys, maintenance will entail cleaning and repainting, but it should be noted that urethane paint presents health and safety problems.

3.4 ALL FOAM (Fig.6) 3.4.1 Construction

These buoys are usually constructed by wrapping closed-cell foam around a central structural core, the layers of foam being heat sealed together during the wrapping process. A major US manufacturer uses ionomer foam which is produced in sheet form. The outer layer of the rolled foam shapes can be "densified" through the application of pressure and heat to make a hard, smooth surface. Pigments are usually incorporated into the foam during the extrusion process, so the colour is continuous throughout the entire hull and daymark. The buoys include a structural steel framework, steel lifting and mooring eyes, and stainless steel connecting hardware. Internal radar reflectors can be mounted in the daymarks.

The manufacturing technique particularly lends itself to the production of "one off' designs as a variety of body shapes can be made without the need for a mould. Buoys of this type are significantly lighter than steel buoys of the same size.

- Filling

- Fasteners

- Quality control

3.4 2 Use

The life and durability of the buoy is entirely dependant on the quality of the foam used. The flexibility of the foam can provide good impact resistance but resistance to aggressive abrasion is not good. This last factor is important for buoys which will dry out on a hard bottom at a tidal site or may be subject to moving ice conditions.

A foam buoy hull can sustain considerable damage or loss of material without sinking.. A damaged buoy may be repaired or recycled by the manufacturer. Other advantages of foam buoys include their lighter weight which may result in good performance in fast water.

### Appendix 1

Advantages:

- The plastic does not corrode.

- It is easier to maintain; only removal of marine growth, no painting on station.

- The complete maintenance can be carried out at sea.

- There is less maintenance on shore for the plastic component (no grit blasting, no painting with the exception of GRP) therefore less resources may be utilised.

- Plastic buoys are of lower weight (1/2 to 1/3 mass of the equivalent diameter steel buoys). Therefore, the service may be able to use smaller buoy tender.

- Whole of life costs may be less than steel types.

- France and The Netherlands, amongst others, have more than 15 years experience of operating rotationally moulded polyethylene (PE) plastic buoys successfully.

- There are a number of commercial companies offering large rotationally moulded plastic buoys.

- Most plastic is recyclable.

- Where plastic buoys are of modular construction, it is possible to change individual parts or segments if they are damaged or need refurbishment.

- Large modular buoys are easier to transport and store, as parts can be disassembled for transit.

- The number of spare parts held can be reduced.

- It is possible to encase a radar reflector within a plastic buoy’s superstructure.

Disadvantages:

- Due to the lighter weight of plastic buoys, there may be more motion on station, however this may be mitigated in the design.

- It is more difficult to change the colour of a plastic buoy, as conventional painting is not reliable. This may increase the number of spares needed, compared with steel buoys, i.e. red, green, black and yellow spares may have to be kept in stock rather than re-painting steel components.

- On current estimates, plastic buoys have a shorter lifetime than steel buoys.

Plastic buoy components will be specific to each manufact

BOLT ON MOORING EYE

LIFTING EYE

L

TAIL TUBE

STAINLESS STEEL THIMBLE TO PROTECT MOORING EYE

BALLAST