EEP12-output-17

Formerly EEP10 / WG3 / WP4

PRODUCT CERTIFICATION TEMPLATE 4d

Buoy Sinkers

Purpose

Product templates identify parameters that should be tested and measured and the standards against which each parameter should be tested and measured to enable a comprehensive evaluation of products.

Scope

This template is applicable for sinkers used for mooring aids to navigation buoys.

Applicable Documents, Recommendations, and Guidelines

IALA Documents

- 1. IALA Guideline 1059, On Float Aid Moorings

- 2. IALA Guideline 1036, On Environmental Considerations in Aids to Navigation Engineering

Test Standards

The Templates quote national and/or international standards. If the manufacturer wishes to use an alternative standard, it is the responsibility of the manufacturer to confirm that the standard used conforms to the IALA quoted standard. Where no test standard is mentioned, the manufacturer shall state the test standard used, preferably with reference to international or national standards.

EEP12-output-17

Formerly EEP10 / WG3 / WP4

Product Certification Template 4d – Buoy Sinkers

Product Type / Manufacturer Name and Reference Number:

| Para No. | Parameter Category | Parameter | Measured Value | Test Method | Comments |
| --- | --- | --- | --- | --- | --- |
| 1 | Physical |  |  |  |  |
|  | 1.1 | Material (steel or cast iron) | Chemical composition | The manufacturer shall provide material certifications indicating the heat number, material designation, chemical composition, and quantity of material represented by the certification. The certification shall also be provided for the material used for the sinker bail (mooring eye). | Each sinker offered by the manufacturer shall be traceable to the heat of steel or cast iron from which it was made. Serial numbers traceable to the heat of steel or cast iron shall be permanently marked on the sinkers (see 1.7 below). |

| Para No. | Parameter Category | Parameter | Measured Value | Test Method | Comments |
| --- | --- | --- | --- | --- | --- |
|  | 1.2 | Material (concrete) | Mix design | The manufacturer shall provide certifications which describe the mix of concrete used, its material properties, and the results of relevant tests (e.g., slump test, pull-out test, etc.). Evidence of successful use of the same type of concrete in a marine environment shall also be provided. | The concrete shall be suitable for use in a marine environment. Each sinker offered by the manufacturer shall be traceable to the mix of concrete from which it was poured. Serial numbers to permit this traceability shall be permanently marked on the sinkers (see 1.7 below). |

| Para No. | Parameter Category | Parameter | Measured Value | Test Method | Comments |
| --- | --- | --- | --- | --- | --- |
| 1.3 |  | Strength of Sinker Bail (Mooring Eye) | lb and/or kg | The manufacturer shall propose a suitable method of conducting this test. | The manufacturer shall indicate the load that the sinker bail (mooring eye) can withstand without rupture, deformation, or stretching beyond the dimensional tolerances of the sinker bail (mooring eye). Each sinker offered by the manufacturer shall have been tested to this load, and the manufacturer shall certify that the products successfully passed the test. The actual test data shall be provided upon request. The test equipment shall have been calibrated to International Standards within 12 months prior to the testing, and certification to this effect shall be made available upon request. |

If the mooring eye has been heat treated after bending to shape then details of the heat treatment process must be provided along with records of the treatment oven temperatures and the time that the eye is maintained at temperature.Hardness and impact tests may be carried out on material samples taken from the heat treated eye to ensure that the heat treatment process has been effective.

| Para No. | Parameter Category | Parameter | Measured Value | Test Method | Comments |
| --- | --- | --- | --- | --- | --- |
| 1.4 |  | Weight | lb and/or kg | The manufacturer shall propose a suitable method of conducting this test. | The manufacturer shall indicate the nominal weights of the sinkers offered. The manufacturer shall then weigh each sinker to determine its actual weight. The nominal weight and actual weight shall be permanently marked on the sinkers (see 1.7 below). The test equipment shall have been calibrated to International Standards within 12 months prior to the testing, and certification to this effect shall be made available upon request. |
| 1.5 |  | Dimensions | in and/or mm | Visual inspection | The manufacturer shall indicate the dimensions of the products offered, and the respective tolerances, and certify that the products have been measured and are in conformance with these values. |

| Para No. | Parameter Category | Parameter | Measured Value | Test Method | Comments |
| --- | --- | --- | --- | --- | --- |
| 1.6 |  | Surface quality |  | Visual inspection | Sinkers shall be free from adhering sand, scale, and other foreign material. Sinker bails (mooring eyes) shall be free from mill defects, burrs, slag, weld spatter, or rough surfaces which might present a safety hazard or interfere with proper performance. Particular attention should be paid to any surface cracking that may indicate bending at incorrect temperatute. |
| 1.7 |  | Marking |  | Visual inspection | The nominal weight and actual weight shall be marked on the sinker (see 1.4 above). In addition, the sinker shall be marked with the manufacturer's name or trademark, the year of manufacture, and a unique serial number by which the sinker can be traced back to the heat of steel or iron, or pour of concrete, from which it was made (see 1.1 and 1.2 above). The marking shall be by casting, welding, inscribing, or other suitable method resulting in a permanent marking. Painting or stencilling shall not be used. The manufacturer shall inspect the products offered and certify compliance with this requirement. |

| Para No. | Parameter Category | Parameter |  | Measured Value |  | Test Method |  | Comments |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 2 | Disposal and recycling |  |  |  |  |  |  |  |  |
| 2.1 |  |  | Recycling |  |  |  |  | The manufacturer shall indicate whether the products are recyclable. The manufacturer shall state if it will undertake the recycling of the products. Reference IALA Guideline 1036. |  |
| 2.2 |  |  | Disposal |  |  |  |  | The manufacturer shall state any material content that would harm the environment if the products are disposed of as normal waste. Reference IALA Guideline 1036. |  |
| 3 | Safety |  |  |  |  |  |  |  |  |
| 3.1 |  |  | Worker safety |  |  |  |  | The manufacturer shall state any special requirements to ensure workers’ safety in the use of the products. |  |

 Where no test standard is mentioned, the manufacturer shall state the test standard used, preferably with reference to international or national standards.









