EEP12-output-18

Formerly EEP10 / WG3 / WP3

PRODUCT CERTIFICATION TEMPLATE 4c

Buoy Shackles and Swivels

Purpose

Product templates identify parameters that should be tested and measured and the standards against which each parameter should be tested and measured to enable a comprehensive evaluation of products.

Scope

This template is applicable for steel shackles and swivels used as mooring fittings on aids to navigation buoys.

Applicable Documents, Recommendations, and Guidelines

IALA Documents

- 1. IALA Guideline 1059, On Aid to Navigation Moorings

- 2. IALA Guideline 1036, On Environmental Considerations in Aids to Navigation Engineering

Test Standards

The Templates quote national and/or international standards. If the manufacturer wishes to use an alternative standard, it is the responsibility of the manufacturer to confirm that the standard used conforms to the IALA quoted standard. Where no test standard is mentioned, the manufacturer shall state the test standard used, preferably with reference to international or national standards.

EEP12-output-18

Formerly EEP10 / WG3 / WP3

Product Certification Template 4c – Buoy Shackles and Swivels

Product Type / Manufacturer Name and Reference Number:

| Para No. | Parameter category | Parameter | Measured Value | Test Method∗ | Comments |
| --- | --- | --- | --- | --- | --- |
| 1 | Physical |  |  |  |  |
| 1.1 |  | Material | Chemical composition | The manufacturer shall provide material certifications from the steel mill for each heat of steel used. The certifications shall indicate the heat number, steel designation, chemical composition, and quantity of steel represented by the certification. | Each shackle and each swivel offered by the manufacturer shall be traceable to the heat of steel from which it was made. Serial numbers traceable to the heat of steel shall be stamped or engraved on these products (see 1.6 below). |

∗ Where no test standard is mentioned, the manufacturer shall state the test standard used, preferably with reference to international or national standards.

| Para No. | Parameter category | Parameter | Measured Value | Test Method | Comments |
| --- | --- | --- | --- | --- | --- |
| 1.2 | Proof strength |  | lb and/or kg | Shackles and swivels shall be proof tested assembled. These items may be proof tested individually or in a series. When shackle pins are to be furnished alone, they may be proof tested individually, or by inserting them into shackle bodies of the appropriate class and tested as assemblies. Application of the proof load shall be at the centerline of the sample. The diameter of the attachments used in the proof tests shall not be greater than the size of the sample being tested. The proof load shall be applied, and the items subsequently inspected to ensure the products successfully passed the test. | The manufacturer shall indicate the load that the shackles and swivels can withstand without rupture or deformation beyond the dimensional tolerances of the products. Each shackle and each swivel offered by the manufacturer shall have been tested to this load, and the manufacturer shall certify that the products successfully passed the test. The actual test data shall be provided upon request. The test equipment shall have been calibrated to International Standards within 12 months prior to the testing, and certification to this effect shall be made available upon request. |

| Para No. | Parameter category | Parameter | Measured Value | Test Method∗ | Comments |
| --- | --- | --- | --- | --- | --- |
| 1.3 |  | Breaking strength | lb and/or kg | A sample number of shackles and swivels shall be break tested assembled. When shackle pins are to be furnished alone, they may be break tested individually, or by inserting them into shackle bodies of the appropriate class and tested as assemblies. Application of the breaking load shall be at the centerline of the sample. The diameter of the attachments used in the proof tests shall not be greater than the size of the sample being tested. The samples shall be brought to the breaking load and held for 15 seconds. The highest load applied to each sample shall be recorded. | The manufacturer shall indicate the load that the shackles and swivels can withstand for a minimum of 15 seconds without rupture. Samples of the shackles and swivels from each heat of steel shall be subjected to this load, and the manufacturer shall certify that the samples successfully passed the test. The actual test data shall be provided upon request. The test equipment shall have been calibrated to International Standards within 12 months prior to the testing, and certification to this effect shall be made available upon request. |

| Para No. | Parameter category | Parameter | Measured Value | Test Method∗ | Comments |
| --- | --- | --- | --- | --- | --- |
| 1.4 |  | Dimensions (length, width, bar diameter) | in and/or mm | Visual inspection | The manufacturer shall indicate the dimensions of the products offered, and the respective tolerances, and certify that the products have been measured and are in conformance with these values. |

If the shackes or swivels have been heat treated after manufacture then the details of the heat treatment process must be provided along with records of the treatment oven temperature and the times that the components are maintained at  temperature. Hardness and impact tests may be carried out on material samples taken from a sample number of shackles to ensure that the heat treatment process has been effective and uniform.

| Para No. | Parameter category | Parameter | Measured Value | Test Method∗ | Comments |
| --- | --- | --- | --- | --- | --- |
| 1.5 |  | Surface quality |  | Visual inspection | All items shall be free from mill defects, burrs, slag, weld spatter, or rough surfaces which might present a safety hazard or adversely affect their serviceability and handling. The manufacturer shall inspect the products offered and certify compliance with this requirement. Shackles and swivels are often furnished in their natural color and finish. If a coating or other finish is used, the manufacturer shall describe the purpose and function of the material. |

| Para No. | Parameter category | Parameter | Measured Value | Test Method∗ | Comments |
| --- | --- | --- | --- | --- | --- |
| 1.6 |  | Marking |  | Visual inspection | Shackles and swivels shall be legibly and permanently stamped or engraved with the manufacturer's name or trademark, the year of manufacture, and a unique serial number by which the item can be traced back to the heat of steel from which is was made (see 1.1 above). The manufacturer shall inspect the products offered and certify compliance with this requirement. |

| Para No. | Parameter category | Parameter | Measured Value | Test Method∗ | Comments |
| --- | --- | --- | --- | --- | --- |
| 2 | Disposal and recycling |  |  |  |  |
| 2.1 |  | Recycling |  |  | The manufacturer shall indicate whether the products are recyclable. The manufacturer shall state if it will undertake the recycling of the products. Reference IALA Guideline 1036. |
| 2.2 |  | Disposal |  |  | The manufacturer shall state any material content that would harm the environment if the products are disposed of as normal waste. Reference IALA Guideline 1036. |
| 3 | Safety |  |  |  |  |
| 3.1 |  | Worker safety |  |  | The manufacturer shall state any special requirements to ensure workers’ safety in the use of the products. |