| # TECHNICAL PROCEDURE TP020 |  | # Refurbishment of the Modular Superstructure |  |
| --- | --- | --- | --- |
| 1 | 1 May 2008 | A. Williams | R. M. Tomkins |
| Issue | Date | Written By | Approved By |

1.	Scope

This procedure covers the maintenance or refurbishment of the Modular Superstructure following 10 years' service on station to bring them fit for a further 10-year service period.

The work is to be undertaken at Harwich and Swansea Depots under the direction of the Buoy Manager.

2.	Inspection and cleaning following return from Vessel

The condition and function of the Modular Superstructure equipment should be thoroughly checked as soon as practicable after it is returned to the Depot.

The complete Modular Superstructure should be soaked with fresh water externally and cleaned of salt deposits and bird lime.

The condition of all electrical cables, glands and connections, including the battery terminals, should be checked.  If of doubtful condition, the cable and/or assemblies should be replaced.

The Modular Superstructure should be checked for compliance with the latest issue design drawings and specifications.

3.	Strip-down Modular Superstructure

All electrical items should be stripped out of the Modular Superstructure, and inspected for degradation in its physical condition.

All cubicles, solar panels and lantern may be re-used for a whole service cycle once. After the second service cycle, these items must be disposed of in accordance with TH procedures.

4.	Batteries

All batteries must be replaced to ensure that their condition is guaranteed. The old batteries must be disposed of in accordance with TH procedures.

5.	Solar Modules

Check the glass face of the solar modules for cracks or signs of water ingress.

Replace all swell latches.

6.	Mechanical Parts

Visually check for cracks at welds, battery fixings and fixing down fasteners.  If suspect, remove fittings from the damaged area, clean and inspect using an inspection light and magnifying glass.  Undertake dye penetrant testing if necessary.

Check for excessive corrosion, especially at crevices and at contact surfaces with dissimilar metals.  If excessive corrosion exists, remove fittings from the corroded area and clean away salt and corrosion deposits.

6.	Re-build

To ensure that a reliable Modular Superstructure is deployed after maintenance, the Buoy Build List should be followed from the pre-commissioning stage onwards. It is important that all checks and tests are carried out it prevent on-station problems.