This questionnaire is designed to gather information from IALA members on their experiences with the use of plastic buoys. This will then be collated and used to enable members to make informed choices on the selection of the most appropriate material for their specific buoy application.

128

- How many buoys do you have in your current buoy fleet ? ………………………………..…

Regarding the materials of construction, how many are:

85

-

-

Steel …………………………………………………………………………..……………….

Composite metal & plastic ………………………………………………………..…………

48

Plastic ……………………………………………………………………………………..…..

Other (please specify) …………………………………………Wood!…………………………….

- Buoy fleet by buoy body diameter and material, please complete the table below:

| Material | 1m dia or less | 1 to 2.2 m dia | Greater than 2.3m dia |
| --- | --- | --- | --- |
| Steel | - | 56 | 29 |
| Composite metal & plastic | - | - | - |
| Plastic | 17 | 24 | 7 |
| Other (Wood) | - | - | - |

- For your plastic buoy fleet, what type of plastic material is used ?

Polyethylene

- Are the plastic buoy bodies filled or empty ?

X

Filled			Empty

Please specify filler type   …Expanded Polystyrene Foam …………………………...

7

- How many years have you been using plastic buoys ? ……………

- Regarding the location / conditions of service for your plastic buoys, check the boxes that apply:

| Inshore | 6 buoys close to the beach |
| --- | --- |
| Offshore | 17 buoys in deep water (17m to 40m) |
| Exposed |  |
| Sheltered | 25 buoys protected by breakwater |
| Breaking waves |  |
| Dries at low tide |  |
| Severe UV exposure | All our buoys |
| Severe sub zero temperature | - |

- Are your plastic buoys a commercial design or your own authority’s design ?

X

Commercial Design			Own Design

- How often do you visit your buoys at sea ?

| Material | 1m dia or less | 1 to 2.2 m dia | Greater than 2.3m dia |
| --- | --- | --- | --- |
| Steel | - | 4 times / Year | 4 times / Year |
| Composite metal & plastic | - | - | - |
| Plastic | 4 times / Year | 4 times / Year | 4 times / Year |
| Other (Wood) | - | - | - |

- For your plastic buoys, what is the main reason for inspection / maintenance at sea ?

- Checking the light equipments, Batteries, Solars, and position every 4 months.

- Checking the mooring chain every 2 years and cleaning marine fouling to prevent the buoy to sink.

- Replacing the buoy every 5 years by new or refurbishment buoy.

We don’t do any maintenance ashore.

We don’t have any AIS equipments fitted on the buoys.

- How often do you return your buoys to shore for maintenance ?

| Material | 1m dia or less | 1 to 2.2 m dia | Greater than 2.3m dia |
| --- | --- | --- | --- |
| Steel | - | 5 years | 5 years |
| Composite metal & plastic | - | - | - |
| Plastic | - | - | - |
| Other (please specify) | - | - | - |

- For your plastic buoys, what is the main reason for inspection / maintenance ashore ?

- What experience do you have in modifying plastic buoys to take new navigation aids, such as AIS ?

- Have you experienced any in service defects with plastic buoys (such as colour retention, mechanical failure, mechanical damage, mooring lug wear) ?

Problem with colour retention, Decreasing the size of mooring lugs .and mechanical failure.

- Please detail any experience you have of repairing or re-painting plastic buoys ?

We don’t repair or re-paint the plastic buoys.

- Can you provide any cost comparisons between plastic buoys and traditional steel buoys (this may include initial cost, use of a smaller ship to support the buoy fleet, reduction in buoy maintenance facilities, reduction in overall maintenance costs)

We haven’t done yet.

- Are you planning to purchase more plastic buoys in the near future ?

X

Yes			No

15 years

- What is the anticipated life of your plastic buoys ? ……………

- What is your disposal policy for plastic buoys at the end of their life ?

There is no specific policy. However, we deliver the buoy to municipallity for disposal.

- With your experience, what is your general opinion of the use of plastic buoys ?

It’s good for some areas and locations. Such a small boats area, medial/low temperature and sheltered area.

- Please provide some photographs of your plastic buoys with sizes & weights (please resize and compress any photographs before insertion):