- Technical Inquiry – Buoy Metallurgy (Ref:  EEP2/10/3).  The Middle East Navigation Aids Service in Bahrain asked the EEP’s advice about severe pitting corrosion they are experiencing on their steel buoys.  The working group developed a number of recommendations in this regard that the Bahrain Authority could pursue:

- Evaluate the quality of surface preparation and coating, including materials and processes used.  Localised areas of corrosion indicate that the coating system has been penetrated.

- Cut a piece of steel from a failed hull and have it analyzed for chemical content to see if there is a problem with steel quality.

- Take care when removing fouling to minimize damage to the coating system (i.e., waterjet rather than scrape with metal scrapers).

- Trial the use of zinc anodes on the buoys.  The Netherlands Authority has had some good experience in this field.

The working group has indicated a willingness to follow up on this issue in more detail.  However, the following questions would first need to be addressed by the Bahrain Authority:

- Are these buoys newly-manufactured, or have they been in service and overhauled (blasted and repainted) before now?

- How old are the buoys?

- How long were they on station before this pitting occurred?

- How is fouling removed from these buoys on station?

The working group suggests that these recommendations and questions be forwarded via letter to the Bahrain Authority.

### Action Item

The IALA Secretariat is requested to forward the above recommendations and questions via letter to the Bahrain Authority.  The working group has also identified the following two Internet sites that may be of help to the Authority, and requests they be included in the letter:

www.key-to-steel.com/Articles/Art60.htm

www.corr-institute.se/english/Web_DT/files/mechanisms.pdf