EEP20	Input paper

Author(s)	Mariano Luis Marpegan – Raúl Escalante

Fluoropolymer-based paint to avoid incrustation

# Summary

We would like to share our experience in the use of fluoropolymer-based paint which confers a coating of low adherence of biological incrustation as well as high UV protection, adding durability to the structure.

## Material properties

Fluoropolymers offer high endurance against most chemical agents. It can withstand high and low temperatures (-260 ºC a +260°C) and also UV rays, without losing its original color.

Given its low coefficient of friction it is applied with sliding agents to confer extra sliding properties for high-performance plastics.

Among its unique qualities is its great durability, versatility, fireproof, endurance and its unconventional resistance against chemical products (acids, bases and solvents) and heat. Common uses include:

- High-performance supports and connections for the aviation and automotive industries.

- Diverse coatings for different products: pipes and tanks holding chemical products, owing to its thermal stability, its low adhesion properties and its resistance against foul weather conditions and UV rays.

- Paint coatings on telecommunication wires. Used in the IT industry because of its high electrical resistivity and generous dielectric properties.

## Experience:

In 2008 the decision was made to test the 3 signals installed in the Río de la Plata: the Magdalena Spar and the BLV 164 and BRL 161 buoys.

The Magdalena Spar was coated with fluoropolymer-based paint which, given its characteristics, produces a smooth non-stick layer which entirely prevents any kind of incrustation from settling.

It is conditional that the painted surface be protected from all kinds of mechanical damage which may  uncover a grip surface liable to the adherence of crustaceans.

The image below clearly shows how there is no trace of biological incrustations on the submerged fluoropolymer-covered surface during the launching of the signal. There is only slight evidence of mud, which can be easily brushed away with the wave of a hand. Conversely, a typically epoxy-covered surface exhibits numerous incrustations throughout.

It is important to underline that just like with antifouling paints, this paint protects the layer from wear; therefore, eventually it will have the same thickness as it had when first applied.

## Benefits of Use

The costs of placing a signal of this kind into service are seen to decrease considerably.

Extended lifespan of signal as it remains installed for longer periods of time; besides, its surface undergoes less wear than if it were covered with conventional paint.

The operating costs for the buoys are lower since fairing has to be done on a less frequent basis.

Improved stability of signal since biological incrustation tends to accumulate on the surface thereby increasing the weight of the signal while reducing buoyancy.

It is worth observing that a swift swipe with one hand will discover an impeccable surface even 1 year after the signal was installed.

The 2 pictures below expose the difference between zones painted and those NOT painted with fluoropolymer.

The activity of biological incrustation can be clearly seen on the areas covered with another type of paint. The difference is noticeable.

The unpainted steel tube placed next to the fluoropolymer-covered area is completely pervaded by biological incrustation while the surrounding area painted with fluoropolymer remains unblemished.

## Purpose of the document

The purpose of this document is to serve as a basis for discussion for a Guideline on the subject

## Related documents

Body text.

# Background

Give the background to the paper.  (Body Text)

# Discussion

Develop as required.  (Body Text)