Advantages and Disadvantages in the use of large plastic buoys (1.8 to 3.0m diameter)

Advantages:

- The plastic does not corrode.

- Less maintenance on station; only removal of marine growth, no painting on station.

- Less maintenance on shore in the workshops for the plastic component (no grid blasting, no paint system of 3 layers or more) therefore fewer personnel and smaller workshops, lower personnel and equipment costs.

- Lower weight (1/2 to 1/3 of the weight of steel buoys in the diameter range 1.8 – 3.0 m) therefore the service can use smaller buoy tender.

- CETMEF and Rijkswaterstaat have more than more than 10 years experience of operating rotomoulded polyethelene (PE) plastic buoys in the 1.8 – 3.0 m diameter size range.

- At least 6 commercial companies offer large rotomoulded plastic buoys.

- Linear PE is recyclable (if not foam filled with polyurethane).

- It is possible to hot-flame-spray PE if the surface colour needs to be changed, but this is not necessary in many cases.

- Large plastic buoys are typically of modular construction. It is therefore possible to change individual body segments if they are damaged.

- Easier to transport and store the sections of the body when compared with conventional single component bodies.

- It is possible to install a radar reflector within a plastic buoy’s superstructure.

- The superstructure can be rotomoulded.

Disadvantages:

- A large plastic buoy will usually contain metal components such as the tail tube, mooring-eyes, lifting-eyes, connecting bolts, lantern-mounting, etc. These metal items will still need maintenance.

- Less weight will result in more rapid motion on station when compared with the heavier steel buoy.

- Repairs are not simple or may often not be possible: it is more difficult to weld PE than steel. It is very difficult to monitor the weld quality.

- There is little experience in ice conditions or in very cold waters although Sweden has some good experience with PE spar-buoys in ice conditions.

- It is more difficult to change the colour of a plastic buoy, as conventional painting is not reliable. This may increase the number of spares needed, compared with steel buoys, i.e. red, green, black and yellow spares may have to be carried rather than re-painting steel components.

- Shorter lifetime than steel buoys –PE lifetimes are estimated to be better than 10 years compared with proven steel lifetimes often considerably in excess of 30 years.

- Less resistance to collision damage than steel.

- Plastic buoy components will be specific to each manufacturer compared to steel components that can be manufactured by any competent steel fabricator.

If an Authority is to consider using a plastic buoy then the following questions should be addressed:

  - Is the plastic buoy big enough as a daymark?

  - Is it big enough to carry a lantern with the required range and the associated power system?

  - Is the focal high sufficient for local sea conditions?

  - Is it possible to secure a suitable mooring chain?

  - Is the motion of the buoy on station to rapid for the AtoN function to be clear to the mariner or for the maintenance staff to work on the buoy?

  - If there are ice conditions will the buoy be suitable?

  - Is the colour non-fading?

  - Can a suitable radar reflector be mounted?

  - What are the inspection and maintenance intervals of plastic parts, mooring system, energy system and lantern?

  - Does anybody want to have plastic buoys; is there any political reason against this?

  - What are the costs of the purchase of a steel buoy?

  - What are the costs of the purchase of a plastic buoy?

  - How long does it take to maintain a steel buoy – and how much does it cost?

  - How long does it take to maintain a plastic buoy – and how much does it cost?

It is necessary to make an economic analysis in which you have to compare the cost of the purchase of a steel buoy and the consequent maintenance costs (including personnel, equipment and material costs) with the same costs for similar use of plastic buoys. In the analysis you can take into consideration that you may be able to use a smaller buoy tender. The analysis is only possible if there is a suitable plastic buoy that can replace the function of the steel buoy.

The work on this paper will be continued.