### Appendix 1 – Technical Factors that may affect the choice of Rotationally Moulded Polyethylene Buoys

[cut from here – put as an input to next EEP for the work item on revision of guideline on plastic buoys]

Advantages:

- The plastic does not corrode.

- Less maintenance on station; only removal of marine growth, no painting on station.

- Less maintenance on shore in the workshops for the plastic component (no grit blasting, no paint system of 3 layers or more) therefore fewer personnel and smaller workshops, lower personnel and equipment costs.

- Lower weight (1/2 to 1/3 of the weight of steel buoys in the diameter range 1.8 – 3.0 m) therefore the service may be able to use smaller buoy tender.

- CETMEF and Rijkswaterstaat have more than 10 years experience of operating rotationally moulded polyethylene (PE) plastic buoys in the 1.8 – 3.0 m diameter size range.

- At least 6 commercial companies offer large rotationally moulded plastic buoys.

- Linear PE is recyclable (if not foam filled with polyurethane).

- It is possible to hot-flame-spray PE if the surface colour needs to be changed, but this is not necessary in many cases.

- Large plastic buoys are typically of modular construction. It is therefore possible to change individual body segments if they are damaged.

- Easier to transport and store the sections of the body when compared with conventional single component bodies.

- It is possible to install a radar reflector within a plastic buoy’s superstructure.

- The superstructure can be rotationally moulded.

Disadvantages:

- A large plastic buoy will usually contain metal components such as the tail tube, mooring-eyes, lifting-eyes, connecting bolts, lantern-mounting, etc. These metal items will still need maintenance.

- Less weight will result in more rapid motion on station when compared with the heavier steel buoy.

- Repairs are not simple or may often not be possible: it is more difficult to weld PE than steel. It is very difficult to monitor the weld quality.

- There is little experience in ice conditions or in very cold waters although Sweden has some good experience with PE spar-buoys in ice conditions.

- It is more difficult to change the colour of a plastic buoy, as conventional painting is not reliable. This may increase the number of spares needed, compared with steel buoys, i.e. red, green, black and yellow spares may have to be kept in stock rather than re-painting steel components.

- Shorter lifetime than steel buoys –PE lifetimes are estimated to be better than 10 years compared with proven steel lifetimes often considerably in excess of 30 years.

- Less resistance to collision damage than steel.

- Plastic buoy components will be specific to each manufacturer compared to steel components that can be manufactured by any competent steel fabricator.