- ARABIAN MARITIME AND NAVIGATION AIDS SERVICES LLC

- PO Box 1677

CPO Seeb

Postal Code 111

Sultanate of Oman

+968 24510283; Fax +968 24510432

Ops 325/1

Date: 10 March 2007

- Mr. Bob McIntosh BSc. CEng MICE

- Projects Group – Team Leader

- Northern Lighthouse Board

- 84 George Street

Edinburgh

EH2 3DA

Scotland

Subject: Working Group 2 – EEP April 2007

I regret that I will not be able to attend EEP 9 in April, however I hope that you might find the following useful, even though Oman’s ‘Conservation Strategy’ is to keep its lighthouses under private ownership and maintain them strictly in accordance with Oman’s environmental laws. The comments are based on the total refurbishment of Didamar Light in the Strait of Hormuz which featured in the IALA Bulletin 2006/4.

- Item 8.1

- Paint specifications. The structure was manufactured from cast steel sections bolted together with a copper dome to the lantern house. AMNAS contacted Jotun paints who provided the following specifications:

- Copper Dome : The surface preparation [using paint stripper and hand-tool removal of old coats] must ensure that the stripping is to bare copper surface. Also the paint stripper should be washed as per the manufacturer’s instructions so as not to leave any traces of the same as it will effect the subsequent new coating. 
Apply Penguard Primer as the primer coat at dft of 40 microns on the bare copper substrate. Apply two coats of Durathane Matt Black/ White as desired. 
Spray application will give a good uniform finish [comment – final application was by hand roller and brush].

- Main Steel Structures, Hand Rails, Supports, Platforms. As these cannot be blast cleaned [the cost of grit blasting was too high] mechanical tools will be used to ensure all loose paint & corrosion is removed using chipping hammers and wire brushes etc. Apply Jotamastic 87 Aluminium as the first coat. If applied by roller/brush apply multiple coats to achieve dry film  thickness of at least 150 microns. Apply two coats of Durathane Grey Jotun color 403 followed by two coats of Gardex Gloss White. Wooden Flag Staff : If bare wood apply Bengalac Wood primer

- Wooden Doors - Marine varnish is of two kinds; single pack or two pack. We recommend two pack Durathane Clear Gloss finished in two/three coats. The first coat maybe thinned 20% with Thinner 10 to ensure penetration into the wood. The subsequent coats maybe diluted 10-15% to get a good finish. It is also possible to spray Durathane. The single pack marine varnish is Clipper Varnish.

- It took a team of 10 workmen 4 weeks to remove all the old paint. High humidity and high daytime temperatures (40°C) were encountered daily. Water to wash the structure was in very short supply, but AMNAS fund that dry brushing achieved a fine final surface. Joints were treated with an acid solution before primer was applied. Six months after the final paint application, some rust spots are beginning to appear. These will be tackled during the periodic visits by AMNAS technicians.

- Removal of 280KG of mercury was conducted following the advice given in the Navguide Chapter 6. None was spilt. The use of small 0.5 litre plastic screw-topped bottles packed in slotted wooden crates facilitated transport from the lantern house to the jetty and subsequent loading to the mother ship.

Item 8.2  Oman has just three historic lighthouses none of which is open to or accessible by the public, nor is likely to be in the foreseeable future. The site Krookies were transferred to AMNAS for the duration of the 25 year Concession Agreement. Ch 1 and 2 of the Conservation Manual contain excellent guidance for AMNAS and is successor to consider in the future.

- Item 8.3 – 8.12. AMNAS has no input other that to wish the Working Group success.

Kind regards,

- Stephen Bennett

- S H G Bennett

Operations and Development Manager