Retroreflecting material on AtoN Marks

IALA Recommendation E-106

On the use of Retroreflecting Material on AtoN Marks within the IALA Maritime Buoyage System

Document ID:	Input paper IALA ENG4, Retroreflecting Material on AtoN Marks

Prepared by:		Jørgen ROYAL PETERSEN, Senior Engineer Aids to Navigation

Date:		April 6, 2016

Version:		2.0

Content

1	Summary	3

2	Preface	3

3	Consideration on the update	3

4	Proposal of content of a reviewed recommendation IALA E-106	3

4.1	General	3

4.2.1	Type of reflection	5

4.2.2	Two basic optical systems of retroreflectivity	5

4.2.3	The Glass Sphere or Bead	5

4.2.4	Prismatic or Cube Corner Reflector	6

4.3	Specification and measurement of retroreflecting material	7

4.4	Calculation and determination of size of Retroreflector	8

4.5	Consideration of particular colours	9

4.6	Degradation of retroreflecting material	9

4.7	Radar reflector and retroreflecting material	9

4.8	Codes for application at buoys in accordance with Maritime Buoyage System (MBS)	10

4.9	Approval and classification of retroreflective material	13

4.10	Application and best practice	20

5	References	29

# Summary

This document are dealing with the review of the IALA Recommendation E-106 “On the use of Retroreflecting Materiel on Aids to Navigation Marks within The IALA Maritime Buoyage System (MBS)”

It is suggested to expand the content of the recommendation to include brief information about technology, design, measurements, classification, best practice etc. and update the table of codes for AtoN marks.

In addition to this it is proposed that the IALA ENG Committee consider adopting or developing standard specification and requirement for retroreflective material for use at AtoN Marks.

# Preface

This document is an input paper for IALA ENG 4 in the proceeding for reviewing and updating The IALA Recommendation E-106 “On the use of Retroreflecting Materiel on Aids to Navigation Marks within The IALA Maritime Buoyage System (MBS)”.

The purpose of this input paper is to give proposals for updating and development of the current version of IALA E-106

# Consideration on the update

Based on experience by use and through the reviewing process of the IALA Recommendation E-106 “On the use of Retroreflecting Materiel on Aids to Navigation Marks within The IALA Maritime Buoyage System” it is identified that the content of the recommendation only describes partly the codes (no codes for the wreck mark buoy and the modified Port and Starboard lateral mark) to be used for marking AtoN by retro-reflecting material and basic technology introduction and specification/requirement of the retro-reflecting material are not included.

It is proposed to update and include an updated code description, basic description of technology and design of retroreflecting material, recommendation on how to select retroreflective material for AtoN purpose in order to harmonise the use of retroreflective material and have a definite and uniform description when ordering and supplying retroreflecting material for AtoN purpose.

IMO has by the SOLAS regulation specification and requirement for retroreflective material and Road Authorities have too classification and standard for retroreflective material.

It is proposed that the IALA ENG Committee consider adopting or developing standard specification and requirement for retroreflective material for use at AtoN Marks.

# Proposal of content of a reviewed recommendation IALA E-106

- General

- Terminology, basic technology and design of retroreflecting material

- Specification and measurement of retroreflecting material

- Calculation and determination of size of Retroreflector

- Consideration of particular colours

- Degradation of retroreflecting material

- Radar reflector and retroreflecting material

- Codes for application at buoys in accordance with Maritime Buoyage System (MBS)

- Approval and classification of retroreflective material

- Application and best practice

## General

The earliest recorded formation of glass into spherical shapes dates back to early Chinese history. Observation of light reflected back towards the light source from these spheres was used to heighten the brightness or brilliance of arts object. Glass spheres of different coloured glasses can be found in ancient jewellery. Many of the cuts of the facets of diamond are made to retroreflect the incident light, resulting in the brilliance of the diamond.

The first use of these materials for purpose of enhancing the conspicuity of objects was probably created in Great Britain around the turn of the century (1800/1900). Observation of light reflected from animal’s eyes, especially those of cats, started the thought of using this technique to enhance the brightness of objects.

The current explanation of the glowing nature of cat’s eyes stems from the highly reflective nature of their retinas. Because these animals were primarily nocturnal and relied on making the most use of the available low light level, the retina is coated with material which reflects over 80 % of the incident light, and traps this light in the eye to increase the detectivity of objects.

Figure 1 A Cat's "glowing eyes"

The history indicates that safety for drivers in the area of transportation was the first to have benefit of the idea to investigate and produce glass spheres with same effect as the “cat’s eyes”.

Today retroreflective material has a widespread use to increase the night time conspicuity of traffic signs, high-visibility clothing, and other items so they are safely and effectively visible in the light of an approaching driver's headlamps or a ships search light.

Retroreflective material is available in arrays in different sizes and colours, sheeting of plastic and metal, adhesive tape etc.  Many different colours and degrees of reflection intensity are provided by numerous manufacturers for various applications.

As with any retroreflector, sheeting glows brightly when there is a small angle between the observer's eye and the light source directed toward the sheeting, but appears non-reflective when viewed from other directions.

For Aids to Navigation purpose the retroreflective material is primary used for floating aids with a distinct code in accordance to the specific floating aid’s function.

Furthermore retroreflective material is used for day boards for leading lines, lettering and numbering, signs for waterways, marking of edges and piers etc.

  - Terminology, basic technology and design of retroreflecting material

The International Commission on Illumination (CIE), the international standardizing body responsible for light and colour measurement, defines retroreflection as follows:

“Reflection in which the reflected rays are preferentially returned in direction close to the opposite of the direction of the incident rays, this property being maintained over wide variation of direction of the incident rays”

Figure 2 Reflective and Retroreflective

### Type of reflection

When looking at a reflecting surface, the surface shows an image and space in front of the surface.

The image may be complete blurred as in surface with diffuse reflection, or it may be sharp as in surface with mirror reflection.

Most practical surfaces have mixed reflection, which is a mixture of diffuse reflection and mirror reflection in the surface, mostly with the surface reflection partly blurred by texture.

A particular kind of reflection is retroreflection, where the surface preferentially shows an image of the part of space around the observer. Retroreflection may be mixed with other kind of reflection.

### Two basic optical systems of retroreflectivity

There are two basic optical systems of retroreflectivity; the Glass Sphere or Bead and the prismatic or Cube Corner Reflector.

Figure 3 Two systems of optical retroreflectivity

### The Glass Sphere or Bead

The simplest retroreflector is a glass sphere or bead. When a light beam is directed at it, the majority of the light bounces off it but a significant amount passes through the front surface and is bent or refracted roughly toward the centre of the rear surface. Some light hitting the rear surface of the sphere is internally reflected back through the front surface of the sphere face and is again refracted onto a course parallel to the direction from which it came.

Only 28 % of the area of the sphere is at a sufficiently favourable angel to return the light beam and there are losses every time the light encounters a surface of the glass, especially when the beam hits the rear wall where a large proportion passes through it rather than being internally reflected. A major improvement in retroreflectivity can therefore be achieved by coating the sphere’s rear surface so that it acts as a mirror (as shown in Figure 4, below)

Figure 4 Glass Sphere or Bead

### Prismatic or Cube Corner Reflector

More efficient is the prismatic or cube-corner reflector. If you take a solid glass cube and slice off one corner with a cut that passes along the diagonals of three adjoining faces you have the basic cube-corner unit which is a squat triangular pyramid shaped prism. When the pyramid is set up with the triangular base directed towards a beam of light, the light passes through the base with very little loss. Once inside the pyramid it is internally reflected off each of the three side faces in turn before being directed back through the base, exiting parallel to the incoming light beam. Reflected light is still parallel to the incoming beam is not square to the face of the pyramid, as the light is equally refracted when entering and leaving the prism.

The cube-corner pyramid prism is a fairly efficient retroreflector but has two limitations:

- Light entering closer to the corners of the triangular base is only internally reflected off the two nearest sides and misses the third side, which is too far away. About 35 % of the incoming light is lost in this way.

- As the angel at which the light approaches the entry face becomes shallower, so an increasing proportion of the light will bounce off the surface instead of entering the pyramidal prism. These losses are relatively small where the light hit it within 10 dg to 15 dg of square but rapidly increase at more acute angels.

Figure 5 Prismatic/Cube Corner Reflector

## Specification and measurement of retroreflecting material

Performance values for retroreflective sheeting are an expression of the efficiency of that material to retroreflect the light at a particular “geometry”; i.e., at one set of observation and entrance angles. (One “geometry” often used in specifications is: 0.2 degrees Observation angle and 4 or 5 degrees Entrance angle.) The number given tells how much light is retroreflected at that “geometry” for a given unit of light falling on a given area of the material. Technically, it is termed the “Coefficient of Retroreflection,” designated by the symbol RA. (Here we’ll sometimes refer to it as the “retroreflectivity value or simply, “retroreflectivity”).

“RA” essentially expresses the relationship:

It is not necessary to know the exact technical meaning of the factors comprising that term (but they are: candela per incident lux per square meter, often abbreviated to “cd/lx/m2”); the important concept to understand is that the retroreflectivity value RA is a ratio. It’s similar to “per cent” and does not tell how bright the sheeting will be on a given sign (even at the distance corresponding to the “geometry” for that particular value). It is simply its “efficiency” at returning light to the source at that particular geometry (the set of observation and entrance angles).

The efficiency of a retroreflective material varies with different observation and entrance angles and the various materials vary in different ways. The practical effect of these differences is what influences the choice among different retroreflective materials for a particular situation, taking into account headlight illumination, practical viewing requirements and distances, and the viewing needs of the user.

Figure 6 Retroreflective basics                                  Figure 7 Arrangement for measurement

## Calculation and determination of size of Retroreflector

Finnish description and formula for calculation and determining size of retroreflector:

Use of retroreflecting film on leading marks in Finnish guidelines

“Reflectors are mostly used as alternatives to lights on small craft routes and other less important roures. However, they have importance on lighted fairways as well in case of failure of a light.

At first, the light source is selected for observing the reflectors. On small crafts 10 000 cd and on ships ca 100 000 cd search lights can be expected.

Then the minimum size of the reflector can be calculated by the formula:

A = D4E/ IR0,052D/18520							(2.4.1)

Modified for the treshold of illuminance:

E = AIR0,052D/18520/ D4							(2.4.2)

A – area of the reflector  [m2];

E – treshold of illuminance [lx];

D – observing distance [m];

I – intensity of the light source [cd];

R – reflecting coefficient of the reflector [lx/m2/cd].	(At 3M web page it is cd/lux/m2)

In principle the calculations can be made as for lights but, as the main purpose is to get strong enough reflection, maximum values need not to be calculated. Retroreflecting film is placed on the middle stripe of the leading mark so that it covers ¾ of that stripe, and a quarter of the area of the whole daymark. Film of the front mark begins from the lower edge of the daymark and the film of the rear mark begins from the upper edge of the daymark (so that that the reflectors will not blur making using the leading line difficult). The reflection is decreasing very fast with the distance and the maximum distance does not exceed 4000 m even with powerful searchlights. In practice the distances are 0 ... 2500 m are used. The colour of the reflector is always white.

When the areas to be covered with the reflectors are determined the value of E is determined for both marks with the formula (2.4.2).”

Example of a calculation…:

## Consideration of particular colours

Copy from the current edition of E-106

## Degradation of retroreflecting material

The deterioration rate or service lifetime of retroreflective material depends of many factors and their influence is type dependent.

Plastic cube-corner prismatic materials are the most common type applied as retroreflective material at AtoN.

The colour may change due to pigment fading and loss of transparency caused by UV exposure. The material for rigid cube corners may crack allowing moisture to penetrate and destroy the TIR, and of course abrasion of the outer surface is very common. Due to the harsh environment the retroreflective material are often exposed for mechanical injury caused by scratching from too close passing vessels, ice condition, change in temperature and humidity etc.

In addition to former, microprismatic materials that are in flexible materials will deform, changing the shape of faces and spreading the returned light, thus lowering the value at the same geometry.

## Radar reflector and retroreflecting material

Experiences have shown that retroreflective material can cause a lower Radar Cross Section (RCS) value if the retroreflective material is applied on the surface of a buoy with an integrated radar reflector.

It is recommended not to apply the retroreflective material on the buoy surface where the surface covering an integrated radar reflector.

## Codes for application at buoys in accordance with Maritime Buoyage System (MBS)

Proposal for updated table of the codes to be used for marking aids to navigation by retroreflecting material.

Before ENG4 this document will be updated with a proposal of a complete list of codes including wreck mark buoy and modified Port and Starboard lateral mark.

## Approval and classification of retroreflective material

It is suggested to collect information of which type of retroreflective material authorities and the suppliers of AtoNs are using and in addition to this ask authorities for information on in-house specification and knowledge on retroreflective material.

It is recognized that German Federal Waterways and Shipping Administration specifying retroreflective sheets by:

- A German Standard DIN 67520

- European Standard DIN EN 12899 (available in English)

  - EN 12899-3 Delineator Posts and Retroreflectors

- Class RA 1 to RA3 included RA3 yellow-retroreflective plus fluorescent are used

By DIN 67520:

Reflexions-Klassen

Die Norm unterscheidet zwischen vier Reflexionsklassen (RA), die je nach Anwendung gewählt werden können.

Die Klassen sind bezeichnet mit:

| Klasse | Eigenschaft | Besonderheit |
| --- | --- | --- |
| RA1 | min. 60 cd/lx pro m² |  |
| RA2 | min. 180 cd/lx pro m² |  |
| RA3A | min. 300 cd/lx pro m² | lange Distanz |
| RA3B | min. 300 cd/lx pro m² | kurze Distanz |

Folienaufbau

In der DIN 67520 werden Reflexionsklassen und Folienaufbau unabhängig voneinander beschrieben. Es sind somit theoretisch beliebige Kombinationen aus Klassen und Aufbau möglich. Beim Aufbau wird unterschieden zwischen

- Aufbau A - eingebundene Glasperlen

- Aufbau B - eingekapselte Glasperlen

- Aufbau C - Mikroprismen

Movement of the buoy and movement of the observing vessel should be considered when selecting and specifying retroreflecting material for floating aids.

Classification of adhesive…

Below is shown some examples of classification of retroreflective material:

## Application and best practice

Primary and for application at floating aids Danish Maritime Authority (DMA) use 3M High Intensity Prismatic Reflective Sheeting, series 3930.

It is non-metalized micro-prismatic lens reflective sheeting designed for the production of durable traffic control signs, work zone devices and delineators that are exposed vertically in service. The series provides long term reflectivity and durability.

Below data sheets of 3M Series 3930 and Reflexite VC 310 Durabright are shown.

Swedish Maritime Administration (SMA) uses 3M 3820 Series:

Best practice to avoid damage on the retroreflective material at a buoy structure

Figure 8 Example of protective arrangement of retroreflective material

# References

[1]	IALA Recommendation E-106 “On the use of Retroreflecting Materiel on Aids to Navigation Marks within The IALA Maritime Buoyage System (MBS)”

[2]	Handbook of Applied Photometry, Optical Society of America, Edited by Casimer DeCusatis

[3]	A brief history of retroreflective sign face sheet materials, by John Lloyd

[4]	DELTA, 2970 Hoersholm, Denmark, Technical Note RS 101