Input paper:   ENG5-10.37

Input paper for the following Committee(s): 	check as appropriate		Purpose of paper:

□  ARM		X ENG		□  PAP						□  Input

□  ENAV	□VTS								X  Information

Agenda item			              10

Technical Domain / Task Number2	TD#2

Author(s) / Submitter(s)			Dr. Ju-Seop Han / Korea Association of Aids to Navigation

# Sea Test Results of Plastic Buoys (Polyethylene, Polyurea foam, Steel)

# Test SUMMARY

In order to analyze the advantages and disadvantages of the buoy type and derive improvement, Ministry of Oceans and Fisheries (PYEONGTAEK Regional Office of Oceans and Fisheries) and KAAN have been jointly test.

- Test location: Pyeongtaek-Dangjin Port(Nearby Bangdo) in Korea

- Test period: Feb. 2016.  ~  Feb. 2018

- Test Samples: 5(Polyethylene 3, Polyurea foam 1, Steel 1)

| Body | diameter(㎜) | height(㎜) | draft(㎜) | weight(kg) | color | install date | quantity |
| --- | --- | --- | --- | --- | --- | --- | --- |
| PE(JET-7000) | 2,600 | 8,789 | 2,996 | 2,085 | R | ‘16.2.19 | 2 |
| PE(PB-26) | 2,600 | 10,513 | 4,469 | 3,539 | R | ‘16.2.19 | 1 |
| Poly Urea Foam | 2,800 | 6,900 | 4,600 | 4,923 | WB | ‘16.3.18 | 1 |
| Steel(LL-26(M)) | 2,600 | 9,400 | 4,100 | 5,982 | R | ‘16.2.19 | 1 |

Figure 1	Photograph of Sea Test (installed buoys)

## Light buoy stability

In order to analyze stability of the light buoys, two-axis tilt angle meters (X, Y-axis measurement of the dynamic angle of tilt in two directions) were installed in the upper steel  tower of the light buoys.

| Classification | BangdoTest A (JET-7000) | BangdoTest D (PB-26) | BangdoTest E (LL-26(M)) | Remark |
| --- | --- | --- | --- | --- |
| Maximum tilt angle | 34.5° | 23.6° | 38.4° |  |

Daily maximum tilt angle of the BangdoTest A (JET-7000), BangdoTest E (LL-26M) is significantly changing the slope, but BangdoTest D (PB-26) is gradually changed.

The cause for the maximum inclination angle of the measuring buoy is unknown. It is necessary to check the stability analysis of the maximum inclination angle from the data measured for about two years.

Figure 2	Graph of daily Maximum Tilt angle

## Chromaticity change of Surface colour

All test light buoys are almost no surface colour change over time (installed within 4 months).

* Portable Spectrophotometer (CM-2600d, KONICA MINOLTA) used only flat color change over time for inspection

| BangdoTest A (JET-7000) | BangdoTest C (Polyurea foam) |
| --- | --- |
| BangdoTest D (PB-26) | BangdoTest E (LL-26M) |
| * Measurement date: First (16.3.18), Second (16.5.25), Third (16.6.17) |  |

## Attachment state of sea algae and shellfish

BangdoTest A (JET-7000) is installed the Zinc Anode (10kg * 2), but the marine life was entirely attached to the lower body and tail pipe.

BangdoTest D (PB-26) is installed the Zinc Anode (30*200*100 * 3). Marine organisms were adhered uniformly on the plastic lower body, and tail pipe has been only partially attached.

BangdoTest E (LL-26M) is installed the Zinc Anode (30*200*100 * 3). The untested side of the light buoy with antifouling paint has been attached sea algae. The lower body and tail pipe were painted antifouling sea algae and shellfish rarely attached.

| BangdoTest A (JET-7000) | BangdoTest C (Polyurea Foam) |
| --- | --- |
| BangdoTest D (PB-26) | BangdoTest E (LL-26M) |

Input document number, to be assigned by the Committee Secretary

Leave open if uncertain