Draft IALA Guideline

1006

On plastic buoys

Edition 4

Document 03/2017

6.	POLYURETHANE / ELASTOMER COATED FOAM (Appendix 4, Figure 5)	4

6.1.	elastomer material – general	4

6.2.	mechanical properties and standards for elastomer plastic	4

6.2.1.	polyurethane elastomer properties	4

6.2.2.	polyethylene solid foam sheet properties	5

6.3.	manufacturing the buoy body of elastomer buoys	5

6.3.1.	Float	5

6.3.2.	assembly of elastomer buoy parts	7

6.4.	types and sizes of elastomer buoys	8

6.5.	construction details of elastomer plastic buoys	10

6.5.1.	general	10

6.5.2.	force transmission	10

6.5.3.	colours of elastomer buoys	10

6.5.4.	lettering methods	11

6.5.5.	metal parts	11

6.5.6.	swimming stability	12

6.6.	advantages of elastomer polyurethane buoys	12

6.7.	handling	13

6.8.	repair & maintenance	15

6.8.1.	general	15

6.8.2.	periodicity	15

6.8.3.	float and tail	15

6.9.	quality control and testing	16

6.10.	recycling	16

# POLYURETHANE / ELASTOMER COATED FOAM (Appendix 4, Figure 5)

## elastomer material – general

These buoys typically consist of a thick, flexible marine grade polyurethane elastomer skin on a flexible closed cell foam core. They have the advantage of overall flexibility and resilience. The flexibility will also be an advantage when the buoy has to be lifted or serviced in rough weather.

The main feature of Elastomer Buoys lies in its float, of high elasticity and lightweight, manufactured with closed-cell polyethylene solid foam sheet (no water absorption) and projected with a layer of coloured polyurethane elastomer.

Thanks to its solid construction, they are virtually unsinkable, even against a strong impact. Besides, they can withstand repeated collisions without deforming.

## mechanical properties and standards for elastomer plastic

### polyurethane elastomer properties

| PROPERTIES | VALUE | RESULT | STANDARD |
| --- | --- | --- | --- |
| Density | Kg./m3 | 900 | BS 4370 PART 1 METH 2 |
| Tensile strength | MPa | 17 | ISO 527 |
| Ultimate elongation | % | 342 | ISO 527 |
| Hardness (Shore A) |  | 95 | DIN 530505 |
| Hardness (Shore D) |  | 52 | DIN 530505 |
| Breaking resistance | N/mm | 35 | DIN EN ISO 6383-1 |
| Water vapour diffusion resistance | nu | 2.279 | EN 1931 |
| External fire performance | - | Class. Broof (t1) | UNE-EN 13501-5 |
| Fatigue motion resistance | Apt. in 1.000 cycles | - | EOTA TR-8 |
| Tensile resistance | 15 N/mm2 |  |  |
| Fire resistance | self-extinguishing |  |  |

### polyethylene solid foam sheet properties

| Physical condition | Solid |
| --- | --- |
| Colour | Coloured |
| Smell | lightly perceptible |
| Melting point | 105-110ºC |
| Flash point | 420-440ºC (ASTM 1929) |
| Ignition temperature | 430-450ºC (DIN 54836) |
| Density | From 30 to 100 kg/m3 |
| Water solubility | Insoluble |
| Water absorption | 1-2% |

## manufacturing the buoy body of elastomer buoys

### Float

The manufacturing process of the elastomer buoy float is based on a solid rolled body of closed-cell polyethylene foam sheet, which is covered by a projection of elastomer polyurethane; thus forming an elastic skin on an elastic core. Depending on the needs, the thickness of the cover could be adapted. This process provides a great recovering capacity and null water absorption.

The core of the elastomer buoys are manufactured of material of different densities, which allows the adaptation to the needs depending on  location, environmental conditions or external influences that require different densities.

The solid body is done by rolling a closed-cell polyethylene foam sheet and binding it by heat, no chemical substance is involved in it. Thus obtaining a solid, compact and extremely flexible body buoy.

This feature provides a solid and elastic float with great recovering capacity and zero water absorption.

In the upper area of the float, a projection of silica granulation is applied to avoid slides of the maintenance staff; being coated with the applied polyurethane and resulting in a non-slip surface.

### assembly of elastomer buoy parts

In the case of the elastomer buoy parts, the float is a solid part, never manufactured in modules. Therefore, the assembly involves others parts of the buoy like metallic structures, tail, top marks, etc…

The process of manufacturing and materials used in the Elastomer floats are the same as those used in fenders of ports for vessel berthing. They are prepared to withstand repeated strong collisions. Thus, the replacement of the float is unexpected.

The interface between the plastic part and the metallic part is designed in order to avoid movement or rotation, to a uniform and robust ensemble.

The mounting of the elastomer buoy, depending on the size, has to be made in horizontal for a safe handling and convenient assembly.

First, we identify the parts of the buoy to be assembled with the indications of the manufacturer and the screws to be used for unions. Then the float is to be assembled with the tail or skirt, joining the tail lugs and the float slits. Then, we ensure this union with the float ring and a set of simple brackets (float bracket).

Secondly, we will mount the buoy ballast weights. To do this, first we use a support in the middle of the tail to avoid damages to the float (one European pallet in good condition can be used). We place the ballasts and ballasts stopper with the screws and washers located inside the tail tube, afterwards we place the ballast weights making contact with the stopper. Then the reinforced brackets are installed (ballasts brackets), in order not to move the ballasts.

Thirdly, we will assemble the buoy superstructure with the tail. As we have mounted the ballasts, the superstructure can be fitted. For safety, we can install another support on the top of the superstructure. This union has a double safety nut.

Finally, the day marks with its plates can be mounted. To conclude, we assemble the protection ring and the top mark with the superstructure.

## types and sizes of elastomer buoys

As they need no mould, the choice of types and sizes, besides being infinite, it is open to que required of the location’s needs.

The diameters of the elastomer buoy that we can find nowadays in the market are between 0.8 to 3.6 meters.

Example of Oceanographic Elastomer buoy.

Example of  Elastomer buoys.

Example of High Mooring Elastomer buoys.

Example of Spar Elastomer buoys.

## construction details of elastomer plastic buoys

### general

The thickness of the polyurethane elastomer layer projected must be optimized to the size, the shape and the environmental conditions of the buoy to be sufficiently robust. The most common range used is from 8 – 20 mm.

During the manufacturing process of the float, different foam density could be used. I this way, at a greater risk of collision, a buoy with a higher resistance can be designed and fabricated.

The elastomer provides good adhesion  for conventional paints; specialized hot plastic spraying processes are available and have been used successfully.

### force transmission

The elastomer buoys do not need any additional structural reinforcement in the float to prevent high forces stress.

### colours of elastomer buoys

The colour of the elastomer buoys is integrated in the projected layer of coloured polyurethane elastomer.

This layer should have UV protection, which prevents discolour of the float during its service life.  The elastomer surface admits later repainting.

Colour pigments must be of the highest quality suitable for marine use and UV exposure. The colours of elastomer buoys should fit to the IALA Recommendations.

To maintain the colour of the mark within the IALA limits, it is necessary to maintain the buoy clean from any deposits or animal droppings.

### lettering methods

Most administrations apply the position name/number on the buoy body. Appropriate methods have to be found to achieve a long-term stability of the lettering. Solutions could be:

Painting

Adhesive foils

Mounted plates (welded or fixed by screws)

Scaring/engraving

Plastic spray method

### metal parts

#### General

As the other technologies, the elastomer buoys includes at least the following metal parts:

lifting eye(s)

mooring eye(s)

standard parts

inserts

ballast (in case of cast iron or steel)

The metal parts of a buoy must be selected in such way, that no galvanic element is produced. Sometimes it is necessary to insulate metal parts (paint, insulating hull, bitumen coat).

#### Lifting eye and mooring eye

Depending on the buoy type, the lifting eye and the mooring eye can be made as follows:

galvanized-steel-part of the tail or skirt

stainless-steel-part of the tail or skirt

The safe working load should be optimized regarding the handling, deploying and recovering of the buoy in order to insure safe operation.

#### Standard parts

Standard parts (screws, nuts, washers, etc.) should be made of stainless steel, hot dip galvanized.

#### Inserts

Inserts are used for fastening the lantern, colour plates, lettering, etc. They can be made from brass or stainless steel.

In the manufacturing process, care should be taken to ensure that threaded inserts are fixed and aligned correctly in the material, otherwise they should be avoided.

Care must be taken when using threaded inserts to avoid detachment of the insert within the elastomer.

#### ballast

Ballast could be needed to achieve good buoy stability. For using a buoy type in different marine conditions, the ballast weights  may be adjustable.

Material: Steel, cast iron, concrete, pig iron, as part of the chain

### swimming stability

For a good hydrostatic design information regarding current, tidal range, wave height, wave interval, wind speed and water depth at the deployment location is needed. The IALA guideline “1099 on the hydrostatic design of buoys” gives detailed information.

## advantages of elastomer polyurethane buoys

The main advantages can be summarised in the following items:

- Fully elastic float, which provides a great recovery capacity without damages against collisions and impacts.

- Upon an impact/collision, they easily recover their original shape.

- In an improbable case of damage on a big collision, it is much easier to repair surface fissures with products of easy application.

- Core made from closed-cell polyethylene foam, with zero water absorption, of one solid piece with great flexibility.

- High Buoyancy: they allow for boarding at the time of maintenance without losing stability.

- Reinforced buoy Stability thanks to its superstructure & tail/skail made from hot-dip galvanized steel, which confers strength & stability to the buoy, and high resistance.

- Anti-sliding surface for better safety during maintenance works.

- Multiple float diameters and volumes available, as they need no mould and so can be quickly made to measure.

- Light float allowing a great chain capacity.

- High Colour Stability against sunlight and UV, avoiding colour degradation.

- Longer service life thanks to its flexibility and impact absorption, thus allowing a float warranty of more than TWENTY (20) YEARS.

- Possibility to increase or decrease the number of counterweights, in order to combine them with the chain weight. This provides the buoy with a great versatility for its installation in both sheltered and open-sea waters.

- Elastomer Polyurethane surface can be repaired and repainted.

- The elastomer polyurethane admits anti-fouling treatment.

## handling

Installation and maintenance equipment involves applying health and safety standards at Workplace. These requirements vary between countries, so that the local specified regulations will be applied. The health and safety of personnel is a priority; so any tasks to the equipment shall be executed by qualified and trained personnel, to implement them in a safe way.

As the float is a unique piece, depending on the size and volume, a machine is suitable for float mounting and heavy parts handling.

Manufacturer should indicate in his user manual the required machine in each case.

The buoy lifting will be made exclusively from the existing lifting points. Do not intend to lift the buoy from some other part of the superstructure to avoid damage to the unions.

The following instructions are very important for a correct use of the Equipment. Please ensure to:

- Comply with worker security provisions and professional regulations.

- Equip all personnel with personal protective measures (PPE) such as gloves or safety shoes or other equipment needed when manipulating components.

- Do the tasks in the presence of a health and security manager that can provide assistance in case of accident.

- Follow the assembly sequence indicated in the manufacturer.

- Have the adequate tools for the assembly of the components.

- Keep a copy of these instructions near the installation site.

As for others plastic material buoys, during the installation, the following indications should be followed:

- Check the correct condition of the elements during the assembly, and ensure their fixing.

- Advise the movements of suspended heavy pieces of equipment and the circulation of machineries during the transport of the pieces.

- Do not start a new step in the assembly tasks until having completed the previous one.

- Do not use components of the buoy as support points during the installation.

- Check the stability of the entire equipment mounted prior to its use.

Regarding the deployment of the elastomer buoys, any different could be taking into account concerning other plastic materials buoys.

Long term storage:

The storage should be done according to the manufacturer instructions.

When plastic buoys are stored outside for a long time (for example on a buoy yard) they should be protected against UV to prevent them from premature aging.

## repair & maintenance

### general

Maintenance is necessary to ensure that equipment and systems of aids to navigation continue operating at the levels required for navigators to navigate the world's waterways safely. In order to extend the buoy lifetime, it is recommended to follow these maintenance guidelines, developed following the IALA Guideline No. 1077 on Maintenance of aids to navigation.

### periodicity

The life of any buoy depends on local operating conditions, as location, sea conditions in the area, water depth, bottom type, presence of abrasive particles into the water, flow velocity, exposure to boat traffic, etc.. The faster wear will appear on buoys located in offshore areas, exposed to harsh sea or which are located in an area with a higher risk of impacts with boats because they delimit a narrow zone of passage.

A checking and replacement program of worn components must be made to maintain a safe operation of the equipment. Historical information is very important to forecast life buoys or beacons in specific locations.

In any case, it is convenient to make exhaustive buoy maintenance on land every 5 years.

### float and tail

The main maintenance to perform in these parts is directly related with the marine incrustations. So that, submerged parts of the float, tail and ballasts should be inspected at least once a year as minimum.

To eliminate the incrustations produced in the submerged part of the float, scratching or pressure water cleaning will be employed. For scratching, a plastic tool, even metallic tool to the float will be used.

In order to reduce incrustations, the application of antifouling painting is recommended. Apply the indicated reference or similar: HEMPEL’S ANTIFOULING NAUTIC 7690B

If there are very serious incrustations, the buoy will have to be lifted, and periodically cleaned.

The purpose of evaluating the tail is to identify the necessary repairs. All the structural elements and connections of the structure will be visually checked to identify obvious marks of corrosion, deformation, fatigue signs and cracking.

In case of detecting corrosion, check the extension by hitting the corroded surface with a hammer, exposing the underlying steel. Removing the corroded area does not alter in any way the structural integrity of the structure. Check mainly unions and screws corrosion, as well as the lack thereof. In case of corrosion, they shall be replaced.

## quality control and testing

A well-designed plastic buoy manufactured in equal and lasting quality can ensure safety requirements.    Also the buoy lifetime can be longer, for example concerning the degradation of colours.

During the manufacturing process of the buoy body and the metal parts some important quality control mechanisms should be applied.

The manufacturer should have an internal quality control principle, for example ISO 9001 or comparable.

If required, each buoy can be delivered with an according quality control report. The content of the report has to be determined according to the customer requirements.

The customer should establish an internal system to monitor the history of the buoy.

The quality control and testing during the manufacture process perform within different phases: during the rolling stage of the closed-cell polyethylene foam sheet, during the interface between the closed-cell polyethylene foam and the elastomer (ensuring the correct adherence) and during the projection phase.

## recycling

Polyurethane is recycled in two primary ways: mechanical recycling, in which the material is reused in its polymer form, and chemical recycling that takes the material back into oligomers or monomers suitable for processing new polyurethanes.

In addition, thanks to its adhesive properties polyurethanes can help recycling other materials such as rubber and wood.

Flexible foam particles such as industrial scrap can be molded and held together with a binder to form a product. Applications include carpet padding, flooring, athletic mats, cushioning, packaging, isolating and acoustical materials.