This is the Working Paper for next ENG session. The TG has a small session planned in London in March to further progress the document. So there will be another input paper to next ENG session. Draft IALA Guideline

1006

On plastic buoys

Edition 4

Document 01/2018

Revisions to this IALA Document are to be noted in the table prior to the issue of a revised document.

| Date | Page / Section Revised | Requirement for Revision |
| --- | --- | --- |
| December 2005 | Entire Document | Reformatted to reflect IALA documentation hierarchy |
| April 2008 | Entire document | Review and update at IALA Floating aids 2008 workshop and EEP11/12. |
| December 2013 | Pages 4,6,7,8 and 9 | References to Guideline 1040 deleted and replaced by Guideline 1077 |
| November 2015 | All pages, all sections | Complete revision and update of the document started |
| April 2016 | All pages, all sections | Complete revision and update of the document started |
| October 2016 | All pages, all sections | Complete revision and update of the document started |
| March 2017 | All pages, all sections | Complete revision and update of the document started |
| October 2017 | All pages, all sections | Complete revision and update of the document |
| January 2018 | All pages, all sections | Complete revision and update of the document |

1.	INTRODUCTION	7

2.	Scope	7

3.	POINTS TO BE CONSIDERED WHEN EVALUATING PLASTIC BUOYS	7

3.1.	Operational Performance	7

3.2.	Life Cycle Cost Comparison	7

3.3.	Plastic Material Types	8

3.4.	Change In Material Properties Of Plastics During Design Life	8

3.5.	Change In Colour Of Plastics During Design Life	8

3.5.1.	General	8

3.5.2.	Ways to assess the expected lifetime of the colour	9

3.6.	Transmission of Forces And Safe Working Load	9

3.7.	Metal parts	9

3.7.1.	Standard parts	9

3.7.2.	Metallic Inserts	10

3.7.3.	Buoy ballast	10

3.8.	Radar visibility	10

3.9.	Static Electrical Charge Build-Up	10

3.10.	Lettering methods	11

3.11.	Design Requirements For Use Of Plastic Buoys In Ice Built Up Areas	12

3.12.	Design Requirements For Use Of Plastic Buoys In Very Hot Climates	12

3.13.	Design Requirements For Use of Plastic Buoys In Extreme Sea Conditions	13

3.14.	Handling and storage	13

3.15.	Repair & Maintenance	13

3.16.	Quality control and testing	13

3.16.1.	General	13

3.16.2.	Quality Assurance Tests	13

3.16.2.1.	Design Confirmation	13

3.16.2.2.	Prototype Testing before series production	14

3.16.2.3.	Manufacturing Quality Control tests	14

3.16.2.4.	Life Cycle Testing	14

3.17.	Recycling / Disposal	15

4.	polyethylene plastic buoys	16

4.1.	polyethylene material - genereal	16

4.2.	mechanical properties and standards for polyethylene	17

4.3.	General considerations with regard to the construction of polyethylene plastic buoys	17

4.3.1.	wall thickness	17

4.3.2.	reserve buoyancy	17

4.3.3.	multi colour possibilities	17

4.3.4.	expansion and shrinkage of polyethylene plastic parts	17

4.3.5.	filling polyethylene plastic buoys	18

4.3.6.	adhesion of colour or foils for buoy lettering	18

4.4.	rotational moulded polyethylene plastic buoys	19

4.4.1.	manufacturing of rotational moulded polyethylene plastic parts	19

4.4.2.	fabrication of rotational moulded polyethylene buoys made by one enclosed module	20

4.4.3.	fabrication of rotational moulded polyethylene plastic buoys made by two or more enclosed modules, welded	21

4.4.3.1.	Fabrication procedure of rotational moulded polyethylene plastic buoys, welded	21

4.4.3.2.	Typical spar- and conical buoys, rotational moulded, welded	21

4.4.3.3.	Use of rotational moulded welded spar- and conical buoys in ice built up areas	22

4.4.3.4.	Typical spars, rotational moulded, welded	23

4.4.4.	fabrication of modular plastic buoys with rotational moulded enclosed modules as floats	23

4.4.4.1.	Modular plastic buoys with complete plastic design	24

4.4.4.2.	modular plastic buoys with hybrid metal/plastic design	25

4.4.4.3.	typical modular plastic buoys with enclosed modules as floats	26

4.5.	high density polyethylene plastic buoys	27

4.5.1.	manufacturing of high density polyethylene plastic parts	27

4.5.1.1.	pipes manufactured by extrusion-process	27

4.5.1.2.	Other high density polyethylene plastic parts	27

4.5.2.	fabrication of high density polyethylene plastic buoys	28

4.5.2.1.	Typical high density polyethylene spar- and conical plastic buoys	30

4.5.2.2.	Typical high density polyethylene plastic spars	31

4.5.2.3.	Use of high density polyethylene plastic buoys in ice built up areas	32

5.	GLASS REINFORCED PLASTIC (GRP)	33

5.1.	General	33

5.2.	Construction	33

5.3.	Example of GRP buoys	33

5.3.1.	Filling	34

5.3.2.	Fasteners / Mooring attachment	34

5.4.	Repair and Maintenance	34

6.	POLYURETHANE / ELASTOMER COATED FOAM (Appendix 4, Figure 5)	35

6.1.	elastomer material – general	35

6.2.	mechanical properties and standards for elastomer plastic	35

6.2.1.	polyurethane elastomer properties	35

6.2.2.	polyethylene solid foam sheet properties	35

6.3.	construction details of elastomer plastic buoys	36

6.3.1.	Manufacturing of plastic parts	36

6.3.2.	assembly of elastomer buoy parts	37

6.4.	types and sizes of elastomer buoys	37

6.4.1.	Multi-colour possibilities of elastomer buoys	37

7.	IONOMER FOAM BUOYS	38

7.1.	General	38

7.2.	Construction	38

7.1.	Example of Ionomer foam buoy	38

8.	Buoy equipment	39

8.1.	Light units	39

8.2.	Monitoring systems and sensors	39

8.3.	Radar reflector	39

8.4.	Racon	39

8.5.	AIS	39

8.6.	Top marks	40

8.7.	Retroreflective sheeting	40

9.	ACRONYMS & Definitions	41

9.1.	Acronyms	41

9.2.	Definitions	41

10.	REFERENCES	41

List of Tables

Table 1: recycling possibilities of different materials used for plastic buoys	15

Table 2: polyethylene types and the manufacturing processes	16

Table 3: small harbour or river markers	20

Table 4: Typical spar- and conical-buoys, welded	21

Table 5: Typical spars, rotational moulded, welded	23

Table 6: Typical Modular buoys	26

Table 7: typical high density polyethylene spar- and conical-buoys	30

Table 8: typical high density polyethylene plastic spars	31

Table 9: polyethylene foam properties	35

List of Figures

Es konnten keine Einträge für ein Abbildungsverzeichnis gefunden werden.

# INTRODUCTION

A plastic buoy may be defined as a floating aid with at least the buoy hull constructed of a plastic material.  Plastic buoys have been in production and use since the 1980’s.

Plastic buoys are commercially available in a wide variety of sizes and shapes, from small one-piece buoys with a diameter of 0.25m to very large modular buoys with diameters of 4.00m. Plastic buoys can be classified as Unitary (one-piece) buoys or Modular (multiple component) buoys.

They are produced mainly from polyethylene materials in different designs.

# Scope

This guideline has been developed to assist aids to navigation (AtoN) manufacturers and authorities when developing and selecting plastic buoys for different purposes. It also provides information about plastic material types; manufacturing techniques; quality control considerations; and standard test procedures commonly in use.

# POINTS TO BE CONSIDERED WHEN EVALUATING PLASTIC BUOYS

## Operational Performance

Due to the lower material density of plastic when compared to steel, plastic buoys are typically significantly lighter than steel buoys.  Lightweight buoys require careful design to avoid a rapid rolling or pitching motion which will detract from their operational effectiveness in waves, wind and current.

The operational performance of a plastic buoy should be stated for different environmental conditions to permit the selection of the correct buoy design.  There are many different designs of plastic buoys available to accommodate a variety of environmental conditions.  The use of a hydrostatic study for the plastic buoy by an accredited Naval Architect can assist in the buoy selection process. Please refer to IALA guideline “1099 on the hydrostatic design of buoys”.

## Life Cycle Cost Comparison

The use of plastic buoys to replace legacy steel buoys is typically warranted when a lower overall life cycle cost can be achieved while also meeting the operational performance requirements as an Aid to Navigation.

The purchase cost of plastic buoys is dependent on the construction technology. Plastic buoys typically have lower ongoing maintenance costs through the elimination of sand-blasting and painting costs and more significantly, the associated vessel; personnel and transportation costs.  Sea-based maintenance can be achieved on most plastic buoys, including jet spray washing and other normal service tasks. Various maintenance procedures are suitable for different plastic materials.  More guidance is available in “IALA Guideline 1077 On Maintenance of Aids to Navigation”.

However, these savings should be analysed against the overall cost of a steel buoy alternative. See also, “IALA Guideline No. 1047 On Cost Comparison Methodology of Buoy Technologies”.

Plastic buoys typically have a shorter design life than a steel buoy and must be replaced earlier than a steel buoy. Factors that directly affect the anticipated design life of a plastic buoy are the degradation of plastic strength and the fading of the colour.

## Plastic Material Types

The required strength of the plastic hull is dictated by the operational environment (sheltered; exposed; ice; etc.) and buoy handling operations.  Different plastic materials are available for use in the manufacturing of plastic buoys; each type has different properties which provide different performance characteristics.  Some plastic materials may offer better resistance to dense marine fouling than other buoy types.  Plastic buoys should be sufficiently robust to withstand fouling being scraped off, or water jet spraying, regularly throughout the working life of the buoy. For plastic buoys, the following plastic materials are primarily used:

polyethylene

glass reinforced plastic (GRP)

polyurethane / elastomer coated foam

Ionomer foam

Polyethylene is the most common plastic used for the manufacturing of plastic buoys. Therefore, the present guideline mainly deals with polyethylene plastic buoys (chapter 4).

## Change In Material Properties Of Plastics During Design Life

Degradation of plastics due to ultraviolet (UV) light must be considered. The type of plastic material selected and the addition of UV inhibitors used to protect the plastic will impact the design life.  Degradation of the plastic due to UV causes the plastic to become more brittle, this loss of ductility reduces the impact strength of the plastic during the design life. The amount of exposure to UV in the operating environment must be considered, degradation of plastic strength and loss of ductility is accelerated in latitudes with greater exposure to UV energy.

At latitudes with higher UV exposure and higher temperatures, the loss of strength occurs faster than at latitudes with lower UV exposure.  Please refer to Appendix 1 – UV Effect on Polyethylene for greater detail and a methodology to calculate relative UV protection based on latitude (only valid for polyethylene plastics).

The rate of degradation varies based on the type of plastic selected and the addition of UV inhibitors or UV stabilizers to protect the mechanical properties of the plastic. Buoy manufacturers should provide rapid weathering tests of the plastic material to prove their predicted long-term stability of the mechanical properties with respect to UV radiation.

## Change In Colour Of Plastics During Design Life

### General

Also colour fading due to UV radiation is to be expected. The fade resistance of the colour pigment used to colour the base plastic resin will determine the length of time the colour will be compliant with “IALA Recommendation E108 on The Surface Colours used as Visual Signals on Aids to Navigation”.

Therefore, the performance of the pigment system is a crucial factor in determining the anticipated useful life of any plastic components. Colour fading will occur more rapidly in latitudes with greater UV radiation.

It is a common misperception that UV inhibitors and stabilizers are added to protect against the fading of colour.  These additives are used to slow the rate of degradation of the mechanical properties of the plastic and NOT to prevent colour fading.

Colour pigments used for all plastics should be of the highest quality suitable for marine use and UV exposure.

Buoy manufacturers should provide rapid weathering tests of the plastic material to prove their predicted rate of colour fading during the design life with respect to UV radiation.

### Ways to assess the expected lifetime of the colour

A common industry practice to measure colour fading is to use accelerated UV weathering in a Xenon Weatherometer  in accordance with appropriate standards completed by a third party accredited test laboratory.

Standards can be:

ASTM D2565 Standard (Standard practice for calculation of col,our tolerances and colour differences from instrumentally measured colour coordinates)

DIN 6174 (colorimetric evaluation of colour coordinates and colour differences according to the approximatelky uniform CIELAB colour space) revoked?

## Transmission of Forces And Safe Working Load

Due to the lower tensile strength of plastic when compared to steel, the transmission of lifting and mooring loads requires careful consideration.  While mooring loads are typically well distributed throughout the plastic hull during operation as a floating aid, additional loads are imposed during buoy deployment and retrieval.

Most buoys will have both a lifting eye and a mooring eye. Depending on the buoy design, the lifting eye and the mooring eye can be designed as follows:

Integrated as part of the plastic hull

A galvanized steel or stainless steel structure for attachment of the hull floats and super structure

The transmission of forces between the mooring point and lifting point is critical in the safe handling of plastic buoys.  The operational conditions for buoy deployment and retrieval must be considered as sea state and current can result in dynamic loads in lifting of the buoy.

Buoy manufacturers should clearly identify the design of force transmission; ultimate yield and the design factors used to specify Safe Working Load.

## Metal parts

A common plastic buoy may include the following metal parts:

lifting eye(s)

mooring eye(s)

standard parts (fasteners)

inserts

ballast (in the case of cast iron or steel)

The metal parts of a buoy should be selected in such way that no galvanic corrosion is produced. Sometimes it is necessary to insulate metal parts (paint, insulating hull, bitumen coat).

Because of the mooring eye wear an appropriate reserve is required which depends on the maintenance intervals. With measurements during the maintenance process, the wear can be determined. The mooring eye should be replaceable in case of wear.

### Standard parts

It is highly desirable to use non-corrosive standard parts, for example from hot-dipped galvanized steel, marine-grade aluminium, marine grade stainless steel or brass.

### Metallic Inserts

Metallic inserts are used for fastening items to the buoy such as the lantern, colour plates, lettering, etc. They can be made from brass or stainless steel.

In the manufacturing process, care should be taken to ensure that threaded inserts are fixed and aligned correctly in the material, otherwise they should be avoided.

Care should be taken and the right amount of torque should be used when securing fasteners into  threaded inserts to avoid detachment or pull-out from the buoy body.

### Buoy ballast

Ballast is often used to achieve buoy stability. An adjustable ballast weight system provides the ability to optimize performance for a variety of operational and environmental conditions.

If the ballast is permanently mounted inside the buoy, it must be secured in place so that no movement is possible.

## Radar visibility

Plastic buoys require the use of a passive radar reflector to be visible to radar. A radar reflector is a passive device designed to enhance the radar conspicuity of aids to navigation. Chapter 4.9.1 “Radar Reflectors” of the IALA NAVGUIDE and chapter 8.3 provide more information.

Most plastic buoys are equipped with a radar reflector, mounted inside or outside of the buoy body. When a radar reflector is integrated inside of the plastic buoy, the plastic material must have low radar attenuating characteristics to avoid decreasing the performance of the radar reflector.

Buoy manufacturers should provide third party test data from an accredited laboratory. It should be avoided to mount the radar reflector behind conducting components, for example solar panels, lettering plates, etc.

## Static Electrical Charge Build-Up

It may be necessary to incorporate a grounding strap on plastic buoys to prevent the build-up of static electricity which may cause shock or damage to electronic equipment.

## Lettering methods

Figure 1

Most administrations apply the position name/number on the buoy body. Solutions for long-term stability of the lettering should be explored. Possible solutions can be (not applicable on all buoy types):

Figure 2

Painting (Figure 1, Figure 2)

Figure 3

Application of adhesive foils (Figure 3)

Mounted plates (welded or fixed by screws, Figure 4 )

Engraving (Figure 5)

Plastic spray method (Figure 6)

Mould-In-Graphic (only for long term use of the buoy on the same position, Figure 7)

Figure 4

Figure 5

Figure 6

Figure 7

## Design Requirements For Use Of Plastic Buoys In Ice Built Up Areas

A year-round use of plastic buoys can save money as winter work and using fleet or contractors to retrieve buoys can be reduced. Some plastic buoys, especially spar and conical shaped buoys are suitable for ice conditions.

The main reasons for ice damage to buoys is insufficient strength in the buoy hull due to a lack of thickness and abrasion due to the selection of plastic material type. Changes in wall thickness also present stress concentration points at the transition of thickness area, therefore wall thickness should be consistent.

When a buoy is in contact with ice floes it can be exposed to impacts; abrasion; cutting and compression.  The buoy hull material must be sufficiently robust to withstand these forces.

The buoy should be strong enough to go under the ice and survive until the ice floe has moved away.  The buoy shape, strength, lifting and mooring points should be constructed accordingly, the size of the lifting eyes frequently requires a compromise between minimum size for ease of handling and reducing the points for ice accretion.

When possible, top marks should be avoided in areas that see ice build-up. If installed, a disposable solution is possible, but environment protection should be considered.

In particular polyethylene plastic buoys are suitable for use under ice conditions, see chapters 4.4.3.3 and 4.5.2.3.

Additional information is available in the Report of the “IALA Workshop on Challenges of Providing AtoN Services in Polar Regions” and the “IALA Guideline No. 1108 On The Challenges of Providing AtoN Services in Polar Regions”.

## Design Requirements For Use Of Plastic Buoys In Very Hot Climates

Careful design considerations should be made when proposing plastic buoys in very hot climates (equatorial regions) as some effects could severely impair the performance of the equipment in place.

The following are examples of problems that may result from prolonged high temperature exposure to plastic material. They should be considered to help determine if the design is suitable for the application (this list is not intended to be inclusive).

parts that bind or corrode from differential expansion of dissimilar materials

materials change in dimension, either totally or selectively

packing, gaskets, seals, etc. become distorted, bind, and fail causing mechanical or integrity failures

gaskets display permanent set

closure and sealing strips deteriorate

shortened operating lifetime

colour fading, cracking or crazing of plastic materials

outgassing of composite materials

The high rates of solar radiation (UV) in these regions can cause surface temperatures to increase by 15 to 30°C  above ambient temperatures, surface temperatures can reach 80°C.  As a result, it is important to consider studies made by various manufacturers comparing material degradation, reaction and resilience under these extreme conditions. For additional information, please see the draft “XXXXX IALA Guideline on Providing AtoN Services in Extremely Hot and Humid Climates”.

## Design Requirements For Use of Plastic Buoys In Extreme Sea Conditions

Plastic buoys can be used in most sea conditions. However, extreme sea conditions (breaking waves, hurricane, debris) will cause high mechanical stress to buoys. The potential for extreme environmental conditions should be considered when selecting plastic buoys to ensure the design and materials are sufficiently robust to achieve survival.

## Handling and storage

The handling of a plastic buoy generally does not differ from steel buoy handling. The weight of a plastic buoys is typically less than steel buoys making them easier to manoeuvre. The equipment required to lift plastic buoys into place can be a reduced and does not require the same lifting capacity as steel buoys.

Long-term storage:

The storage should be done according to the manufacturer instructions (for example to avoid deforming of spar buoys).

When plastic buoys are stored outside for a long time (for example on a buoy yard) they should be protected against UV to prevent them from premature aging and fading.

## Repair & Maintenance

Maintenance procedures are outlined in IALA Guideline “No.1077 on Maintenance of Aids to Navigation”, chapter 2 synthetic buoys.

Polyethylene plastic buoys can be repaired by trained technicians using hot fusion welding equipment in the required colours.

Modular buoys permit the replacement of components that are damaged beyond repair and thus avoid a total loss.

## Quality control and testing

### General

A well-designed and manufactured plastic buoy of good and lasting quality can provide reliable performance at sea for many years with good colour retention and safety of handling.

During the manufacturing process of the buoy body and the metal parts, some important quality control mechanisms should be applied:

The manufacturer should have an internal quality control principle, for example ISO 9001 or comparable.

If required, each buoy can be delivered with a quality control report. The contents of the report should be determined beforehand and satisfy the customer’s requirements.

The customer should establish an internal system to monitor the life cycle of the buoy.

### Quality Assurance Tests

In order to ensure the buoy longevity, the following quality tests can be applied.

#### Design Confirmation

Prior to production of prototypes, the design should be thoroughly reviewed to confirm performance expectations, the following reviews are recommended:

Hydrostatic and hydrodynamic analysis to determine anticipated performance

Approval of design for transmission of loads

#### Prototype Testing before series production

After manufacturing the first samples of plastic parts these could be checked according to the requirements:

Measurement of the overall dimensions of each part

Measurement of the weight of each part

Measurement of the wall thickness on different points if applicable

Check the water tightness of the enclosed modules by pressure tests

Check the surface

Chromaticity measurements

Mechanical tests

Sawing of the compartments to get detail information if applicable  – destructive testing

In addition to the measurements described above, the following tests should be performed on the assembled prototype buoys:

Tension tests up to the anticipated break load for all Lifting and Mooring points

In water hydrostatic stability tests to confirm actual performance versus anticipated performance

#### Manufacturing Quality Control tests

Dependant on customer requirements the following tests can be performed on each buoy body or batch:

Measurement of the overall dimensions

Measurement of the weight

Measurement of the wall thickness at different points

Checking the water tightness

Tension tests up to a specified work load

Check the surface finish

Chromaticity measurements (in accordance with IALA E108 standard)

#### Life Cycle Testing

In accordance with “IALA Guideline 1077 On Maintenance of Aids to Navigation”, the buoy should be tested periodically :

Chromaticity measurement to ensure continued compliance with the requirements of “IALA Recommendation E108 on The Surface Colours used as Visual Signals on Aids to Navigation”.

Inspection of the buoy for deterioration, tension tests to verify assumptions regarding the anticipated useful life and safety of all lifting components.

## Recycling / Disposal

Buoy designs and materials should be selected to minimize their environmental impact upon disposal at the end of their useful life. Considerations should be given to the three “R’s” of environmental protection, namely Reuse, Waste Reduction and Material Recycling.  Also, it is desirable that manufacturing processes be environmentally friendly. The buoy design proposed is 100% recyclable.

Additional Information can be found in Chapter 6.9 of “IALA Guideline 1036 Environmental Considerations in Aids to Navigation Engineering”.

The following table give information about the recycling possibilities of different materials used for plastic buoys.

| Component | Material Type | Ease of Recycling | Recycling Method |
| --- | --- | --- | --- |
| Hull | Polyethylene | Easy – Readily Accepted | Plastics Recycling Depot |
|  | Polyurethane Foam | Is to separate from the other buoy materials | Plastics Recycling Depot |
|  | glass reinforced plastic (GRP) | Not recyclable |  |
| Foam Filling | Fused Expanded Polystyrene | Easy – Readily Accepted | Plastics Recycling Depot |
|  | Polyurethane Foam | Is to separate from the other buoy materials | Plastics Recycling Depot |
| Tower | Polyethylene | Easy – Readily Accepted | Plastics Recycling Depot |
|  | Aluminium | Easy – Readily Accepted | Metal Recycling Depot |
| Radar Reflector | Aluminium | Easy – Readily Accepted | Metal Recycling Depot |
| Ladders & Railings | Stainless Steel | Easy – Readily Accepted | Metal Recycling Depot |
|  | Aluminium | Easy – Readily Accepted | Metal Recycling Depot |
| Core Structure | Polyethylene | Easy – Readily Accepted | Plastics Recycling Depot |
|  | Galvanized Steel | Easy – Readily Accepted | Metal Recycling Depot |
| Lifting & Mooring Connection Bars | Stainless Steel | Easy – Readily Accepted | Metal Recycling Depot |
|  | Galvanized Steel | Easy – Readily Accepted | Metal Recycling Depot |
| Threaded Inserts | Stainless Steel | Easy – Readily Accepted | Metal Recycling Depot |
|  | Brass | Easy – Readily Accepted | Metal Recycling Depot |
| Fasteners | Stainless Steel | Easy – Readily Accepted | Metal Recycling Depot |
|  | Galvanized Steel | Easy – Readily Accepted | Metal Recycling Depot |
|  | Aluminium | Easy – Readily Accepted | Metal Recycling Depot |
| Ballast | Concrete | Easy – Readily Accepted | Clean Fill Designated Infill |
|  | Steel | Easy – Readily Accepted | Metal Recycling Depot |
|  | Cast Iron | Easy – Readily Accepted | Metal Recycling Depot |

- Table 1: recycling possibilities of different materials used for plastic buoys

# polyethylene plastic buoys

## polyethylene material - genereal

Polyethylene is a thermoplastic, at a temperature of about 100 °C it behaves plastically and after cooling the material solidifies. Thus, it can be easily formed and welded under the influence of heat. This provides the ability to make repairs to plastic buoys made of polyethylene. The high ductility and the high cold break resistance are advantageous.

Within the polyethylene family, there are different types that have different densities and molecular structures and therefore different material properties. The most common types used in the manufacturing of plastic buoys are:

Linear low-density polyethylene (LLDPE)

Low-density polyethylene (LDPE)

Medium density polyethylene (MDPE)

High density polyethylene (HDPE)

The following table gives an overview about the polyethylene types and the manufacturing processes for each.

| Polyethylene Resin Type | Rotational Moulding process | Extrusion process |
| --- | --- | --- |
| Low Density , Linear Low Density , Medium Density | X |  |
| High Density |  | X |

- Table 2: polyethylene types and the manufacturing processes

The key difference between the two methods of forming the plastic is the use of pressure.

The rotational moulding process uses only heat to transform plastic resin into a finished shape.

Plastic pipes and plates manufactured in an extrusion process are formed using heat under high pressure which forms strong molecular chains resulting in greater strength, impact and abrasion resistance.

The different polyethylene types and their different manufacturing processes lead to 2 main polyethylene plastic buoy types:

“rotational moulded polyethylene plastic buoys” made of plastic parts fabricated by the rotational moulding process, see chapter  4.4.

“high density polyethylene plastic buoys” made of plastic parts fabricated with High Density polyethylene pipes, plates and components, see chapter 4.5

## mechanical properties and standards for polyethylene

The following  mechanical properties of polyethylene material must be carefully chosen as base for a high quality plastic buoy. They can be tested according to the standards named in brackets behind them.

density (ISO 1183/ASTM D-4883/ASTM D-1505)

hardness (DIN 53505)

yield strength (DIN EN ISO 527-1, DIN EN ISO 527-2)

fracture Strength (DIN EN ISO 527-1, DIN EN ISO 527-2)

elongation (DIN EN ISO 527-1, DIN EN ISO 527-2)

abrasion resistance (DIN 53516)

impact resistance (ISO 6603/02)

## General considerations with regard to the construction of polyethylene plastic buoys

### wall thickness

The wall thickness of the plastic parts should be optimized for the buoy size and shape; material degradation during design life and the environmental conditions to ensure the buoy is sufficiently robust.  The range is from 5 – 40 mm.

### reserve buoyancy

The composition of a buoy of several enclosed modules offers the advantage that a reserve of buoyancy remains in case of damage to one or modules.

A reserve buoyancy also can be achieved by filling the buoy body with floatation material according to chapter 4.3.5.

### multi colour possibilities

The composition of a buoy of different parts or several enclosed modules offers the advantage that multi-colour buoys can be realised. Examples of these buoys can be found in the chapters in which the different buoy types are described.

### expansion and shrinkage of polyethylene plastic parts

Polyethylene material will expand and contract about 3 to 5 %, depending on the colour and ambient temperature. Care should be taken in the design to ensure compatibility between different materials (e.g. elongated or oversized clearance holes).

### filling polyethylene plastic buoys

Polyethylene plastic buoys can be filled with polystyrene or polyurethane foam, which can have the following advantages:

Filling can increase the impact stability/shock resistance.

In case of leakage the filling can secure the buoy from sinking.

Figure 8

If filling is used, it must be of the highest quality closed-cell specification to prevent water absorption.

Information about the density and the water absorption behaviour of the foam should be taken in to consideration.

Figure 9

Filling material should be of sufficient quality to survive the expected lifetime of the buoy.

Some disadvantages may exist in the use of foam filling:

Some polyurethane foam types may not be recyclable. Furthermore the combination of polyethylene and foam is not easy to separate.

For filling in foam into the floats additional holes are necessary. These are weak spots and must be closed carefully after the filling.

Figure 10

Figure 8 shows a rotational moulded float filled with polystyrene foam, Figure 9 shows a polyurethane foam filled float. High density polyethylene buoys are frequently filled with polystyrene billets as shown in Figure 10.

### adhesion of colour or foils for buoy lettering

Especially polyethylene provides poor adhesion for conventional paints or foils for buoy lettering. Specialized hot plastic spraying processes or “Mould In Graphics” are available and have been used successfully. For further information see chapter 3.10.

## rotational moulded polyethylene plastic buoys

Figure 11

Available on the market is a great variety of different types and sizes of rotational moulded polyethylene plastic buoys. Depending on the type, size/diameter and area of application different designs of polyethylene plastic buoys are existing. Generally, small buoys are made from one or more enclosed modules, while larger types may be modular plastic or hybrid metal/plastic.

The following chapters give an overview of the manufacturing procedure of rotational moulded plastic parts and typical rotational moulded plastic buoys.

### manufacturing of rotational moulded polyethylene plastic parts

Rotational moulding can be used for the production of large, hollow, seamless plastic parts (enclosed modules). During the rotational moulding process the base resin (Low Density , Linear Low Density , Medium Density) is transformed with heat only.

Figure 12

A thin-walled hollow mould gives the outer shape of the plastic part. The mould is filled with plastic, is then slowly rotated bi-axially, and heated. The melting temperature of the plastic depends on the plastic material used (Figure 11 and Figure 12).

Figure 13

During  the cooking process, the plastic resin becomes molten and slowly settles on the inner mould surface, the bi-axial rotation is programmed to create a relatively uniform distribution of the plastic, the plastic is heated until it is properly cured and then the cooling phase of the process begins. The wall thickness depends on the amount of plastic resin used and this will determine the amount of time required to properly cure the plastic. Wall thicknesses may be from 6 mm to 35 mm depending on the required strength and design of the buoy (Figure 13).

Figure 14

It is also possible to integrate metal parts into the plastic parts during the moulding process used for mooring and lifting and fastening systems (Figure 14).

Rotational moulding is particularly suitable for small to medium series production. The advantages are the relatively low mould costs and the almost unlimited possibilities of shaping.

Figure 15

The enclosed modules, manufactured as described above, can either be used directly as a buoy, be welded to buoys or mounted as floats on a core structure.

Figure 16

Figure 15 shows a big enclosed module (float, length 2.17 m, outer radius 1.21 m, wall thickness 20 mm), Figure 16 shows a small enclosed module (small marker, 0.5 m diameter, 0.7 m height).

### fabrication of rotational moulded polyethylene buoys made by one enclosed module

Figure 17

Rotational moulded plastic buoys made of 1 enclosed module are often used as small harbour or river markers.

The lifting and the mooring eyes are made as a part of the plastic body (Figure 17) or from additional metal components (Figure 18).

Figure 18

The application of these (small) plastic buoys usually requires only a monochrome version, the multi-colour variant is not needed.

Typical technical data are:

| Parameter | Value |
| --- | --- |
| Application area | harbour, rivers, marinas |
| diameter in the water line (m) | ≈ 0,5 |
| height above water line/focal plane (m) | 2 |
| height over all (m) | 3 |

- Table 3: small harbour or river markers

### fabrication of rotational moulded polyethylene plastic buoys made by two or more enclosed modules, welded

#### Fabrication procedure of rotational moulded polyethylene plastic buoys, welded

Figure 19

Buoys, which consist of two or more enclosed modules, are usually welded together from rotational moulded plastic parts. Figure 19 and Figure 20 are showing the welding process.

Figure 20

The advantages of this modular design using enclosed modules can be:

The wall thickness of the lower elements can be made bigger than from the upper elements because of stability and ballast reasons.

The underwater elements do not necessarily have to be executed in the traffic-efficient colour (cost savings).

Multi-colour buoys can be realized easily.

The buoy can be divided into a few waterproof sections (reserve buoyancy).

The radar reflector and other devices can be placed easily inside the buoy body.

#### Typical spar- and conical buoys, rotational moulded, welded

Widely used spar- and conical buoys up to 1.5 m are the buoys described in the following table (3 typical sizes).

| Parameter | big spar/conical buoy | middle spar/conical buoy | small spar/conical buoy |
| --- | --- | --- | --- |
| Application area | see, coast, estuary | coast, estuary | estuary, shallow water |
| Biggest diameter in the water line (m) | ≈ 1.0 - 1,6 | ≈ 0.8 - 1,0 | ≈ 0.4 - 0.8 |
| Height above water line/focal plane (m) | ≈ 3 | ≈ 2.6 | ≈ 2 |
| Height over all (m) | ≈ 6 | ≈ 5-6 | ≈ 2-5 |

- Table 4: Typical spar- and conical-buoys, welded

Figure 21

Figure 22

Figure 23

Figure 21 and Figure 22 are showing examples. Figure 23 shows an exploded drawing and the possibility to realize multi-colour plastic combinations: By welding individual plastic parts or enclosed modules, the required color combinations can be realized.

Figure 24

#### Use of rotational moulded welded spar- and conical buoys in ice built up areas

For general demands concerning the design and use of plastic buoys in ice conditions, see chapter 3.11. Rotational moulded welded plastic buoys may be used in operational areas with light ice conditions. An example of a rotational moulded conical buoy in light ice is shown in Figure 24.

It is the movement of ice and especially free flowing ice that causes damage to the buoys. The type of rotational moulding polyethylene and the wall thickness of the hull are critical for survival. Manufacturers should state the ice resistance capability for rotational moulded plastic buoys. In aggressive ice conditions, the use of high density polyethene plastic buoys (see chapter 4.5) with greater strength and abrasion resistance are recommended.

#### Typical spars, rotational moulded, welded

Spars with the following characteristics are common, two typical types are shown:

| Parameter | Small spar | Medium spar |
| --- | --- | --- |
| Application area | Marinas, Inland waters | Coastal, Ports, Inland waters |
| Diameter (m) | 0,25 – 0,40 | 0,40 – 0,60 |
| Height above water line/focal plane (m) | 0,75 – 1,50 | 1,50 – 2,00 |
| Height over all (m) | 2,00 – 3,00 | 4,00 – 5,00 |

Figure 25

Figure 26

Table 5: Typical spars, rotational moulded, welded

Figure 25 and Figure 26 are showing examples.

### fabrication of modular plastic buoys with rotational moulded enclosed modules as floats

For bigger plastic buoys (diameter more than 1.5m up to 4m) rotational moulded enclosed modules are used as floats.

The floats are mounted on a core structure, which consists of plastic pipes (complete plastic design, chapter 4.4.4.1) or a metal construction (hybrid metal/plastic design, chapter 4.4.4.2).

The advantage of the modular design are:

The modular design can simplify handling and transport.

Defective parts can be changed easily.

A negative aspect is that those plastic buoys are not suitable for use under ice conditions.

#### Modular plastic buoys with complete plastic design

Figure 27

Modular buoys with a plastic core structure (complete plastic design) are consisting at least of the following elements (Figure 27):

enclosed modules as floats

polyethylene tail tube

polyethylene top structure

mooring and lifting eyes made of steel

cast iron ballast weight

Figure 28

The main advantage of those buoys is that no maintenance is required (except the mooring and lifting eyes).

Multi-colour-combinations can be realised as follows:

The floats can be made of different colours and combined according to the needed colour combination, on the polyethylene top structure coloured polyethylene plates can be mounted (Figure 28).

Figure 29

The so called “Mould-In –Graphics” can also be used to create multi-colour buoys (Figure 29).

#### modular plastic buoys with hybrid metal/plastic design

Figure 30

Modular buoys with hybrid metal/plastic design are consisting at least of the following elements (Figure 30):

enclosed modules as floats

steel tail tube or skirt

aluminium or plastic top structure

mooring and lifting eye made of steel

cast iron ballast weight

Multi-colour-combinations can be realised as follows:

The floats can be made of different colours and combined according to the needed colour combination, an aluminium top structure can be painted with different colours (Figure 31).

Figure 31

On a polyethylene top structure coloured polyethylene plates can be mounted. Another possibility is the mounting of a cap with the needed colour combination on the buoy body.

#### typical modular plastic buoys with enclosed modules as floats

Figure 32

The following sizes of modular plastic buoys with polyethylene floats are typical, regardless of whether it is the complete plastic design (chapter 4.4.4.1) or the hybrid metal/plastic design (chapter 4.4.4.2):

| Parameter | small modular spar/conical buoy | middle modular spar/conical buoy | big modular spar/conical buoy |
| --- | --- | --- | --- |
| Application area | coastal, shelter, rivers, ports | open sea, coastal, estuary | open sea estuary |
| Biggest diameter in the water line (m) | 1.5/1.8/2 | 2.2 -2.6 | 3-4 |
| Height above water line/focal plane (m) | 1.7- 4.2 | 3.8- 6.5 | 5-8 |
| Height over all (m) | 2.7-7.9 | ≈ 8.6 | 12-15 |

- Table 6: Typical Modular buoys

Figure 33

Figure 32 and Figure 33 are showing plastic buoys in complete plastic design.

Figure 34

The buoy shown in Figure 34 is an example for a hybrid metal/plastic design.

It is equipped with grey polyethylene floats and a high visibility metallic spar, offering the day mark of the buoy. See IALA 1094 Guideline for additional information regarding day marks.

## high density polyethylene plastic buoys

### manufacturing of high density polyethylene plastic parts

#### pipes manufactured by extrusion-process

Figure 35

Plastic extrusion is a high-volume manufacturing process in which plastic is melted and formed into a continuous profile. The base resin is transformed with heat under significant pressure. This process is used to produce tubes/pipes, plates etc.

The significantly higher molecular weight of the high density resin and the extrusion process create a material with significantly greater strength, abrasion and impact resistance than the polyethylene formed in rotational moulding.

Figure 36

The process starts with feeding plastic from a funnel into the extruder. In the extruder, the plastic is compacted by a rotating screw, melted and pressed through a nozzle. The nozzle gives the end product its profile. This is followed by the cooling process, which is usually achieved by a water bath. Figure 35 shows pipe manufacturing by extrusion process.

Pipes can be extruded in a single colour or they may be extruded with the outside 20% in a separate colour, this process is called “co-extrusion”, the main part of the wall thickness is in black. (Figure 36).

Figure 37

Pipes used for polyethylene buoys are mainly used in pressured lines like water and other liquids. The most common material is HD 100 polyethylene. The wall thickness and the pressure class vary depending on the SDR (side to diameter ratio). Typical for buoy applications are SDR 17 and SDR 26. Figure 35 shows extruded pipes as raw material for spars.

#### Other high density polyethylene plastic parts

Figure 38

Other polyethylene plastic parts (mainly the smaller and special parts) can be made by the cutting of high density polyethylene plates, pipes and compression moulded parts, etc., see Figure 38 . Also a combination with metal parts is possible (Figure 39).

Figure 39

### fabrication of high density polyethylene plastic buoys

High Density Polyethylene plastic buoys are fabricated by skilled technicians using Extruded HDPE Pipe, HDPE Plates and small HDPE parts. The fabrication process includes the cutting and welding of the components to create the desired design shape.

A number of different design shapes can be achieved but there are some limitations based on the diameters of extruded pipes used as floats. As a result, the majority of buoys have a Spar type shape with a length to diameter ratio of 5-15 to 1.

Larger buoys are fabricated with bulkheads to form several watertight buoyancy modules that offer the advantage of reserve of buoyancy in case of damage to one or more segments. Additional security of the reserve buoyancy is also achieved by filling the buoy body with floatation material like polystyrene, see chapter 4.3.5.

Buoy fabrication by welding together extruded pipe sections is particularly suitable for small series production and customized buoy solutions. The advantages are a robust body of extruded pipe with the possibility to integrate components and devices inside the buoy body. It is possible to attach metal parts with bolts parts or plastic inserts by extrusion welding. In either case the skin of the buoy distributes loads evenly to the whole buoy body.

Standards for the extrusion-made pipes are:

EN 12201-1, Plastics piping systems for water supply Polyethylene (PE). Part 2: Pipes

EN ISO 1133, Plastics – Determination of the melt mass-flow rate (MFR) and the melt volume-flow rate (MVR) of thermoplastics (ISO 1133:1997)

EN ISO 2505, Thermoplastics pipes.  Longitudinal reversion. Test method and parameters (ISO 2505:2005)

EN ISO 3126, Plastics piping systems – Plastics piping components – Measurement and determination of dimensions

EN ISO 6259-1, Thermoplastics pipes. Determination of tensile properties. Part 1: General test method (ISO 6259-1:1997)

EN ISO 13920, Welding- General tolerances for welded constructions – Dimensions for length and angles Shape and position

ISO 6259-3, Thermoplastics pipes – Determination of tensile properties – Part 3: Polyolefin pipes

Figure 40

ISO 13953, Polyethylene (PE) pipes and fittings – Determination of the tensile strength and failure mode of test pieces from a butt-fused joint

ISO 16770, Plastics – Determination of environmental stress cracking (ESC) of polyethylene – Full-notch creep test (FNCT)

ISO/TR 10358, Plastics pipes and fittings – Combined chemical-resistance-classification table

HDPE pipes can be joined together with a heat and pressure process known as Fusion or Mirror Welding, the resulting fusion weld is stronger than the pipe (Figure 40). This process allows pipes of different colours to be joined together and permits the creation of watertight sections with the addition of internal bulkheads.

Figure 41

HDPE plates and parts can be joined to the pipes using an HDPE Extrusion Welding process using heat to bond molten HDPE welding wire to the surfaces between pipe and plate (Figure 41). This process is typically used to add strengthening plates for Lifting and to make transitions between components strong and watertight.

Available on the market is a great variety of different types and sizes of high density polyethylene plastic buoys. The following chapters give an overview about the most common types.

The possibilities to produce multi-colour plastic buoys according to the IALA maritime buoyage system (MBS) are as follows:

Enclosed modules can be made of different colours. They can be welded together according to the needed colour combination.

Extruded pipes can be manufactured in multi colour combinations (for example red-white). The different plastic pipes can be welded (Figure 42).

Figure 42

Other possibilities are the welding of coloured plastic plates on the buoy body or the mounting of a cap with the needed colour combination .

#### Typical high density polyethylene spar- and conical plastic buoys

Figure 43

Widely used as spar- and conical buoys up to 1.5m are the buoys described in the following table (3 typical sizes). Figure 43, Figure 44 and Figure 45 are showing examples.

| Parameter | big spar/conical buoy | middle spar/conical buoy | small spar/conical buoy |
| --- | --- | --- | --- |
| Application area | see, coast, estuary | coast, estuary | estuary, shallow water |
| Biggest diameter in the water line (m) | ≈ 1.0 - 1,6 | ≈ 0.8 - 1,0 | ≈ 0.4 - 0.8 |
| Height above water line/focal plane (m) | ≈ 3 | ≈ 2.6 | ≈ 2 |
| Height over all (m) | ≈ 6 | ≈ 5-6 | ≈ 2-5 |

Figure 44

Figure 45

Table 7: typical high density polyethylene spar- and conical-buoys

#### Typical high density polyethylene plastic spars

Figure 46

The most HDPE spars consist mainly of one or more plastic pipe sections manufactured by an extruding-process. The top and the bottom parts are also made of plastic and become mainly fusion welded on the pipe(s).

The buoy can be divided into a few waterproof sections.

Radar reflector and other devices are usually placed inside the buoy body.

Buoys can be easily customized according to specifications.

Figure 47

Some of them can be equipped with a light-unit and a battery compartment (primary battery).

The buoys are usually filled with polystyrene or polyurethane foam.

Some spars can be used can be used as “all-year-round” buoys in ice covered areas as well

Figure 48

Spars with the following characteristics are common, Figure 46, Figure 47 and Figure 48 are showing examples.

| Parameter | Small spar | Medium spar | Big spar |
| --- | --- | --- | --- |
| Application area | Marinas, Inland waters | Coastal, Ports, Inland waters | Offshore, Coastal |
| Diameter (m) | 0,16 – 0,225 | 0,4 – 0,5 | 0,8 – 1,0 |
| Height above water line/focal plane (m) | 2,0 – 3,0 | 2,5 – 3,5 | 3,0- 4,0 |
| Height over all (m) | 2,5 – 6,0 | 6,0 – 9,0 | 8,0 – 11,0 |

- Table 8: typical high density polyethylene plastic spars

#### Use of high density polyethylene plastic buoys in ice built up areas

Figure 49

For general demands concerning ice stable design of plastic buoys see chapter 3.11.

High Density polyethylene buoys are particularly suitable for ice conditions. In aggressive ice conditions, the use of extruded HDPE plastic for increased strength and abrasion resistance is recommended.

The main reason for by ice destroyed plastic buoys are too thin or not homogeneously realized wall thicknesses. The wall thickness must be choosen accordingly (15 – 30 mm) and realized homogeneously while the production process.

Figure 50

The spar buoy shown in Figure 48 can be used in aggressive ice conditions, see Figure 49 (solid ice-field) and Figure 50 (crushed ice).

# GLASS REINFORCED PLASTIC (GRP)

## General

GRP is the usual abbreviation for glass reinforced plastic which in its most common form consists of glass matt bonded by polyester resin.

## Construction

Complex shapes can be produced by laying-up resin and glass reinforcement into a mold by hand (or spray machine). The cylindrical buoy body is normally formed by joining two half body shapes. It is important to note that the joint is often the weakest area of the body.

The strength of GRP is dependent of the ratio of glass fibre to resin and thus this is another area which requires definition and quality control. High strength (required in ice conditions) can be achieved by the use of carbon or Kevlar fibres but the costs may be high. These fibres may be used in specific stress areas of the buoy.

The outer layer of resin, the gel coat, prevents water absorption into the glass reinforcement and should be protected from mechanical damage. This is usually provided by some form of fendering.

## Example of GRP buoys

Figure 51

Figure 51, Figure 52 and Figure 53 are showing samples of GRP buoys.

Figure 52

Figure 53

### Filling

In the event of a collision, a GRP buoy may well crack from an impact which would only dent a steel buoy. To prevent the buoy from sinking the buoy should be divided into separate watertight compartments or filled with polyurethane foam or polystyrene foam.

### Fasteners / Mooring attachment

Care should be taken when bonding metal attachment points into GRP due to the considerable difference in thermal expansion rates between metals and plastics, and the inherent flexibility of the GRP. Another option is to use through bolted fixings with generous backing plates and resilient washers or coatings between the metal and the GRP.

## Repair and Maintenance

GRP buoys will require cleaning, repainting and any necessary repair to the gel coat.

Repair of GRP is usually straightforward but does require standards of cleanliness and specific working temperatures – during the repair process, i.e. dry, 20 degrees Celsius. Effective drying of damaged laminates or foam cores may also be difficult in cold climates. It may be necessary to use heaters to warm and dry damage areas and to ensure effective curing of the repair.

The final surface colour of GRP buoys can be incorporated into the gel coat. If this not the case or if a colour change is required, then buoys will require normal painting to achieve the required surface colours.

GRP buoys may be cleaned onsite using water jetting, however care should be taken to ensure paint flakes and surface materials avoid polluting the surrounding environment.

The area in which a foam filled buoys are used should be considered as oily water in around the Port environment could penetrate the damaged buoys, making the repair of it very difficult.

Maintenance procedures are outlined in IALA Guideline No. 1077.

# POLYURETHANE / ELASTOMER COATED FOAM (Appendix 4, Figure 5)

## elastomer material – general

These buoys typically consist of a thick, flexible marine grade polyurethane elastomer skin on a flexible closed cell foam core. They have the advantage of overall flexibility and resilience. The flexibility will also be an advantage when the buoy has to be lifted or serviced in rough weather.

The main feature of Elastomer Buoys lies in its float, of high elasticity and lightweight, manufactured with closed-cell polyethylene solid foam sheet (no water absorption) and projected with a layer of coloured polyurethane elastomer.

Thanks to its solid construction, they are virtually unsinkable, even against a strong impact. Besides, they can withstand repeated collisions without deforming (recovery capacity). The elastomer polyurethane admits anti-fouling treatment.

## mechanical properties and standards for elastomer plastic

### polyurethane elastomer properties

The following  mechanical properties of polyurethane elastomer material must be carefully chosen as base for a high quality plastic buoy. They can be tested according to the standards named in brackets behind them.

density (BS 4370 PART 1 METH 2)

tensile strength (ISO 527)

ultimate elongation (ISO 527)

hardness (DIN 53505)

breaking resistance (DIN EN ISO 6383-1)

water vapour diffusion resistance (EN 1931)

external fire performance (UNE-EN 13501-5)

fatigue motion resistance (EOTA TR-8)

### polyethylene solid foam sheet properties

| Physical condition | Solid |
| --- | --- |
| Colour | Coloured |
| Smell | lightly perceptible |
| Melting point | 105-110ºC |
| Flash point | 420-440ºC (ASTM 1929) |
| Ignition temperature | 430-450ºC (DIN 54836) |
| Density | From 30 to 100 kg/m3 |
| Water solubility | Insoluble |
| Water absorption | 1-2% |

- Table 9: polyethylene foam properties

## construction details of elastomer plastic buoys

### Manufacturing of plastic parts

Figure 54

Figure 55

The manufacturing process of the elastomer buoy float is based on a solid rolled body of closed-cell polyethylene foam sheet and binding it by heat (Figure 54, Figure 55). No chemical substance is involved in it.

The thickness of the polyurethane elastomer layer projected must be optimized to the size, the shape and the environmental conditions of the buoy to be sufficiently robust. The most common range used is from 8 – 20 mm.

Figure 56

The rolled body is covered by a projection of elastomer polyurethane (Figure 56); thus forming an elastic skin on an elastic core.  So the body buoy is solid, compact, extremely flexible, has a  great recovering capacity and zero water absorption.

Depending on the needs, the thickness of the cover could be adapted. This process provides a great recovering capacity and null water absorption.

Figure 57

The core of the elastomer buoys are manufactured of material of different densities, which allows the adaptation to the needs depending on  location, environmental conditions or external influences that require different densities.

In the upper area of the float, a projection of silica granulation is applied to avoid slides of the maintenance staff (Figure 57); being coated with the applied polyurethane and resulting in a non-slip surface.

In the case of the elastomer buoy parts, the float is a solid part, never manufactured in modules. The process of manufacturing and materials used in the Elastomer floats are the same as those used in fenders of ports for vessel berthing. They are prepared to withstand repeated strong collisions. Thus, the replacement of the float is unexpected.

### assembly of elastomer buoy parts

Figure 58

The assembly involves others parts of the buoy like metal structures, tail, top marks, etc… (Figure 58)

Figure 59

The interface between the plastic part and the metallic part is important to avoid movement or rotation, to a uniform and robust ensemble.

Figure 60

The mounting of the elastomer buoy, depending on the size, has to be made in horizontal for a safe handling and convenient assembly (Figure 59).

## types and sizes of elastomer buoys

Figure 61

As they need no mould, the choice of types and sizes is open to the location’s needs. The diameters of the elastomer buoys at the market are between 0.8 to 3.6 meters, the height of the float can be up to 2.8m. Figure 60 , Figure 61 and Figure 62 are showing examples of elastomer buoys.

Figure 62

### Multi-colour possibilities of elastomer buoys

The colour of the elastomer buoys is integrated in the projected layer of coloured polyurethane elastomer.

This layer should have UV protection, which prevents discolour of the float during its service life.  The elastomer surface admits later repainting.

For realizing multi-colour buoys the elastomer provides good adhesion for conventional paints; specialized hot plastic spraying processes are available and have been used successfully.

# IONOMER FOAM BUOYS

## General

The life and durability of the buoy is entirely dependent on the quality of the foam used. The flexibility of the foam can provide good impact resistance but resistance to aggressive abrasion is not good. This last factor is important for buoys which will dry out on a hard bottom at a tidal site or may be subject to moving ice conditions.

A foam buoy hull can sustain considerable damage or loss of material without sinking. A damaged buoy can not be repaired by the user. The material is not recyclable. Other advantages of foam buoys include their lighter weight which may result in good performance in fast water.

## Construction

Figure 63

These buoys are usually constructed by wrapping closed-cell foam (ionomer foam which is produced in sheet form) around a central structural core, the layers of foam being heat sealed together during the wrapping process. The outer layer of the rolled foam shapes can be "densified" through the application of pressure and heat to make a hard, smooth surface. Pigments are usually incorporated into the foam during the extrusion process, so the colour is continuous throughout the entire hull and daymark. The buoys include a structural steel framework, steel lifting and mooring eyes, and stainless steel connecting hardware.

The manufacturing technique particularly lends itself to the production of one-off designs as a variety of body shapes can be made without the need for a mold. Buoys of this type are significantly lighter than steel buoys of the same size.

## Example of Ionomer foam buoy

Figure 63 shows an example of a ionomer foam buoy.

# Buoy equipment

Similar to steel buoys additional equipment can be mounted in or on the plastic buoy. The following chapters give an overview about the components.

## Light units

Plastic buoys can be equipped with lanterns (powered by solar-, wind- or wave energy respectively by a primary battery or gas) or self-contained lanterns.

Compact self-contained lanterns become increasingly smaller. At the same time, the amount of their functions increases. Chapter 3.2.8 “Integrated Power Supply Lanterns” of the IALA Navguide and the IALA guideline 1064 “Integrated Power Systems Lanterns” give information in detail.

If the plastic buoy is used under ice conditions according to chapters 12, 4.4.3.3 and 4.5.2.3, the self-contained lantern or the stand alone lantern must also be designed to be ice-resistant. At some plastic buoys (especially spars) a primary battery instead of a solar power supply is used then.

## Monitoring systems and sensors

Modern self-contained lanterns can be equipped with a remote monitoring and remote control system or sensors. Depending from the buoy location different communication ways for the data transfer can be used.

The status of the lantern, the power supply and other devices as well as buoy related data can be determined, transferred and displayed. This enables further optimization of the technical maintenance operation, especially with regard to the cost intensive buoy tender fleet.

The IALA Guideline 1008 “Remote monitoring and control of aids to navigation” gives information in detail.

## Radar reflector

A radar reflector is a passive device designed to enhance the radar conspicuity of aids to navigation (Figure 64). Chapter 4.9.1 “Radar Reflectors” of the IALA Navguide provides more information. (more information: paper of Dr. Speckter and VV-WSV 2406).

Figure 64

Most plastic buoys are equipped with a radar reflector, mounted inside or outside of the buoy body.

The advantage of an integrated radar reflector is, that the radar reflector is protected from environment conditions. The disadvantageous effects are:

The retrofitting of a radar reflector could be difficult (if ever required)

The surrounding polyethylene wall reduces the reflection performance of the radar reflector, but according to experience the reduction is not significant The effects have to taken into considerations.

## Racon

A Radar beacon (racon) enhances the radar detection and identification of the object on which it is mounted. For detail information look at chapter 4.9.3 “Radar Beacon” in the IALA-Navguide and the “IALA Guideline No. 1010 on Racon Range Performance”.

## AIS

Buoys can be equipped with AIS-transponders to transmit different messages. Also remote monitoring is possible. For detail information look at the IALA Recommendation “A-126 On The Use of the Automatic Identification System (AIS) in Marine Aids to Navigation Services” and the IALA guideline  “1098 the application of AIS - AtoN on buoys”.

## Top marks

The shape and the dimensions of top marks are described in the IALA guideline 1094. Top marks can also be designed to enhance the radar response.

The use of top marks are normally avoided in ice covered waters because they tend to get damaged during winter.

## Retroreflective sheeting

Figure 65

Plastic buoys can be equipped with retroreflective sheeting, so the mariner can detect the position and colour at night by use of a searchlight (Figure 65).

For detail information look at the IALA Guideline 1094 and the new guideline “retroreflective materials”.

# ACRONYMS & Definitions

## Acronyms

IMO	International Maritime Organization (Acronym style)

## Definitions

Abcde (Body text)

# REFERENCES

Body text

Abcd

Efgh

Advantages and Disadvantages of Plastic Buoys

ADVANTAGES

Plastic does not corrode;

It is easier to maintain; only removal of marine growth, no painting for plastic parts required;

There is less maintenance on shore for the plastic components (no grit blasting, no painting with the exception of GRP) therefore less resources may be utilised;

Plastic buoys are of lower weight (1/2 to 1/3 mass of the equivalent diameter steel buoys). Therefore, the service may be able to use smaller buoy tender;

Whole life costs may be less than steel buoys; see also IALA Guideline No. 1047 On Cost Comparison Methodology of Buoy Technologies

Since the 1980´s plastic buoys have been operated successfully; showing an average life time over 20 years without maintenance need of the buoy  superstructure

There are a number of commercial companies offering plastic buoys;

Most plastic is recyclable;

Where plastic buoys are of modular construction, it is possible to change individual parts or segments if they are damaged or need refurbishment;

Large modular buoys are easier to transport and store, as parts can be disassembled for transit;

The number of spare parts (whole buoys held) can be reduced;

It is possible to encase a radar reflector within a plastic buoy’s superstructure.

DISADVANTAGES

It is more difficult to change the colour of a plastic buoy, as conventional painting is not reliable for plastic surfaces;

Generally plastic buoys have a shorter lifetime than steel buoys this however requires regular maintenance (painting) of the steel buoys, unlike plastic buoys;

Plastic buoy components will be specific to each manufacturer and may therefore not be interchangeable;