IALA Guideline

DRAFT

Application of Retroreflecting Material on Marine Aids to Navigation

Edition x.x

Document date

| Date | Details | Approval |
| --- | --- | --- |

1.	Introduction	5

2.	Scope	5

3.	Retroreflective material for aids to navigation purposes	5

3.1.	Floating Aids to Navigation	5

3.2.	fixed Aids to navigation	6

4.	HISTORY	6

5.	Terminology, PRINCIPLE, basic technology and design	7

5.1.	Reflection and retroreflection	8

5.2.	The glass sphere or bead	8

5.3.	Prismatic or cube corner reflector	9

6.	Characterising and measurement of retroreflecting material	11

6.1.	Coefficient of Retroreflection	11

6.2.	Colour	13

7.	Classification and Standards of Retroreflective Material	13

8.	Consideration when specifying Retroreflective Material	14

8.1.	Floating Aids to Navigation	14

8.1.1.	SMALL BUOYS	15

8.1.2.	LARGE BUOYS	15

8.2.	Fixed Aids to Navigation	19

8.3.	General considerations for Floating and Fixed Aids to Navigation	20

8.3.1.	Colour	20

8.3.2.	Photometric Performance when wet	22

8.3.3.	Temperature	22

8.3.4.	Flexibility	22

8.3.5.	Cleanability	22

8.3.6.	Application of Retroreflective Material	22

8.3.7.	Degradation of Retroreflective Materials	22

8.3.8.	Precaution when using Radar Reflector in combination with Retroreflecting Materials	23

8.4.	Calculation of Size of Retroreflectors	23

8.4.1.	Example of calculation size of retroreflector in a leading line	25

9.	best practice and typically application	27

10.	ACRONYMS & Definitions	33

10.1.	Acronyms	33

10.2.	Definitions	33

11.	REFERENCES	33

List of Tables

Table 1	Example table	33

List of Figures

Har ikke fundet nogen tekst til listen over figurer.

List of Equations

Har ikke fundet nogen tekst til listen over figurer.

Introduction

Retroreflective material has in general widespread use to increase the night time conspicuity.

The most commonly and well-known use is in enhancing the light returned from vehicle headlights to enable the drivers to detect warnings, impart information and aid the driver through the necessary manoeuvres. For this reason road traffic signs are equipped with retroreflective material.

Another application is high-visibility clothing for workers, authority personal etc. to be safely and effectively visible. Equipment for life rafts/boats and life vests use retroreflective material according to SOLAS regulations.

Retroreflective material for marine aids to navigation has a widespread use in narrow and complicated waters and fairways, including ice conditions and long and dark nights during wintertime. Retroreflective material is a cheap and effective way to obtain a high level of night time conspicuity.

The IALA Recommendation R0106(E- 106) describes the nautical requirement for use of retroreflective material on floating aids according to the IALA Maritime Buoyage System (MBS).This guideline will give more detailed information  on what retroreflectivity is and how retroreflectivity is achieved.

Scope

The guideline provides a general informative overview for Marine Aids to Navigation authorities and suppliers of retroreflective material. It includes terminology, design, characterising, classification and guidance on its use for Marine Aids to Navigation purposes.

Retroreflective material for aids to navigation purposes

For floating aids retroreflective materials should be used with the code in according to the IALA R0106(E-106).

Further there are many applications for fixed Aids to Navigation, e.g.:

Day boards for leading lines

Structures of beacons and lighthouses

Signs for waterways

Lettering and numbering

Marking of obstacles and piers

Floating Aids to Navigation

Commonly retroreflective material are used as an alternative to lights on buoys on less important fairways and fairways for leisure crafts; however, they also have importance on lighted fairways in case of failure of a light.

Generally the shape, the structure and the size of the buoy cannot be made visible with retroreflective material. Due to this limitations retroreflective material it is used for short range navigation(less than 1M) on buoys only.

The nautical requirement of retroreflective material for floating aids is described and specified by IALA Recommendation R0106(E – 106), Use of Retro-reflective Materials on Aids to Navigation Marks within the IALA Maritime Buoyage System.

IALA Recommendation R0106(E -106) deals with  two types of codes for floating aids – the Standard Code and the Comprehensive code.

The Standard Code is mostly for detecting with a degree of identification, especially for lateral marks.

The Comprehensive Code gives a more detailed identification of an aid. The Comprehensive Code often used in complicated channels and archipelagos.

fixed Aids to navigation

Retroreflective material is used for different types of fixed aids to navigation and for purposes related to safe navigation or warning of obstructions close to navigational water and fairways.  Applications where retroreflective materials are used can be  for day boards for leading lines, lettering and numbering, signs for waterways, marking of edges, jetties, piers etc.

Figure 1 Illuminated ID number on a day board (DMA Greenland)

HISTORY

The earliest recorded formation of glass into spherical shapes dates back to early Chinese history. Observation of light reflected back towards the light source from these spheres was used to intensify the brightness or brilliance of arts object. Glass spheres of different coloured glasses can be found in ancient jewellery. Many of the cuts of the facets of diamond are made to retroreflect the incident light, resulting in the brilliance of the diamond.

The first use of retroreflective material for purpose of enhancing the conspicuity of objects was probably created in Great Britain around the turn of the century (1800/1900). Observation of light reflected from animal’s eyes, especially those of cats, started the thought of using this technique to enhance the brightness of objects.

The explanation of the glowing nature of cat’s eyes stems from the highly reflective nature of their retinas. These animals were primarily nocturnal and relied on making the most use of the available low light level. The tissue (tapetum lucidum) immediately behind the retina is coated with material which reflects over 80 % of the incident light, and reflects visible light back through the retina, increasing the light available to the photoreceptors and then increase the detectability of objects.

Figure 2 Cross section of a Cat's eye

Figure 3 Cat's "glowing eyes"

The first use of the “cat eye” principal was for the safety of drivers in road traffic application,. therefore investigations were made resulting in the production of glass spheres with retroreflective features.

Figure 4  Cat's eye for a bicycle

Retroreflective material is today available in arrays in different sizes and colours, sheeting of plastic and metal, adhesive tape etc.  Numerous manufacturers for various applications provide many different colours and degrees of reflection intensity.

As with any retroreflector, sheeting glows brightly when there is a small angle between the observer's eye and the light source directed toward the sheeting, but appears non-reflective when viewed from other directions.

Terminology, PRINCIPLE, basic technology and design

The International Commission on Illumination (CIE), the international standardizing body responsible for light and colour measurement, defines retroreflection as follows:

“Reflection in which the reflected rays are preferentially returned in direction close to the opposite of the direction of the incident rays, this property being maintained over wide variation of direction of the incident rays”

Figure 5 Reflective and Retroreflective

Figure 6 Illustration of the cone of retroreflected light

Reflection and retroreflection

When looking at a reflecting surface the image may be complete blurred as in surface with diffuse reflection, or it may be sharp as in surface with mirror reflection, see figure 7.

Most practical surfaces have mixed reflection, which is a mixture of diffuse reflection and mirror reflection in the surface, mostly with the surface reflection partly blurred by texture.

A particular kind of reflection is retroreflection, where  most of the light is reflected back to the observer.

Figure 7 Retroreflection compared with other reflection patterns

The glass sphere or bead

There are two basic optical systems for obtaining retroreflection – the Glass Sphere or Bead and the Prismatic or Cube Corner Reflector.

Figure 8 Glass Bead and Prismatic Retroreflectors

The simplest retroreflector is a glass sphere or bead and this type was the first retroreflective element used for the so-called “Cat’s Eye”. Depending of the construction the glass sphere/bead can be divided in three different types in respective order according to improvement – exposed glass bead, enclosed glass bead and encapsulated glass bead.

When a light beam is directed at it, the majority of the light bounces off it but a significant amount passes through the front surface and is bent or refracted roughly toward the centre of the rear surface. Some light hitting the rear surface of the sphere is internally reflected back through the front surface of the sphere face and is again refracted onto a course parallel to the direction from which it came.

Only 28 % of the area of the sphere is at a sufficiently favourable angel to return the light beam and there are losses every time the light encounters a surface of the glass, especially when the beam hits the rear wall where a large proportion passes through it rather than being internally reflected. A major improvement in retroreflectivity can therefore be achieved by coating the sphere’s rear surface so that it acts as a mirror, see figure 9

Figure 9 Glass Sphere or Glass Bead

Prismatic or cube corner reflector

More efficient is the prismatic or cube-corner reflector.

If you take a solid glass cube and slice off one corner with a cut that passes along the diagonals of three adjoining faces you have the basic cube-corner unit which is a squat triangular pyramid shaped prism. When the pyramid is set up with the triangular base directed towards a beam of light, the light passes through the base with very little loss. Once inside the pyramid the light is internally reflected off each of the three side faces in turn before being directed back through the base, exiting parallel to the incoming light beam. Reflected light is still parallel to the incoming beam  as the light is equally refracted when entering and leaving the prism, see figure 10.

The cube-corner pyramid prism is a fairly efficient retroreflector but has two limitations:

Light entering closer to the corners of the triangular base is only internally reflected off the two nearest sides and misses the third side, which is too far away. About 35 % of the incoming light is lost in this way.

As the angel at which the light approaches the entry face becomes shallower, so an increasing proportion of the light will bounce off the surface instead of entering the pyramidal prism. These losses are relatively small where the light hit it within 10 dg to 15 dg of square but rapidly increase at angels that are more acute.

Figure 10 Principle of Prismatic/ Cube Corner Reflector

Figure 11 Detail of Prismatic Retroreflector

The glass bead is less effective compared to the prismatic retroreflector and have a broader returning angel, see figure 12.

Figure 12 Dispersion path from Glass Bead and Prismatic Retroreflectors

Characterising and measurement of retroreflecting material

Mainly the retroreflective material is characterised by two properties  – the coefficient of retroreflection (RA) and the colour (CIE 1931)

Coefficient of Retroreflection

Performance values for retroreflective sheeting are an expression of the efficiency of that material to retroreflect the light at a particular “geometry”; i.e., at one set of observation and entrance angles. (One “geometry” often used in specifications is 0.2 degrees observation angle and 5, 30 and 40 degrees entrance angle.) The number given tells how much light is retroreflected at that “geometry” for a given unit of light falling on a given area of the material. Technically, it is termed the “Coefficient of Retroreflection,” designated by the symbol RA . (Here we’ll sometimes refer to it as the “retroreflectivity value” or simply, “retroreflectivity”).

“RA ” essentially expresses the relationship “light out/light in”:

RA = light out/ light in

[cd/m2 * 1/lx] = [cd/(lx * m2)]

Figure 13 Coefficient of Retroreflection (Ra)

The important concept to understand is that the retroreflectivity value RA is a ratio. It’s similar to “per cent” and does not tell how bright the sheeting will be on a given sign (even at the distance corresponding to the “geometry” for that particular value).

It is simply its “efficiency” at returning light to the source at that particular geometry (the set of observation and entrance angles).

The efficiency of a retroreflective material varies with different observation and entrance angles and the various materials vary in different ways. The practical effect of these differences is what influences the choice among different retroreflective materials for a particular situation, taking into account headlight illumination, practical viewing conditions and distances, and the viewing needs of the user.

Figure 14 CIE Goniometer system for specifying and measuring retroreflectors

Determination of the RA is carried out by a laboratorium arrangement shown in figure 14.

The ‘observation angle’ α is the angle between the light source, producing the incoming light, and the observer equal to the human eye. Most of the available retroreflective material is designed for road traffic signals and in common the applied ‘observation angle’ is for this purpose. In practise, the angle is given by the vertical distance between the head light (light source) of the car and the driver’s position (observer) in the car and in addition to this the distance of use.

The ‘entrance angle’ is the angle from the ‘light source’ axis to the ‘retroreflector axis’ and is characterised by two components, β1 and β2. In technical data sheets of retroreflective materials, it is most common only to display the value of β1.

The ε is the angle describing the rotational angle of the specimen around the perpendicular of the reflecting surface.

The table below, figure 15, shows a typical datasheet from a manufacture of retroreflective material.

The table shows at left the geometry of the measurements. Three sets of the ‘observer angle α’ and three sets of the ‘entrance angle β1’. Remark that β2 = 0

The actual retroreflective material is available in six different colours and the value of Ra [cd/ (lx*m2)] respectively each colour is displayed under different geometry.

Figure 14 Example of data sheet for retroreflective film (Coefficient of Retroreflectivity)

Colour

Retroreflective material is typically available in signal colours for white, yellow, red, green, blue and orange.

Although there is a colour for orange, but it is not recommended to use this colour for Marine Aids to Navigation purpose due to its confusion with yellow and red.

The surface colour is described by a luminance factor β and two chromaticity coordinates x, y (see IALA Recommendation E – 108 On Surface Colours).

Measurement of the colour of retroreflective material is carried out by same method as for other surfaces colours and in accordance with IALA Recommendation E – 108 On Surface Colours.

The table below, figure 16, shows the chromaticity coordinates for the above mentioned retroreflective material. A typical way to present the actual chromaticity coordinates and luminance factors in a data sheet is displaying corner coordinate belonging to a specific standard and then confirm that the actual retroreflective material is in accordance to that standard.

Almost always the chromaticity coordinates for colour specification in datasheets are for daytime observations but some manufacturers also have information of night time observations. For retroreflective-fluorescent material, the colour specification is usually available both for daytime and night time due to use also in daytime.

Retroreflective film in black colour is available. In daytime it is visibly black and during night time, when illuminated, it will appear white.

Figure 16 Example of data sheet for retroreflective film (Chromaticity and Luminance factor)

Classification and Standards of Retroreflective Material

Standardisation of retroreflective material is related to the increase in use of automobiles and historical the first specification on the topic for safe driving was probably  formulated in the United States in the 1930s.

The start of the international standardation on retroreflective materials began in Vienna in 1968 with the Convention of Road Signs and Signals. Today CIE is the international organization for the standards in light and colour.

Many technical reports and documents are dealing with the recommendations for signals, retroreflection, and roadway lighting are the basis for international agreements. The geometry of measurement differs somewhat among various countries; however, the today’s international trend is to specify the characteristics of retroreflectors in terms of the driving or transportation scenario.

Specific guidelines for retroreflective material for marine aids to navigation is not currently available and it seems like common practice for Aids to Navigation administrations and suppliers not having further requirement than the requirement for the IALA code in accordance with IALA  Recommendation R0106(E – 106).

Different organisations are working with and preparing standards, recommendations, technical documents and reports about retroreflective materials.

Viewing for available standards and procedures on the subject area, ASTM (American Society for Testing and Materials) and CIE (Commission Internationale De L’éclairage/ International Commission on Illumination) have a leading role and detailed documents and specifications are issued by EN, DIN and other bodies.

Typical data sheets describing retroreflective materials are commonly referring to ASTM or to EN/DIN standards. For measurement procedures, reference is to CIE Technical Report 54.2 on Retroreflection, Definition and Measurement.

Commonly used standard in Europe is:

EN 12899-1 (Fixed, vertical road traffic signs):

Class RA1

Class RA2

DIN 67520 (Retro-reflecting materials for traffic safety):

Class RA1

Class RA2

Class RA3A

Class RA3B

Class RA1 refers to the lowest grade of retroreflective material, sometimes known as Engineer Grade.

Class RA3A and class RA3B includes florescent retroreflective material

Consideration when APPLYING Retroreflective Material

When applying retroreflective materials for Aids to Navigation the type of use must be considered. In general, the application for floating aids and fixed aids differs. For example floating aids are dynamic objects with limited size and fixed aids are static objects that may be very large.

Floating Aids to Navigation

Floating Aids to Navigation is typically buoys and used for short range navigation. Buoys can have different design and different size. The hydrostatic properties of the buoy have great influence on how the buoy performs with the retroreflectors during different sea conditions, including wind, current, waves etc.

When approaching and passing a buoy the observer sees the buoy from very different positions. In addition the buoy may move vertically and may heel, see Figure 15.

Figure 15 Movement pattern of a buoy (spar buoy)

SMALL BUOYS

On small buoys and spar buoys, the retroreflective material is commonly applied as a band on the full circumference of the buoy – the retroreflector is therefore omnidirectional.

Omnidirectional retroreflective band

Figure 16 Band on the full circumference on small buoys

LARGE BUOYS

On larger buoys the shape, size and the structure of the buoy do not allow to use a band on the full circumference of the body of the buoy. In this case the retroreflective sheets are applied to the buoy body at specific possible positions on the circumference.

There are three commonly used arrangements shown in figures underneath.

In each figure the positions of the retroreflective sheets are shown and the figures also shows how they are seen from the observer in different directions

The retroreflective coverage is best at 90°, 120° and 180°, respectively. At the 180° application and with a viewing angle of 90° there is none or minor coverage depending of the lengths of the band and the diameter of the structure where the retroreflective band is fitted.

Figure 18 Retroreflector applied for every 90 Degrees

Figure 19 Retroreflector applied for every 120 Degree

Figure 20 Retroreflector applied for every 180 Degrees

Notice: Care should be taken for safe water marks and emergency wreck marking buoys when using comprehensive code with vertical stripes. In this case an arrangement with an angle of 90° is preffered.

The shape of the buoy have influence on the retroreflectivity. As illustrated at figure 21, the entrance angel for the red buoy is better than for the green buoy, and a heeling of the buoy due to wind and current can have excessive influence of the retroreflectivity. Figure 23 shows a spar buoy with a excessive heeling of approx. 45° and compared to data sheets of common used retroreflective the reduction in retroreflectivity is significant.

Figure 21 Buoys shape compared with the viewing angel

Due to the dynamic movements and heeling, determination of night time range can be difficult and insufficient.

Thus, a daymarker buoy is not comparable with a lighted buoy.

Figure 2 Spar buoy healing approx. 45 Degree

Movement of the buoy and movement of the observing vessel including the eye height of the observer should also be considered when selecting and specifying retroreflecting material for floating aids, see figure 23.

Figure 23 Eye height compared for a small and a large vessel

The curvature of the buoy has influence on the retroreflectivity as illustrated at figure 24. A searchlight illuminates two buoy body structures and lengths of the dotted lines present the retroreflected intensity. In the left illustration, the curvature of the buoy cause a lower retroreflectivity than the flat structure of the buoy illustrated to the  right. The reason is that the entrance angel of the light is increased and a large entrance angel cause less retroreflectivity. In fact, a curved retroreflective band can have a very small ‘active’ area and consequently a very limited retroreflectivity. The reflectivity of a spar buoy, with a limited diameter, can be increased with a broader retroreflective band (vertical) causing a larger ‘active’ area in the observers direction.

For floating aids, it is preferable to choose retroreflective material with large entrance angle (β).

Figure 24 Retroreflectivity depending on the curvature shape of the buoy

Fixed Aids to Navigation

Fixed Aids to Navigation is static and their use is closely comparable with the use of retroreflective materials for road signs and marking for traffic.

Therefore, use of retroreflective material and estimation of range can be more detailed and effective compared to floating aids with continually movements and continually observer geometry.

Fixed aids to navigation with retroreflector is commonly for longer distance navigation compared to retroreflector applied on floating aids.

Day boards in leading line can be of a size of several square meters.

Figure 25 Large day board for a leading line (DMA Greenland)

General considerations for Floating and Fixed Aids to Navigation

Colour

A retroreflective surface should not be used for daymarks throughout.

The retroreflective principle works only when the surface is illuminated at night with a searchlight near the observer.

In daylight the retroreflective colours show low luminance and are not very conspicuous.

Manufactures of retroreflective material has introduced retroreflective-fluorescent films. However, the colours available are made for road traffic signals and there is not a complete set of films for the IALA MBS colours.

Care should be taken that the amount of white retroreflecting material used on an aid does not detract from its daytime appearance. For cardinal marks in standard code, black retroreflective film showing white colour when illuminated in nighttime

Figure 26 Spar buoy with green retroreflective band

Information regarding coding of colours for floating aids is described in IALA Recommendation R0106 (E-106).

It may be difficult for the observer to discriminate between yellow and white retroreflecting materials particularly where only one of these colours is being observed on its own. Thus only one yellow band may be used on a special mark to avoid confusion with a West Cardinal mark in the comprehensive code (two yellow band).

It may also be difficult for the observer to discriminate between green and blue retroreflecting materials, particularly where only one of these colours is being observed on its own. In principle, green buoys should carry only one green band, whereas blue is always used in combination with another colour, except in the case of East Cardinal marks which have two blue bands according to IALA R0106 (E – 106). However, this principle may be violated if one of the bands has become damaged.

The coefficient of retroreflection of blue and red is  much lower than white or yellow, and to ensure proper recognition the following must be observed:

• Safe water marks:

The red bands or stripes must be at least twice the width of the white bands or stripes. The separation distance between the colours must be at least twice the width of the white bands or stripes.

• North and South Cardinal Marks:

The blue bands must be at least twice the width of the yellow bands. The separation distance must be at least twice the width of the yellow bands.

To ensure proper recognition of isolated danger marks the blue and red bands should be of equal width and separated by a distance at least equal to the width of a band.

Retroreflective material simply for detection purpose use only white material in form of letters, numbers or symbols.

Figure 27 South Cardinal, Comprehensive Code, double blue band and single yellow band

Photometric Performance when wet

The photometric performance of the retroreflective material can change under wet condition. Particularly glass bead retroreflector can have decreased performance under wet condition. Tests have shown that micro prismatic retroreflector, compared to glass bead, performs better under wet condition.

Temperature

High and low temperature can cause deformation of the retroreflective material and the deformation can cause loss of coefficient of retroreflection, cracking, distortion and reduced lifetime.

When specifying retroreflective materials it is important to select materials with technical temperature specifications at least equal to or better than the local annual temperature variation.

Flexibility

Buoys can have curved and sharp edges and it is necessary to select the retroreflective materials that can be bended as necessary.

If the flexibility is not adequate for the actual use, the retroreflective material will crack and there will be a loss in retroreflectivity.

Cleanability

To obtain high performance retroreflectivity and long lifetime of the material it is important that the retroreflective material have good self-cleaning characteristics.

Gloss and uniform surface is recommendable.

Application of Retroreflective Material

Proper application technique is very important to obtain optimal retroreflective performance and to insure long lifetime of the retroreflective material.  The manufacture’s instruction for applying retroreflective material must be followed. Data sheet of the product have commonly detailed information.

Read all health hazard, precautionary and first aid statements before handling the material.

Degradation of Retroreflective Materials

The deterioration rate or service lifetime of retroreflective material depends of many factors and their influence is type dependent.

Plastic cube-corner prismatic materials are the most common type applied as retroreflective material at aids to navigation.

The colour may change due to pigment fading and loss of transparency caused by UV exposure. The material for unbending cube corners may crack allowing moisture to penetrate and destroy the sheet. Due to the harsh environment the retroreflective materials are often exposed for mechanical injury caused by scratching from to close passing vessels, ice scratching, change in temperature and humidity etc.

Microprismatic materials that are used in flexible materials will deform, changing the shape of faces and spreading the returned light, thus lowering the value at the same geometry.

Precaution when using Radar Reflector in combination with Retroreflecting Materials

Experiences have shown that retroreflective material consisting of metal folio can cause a lower Radar Cross Section (RCS) value. It is recommended not to apply the retroreflective material on the buoy surface where the surface covering an integrated radar reflector.

Calculation of Size of Retroreflectors

For calculation of the approximately size of a retroreflector, following quantities must be known:

- the intensity of the searchlight, Is [cd]

- the distance between the searchlight and the retroreflector, d [m]

- the retroreflectivity (datasheet from supplier), Ra [cd/lx/m2]

- the meteorological visibility, V [m]

Allard’s law allows the calculation of the illuminance as a function of distance, luminous intensity and the meteorological visibility, Reference to [7]

Ed=I0.05dVd2

Where:

E	is the illuminance at the eye of the observer [lx]

I	is the luminous intensity [cd]

d	is the distance between the light and the observer [m]

V	is the meteorological visibility (V=V0,05), see IALA dictionary

Figure 28 Quantities of Allard's Law

Figure 29 Quantities of Retroreflectivity

Calculation of incidence illuminance (E) at the retroreflector:

E=IsI0.05dVd2

Calculation of the luminous intensity of the retroreflector:

IIr=Ra*E*A

Where:

Ir	is the luminous intensity of retroreflector [cd]

Ra 	is the retroreflectivity of the reflector, [cd/lx/m2]

E	is the incident illuminance at the retroreflector surface, [lx]

A	is the size of the retroreflector, [m2]

Separated for A and calculate the size of the retroreflector:

A=IIrRa*E

The luminous intensity, Ir, must be equal to or greater than the user distance for the retroreflective material to be visible. The value derives from a table converting range in nautical miles to luminous intensity (cd)

Example of calculation size of retroreflector in a leading line

Figure 30 Leading line with retroreflectors

Figure 31 Data Sheet of retroreflective film

Example:

A day board in a leading line is fitted with white retroreflective film. The retroreflective film conforms to EN 12899-1:2007 for class RA 2, and have a coefficient of retroreflection of 250 cd/ (lx*m2) covering a viewing angel β of +5°. Due to the distance vessel/retroreflector and site of observer on the bridge just below the searchlight, the observation angel α is selected to be 0.2°

The maximum user distance is one NM (1,852 meter) and inbound vessels have commonly a searchlight with a luminous intensity of 100,000 cd. It is a clear night with a visibility of 10 NM (18,520 meter). There is no background light.

Calculate the minimum size of the retroreflector in m2.

1. Calculate the incident illumination at retroreflector:

E=IIs0.05dVd2

E=100,0000.0518521852018522

E=0,021608 lx

2. Calculate the minimum size of the retroreflector:

A=IrIRa*E

A=1250*0,021608

(The observation distance in the example is 1 NM and 1 NM is equal to 1 candela, therefore I = 1 cd)

A=0,185 m2

Equivalent to a retroreflective board of 0,43 x 0,43 meter!

best practice and typically application

In this chapter, different picture shows best practice on application of retroreflective materials.

Figure 32 Example of a protective arrangement of retroreflective material (SeaHow and Sabik)

ACRONYMS & Definitions

Acronyms

IMO	International Maritime Organization (Acronym style)

MBS	IALA Maritime Buoyage System

CIE	COMMISION INTERNATIONALE DE L’ECLAIRAGE/ INTERNATIONAL COMMISSION ON ILLUMINATION

Definitions

The definition of terms used in this Guideline can be found in the International Dictionary of Marine Aids to

Navigation (IALA Dictionary) at (http://www.iala‐aism.org/wiki/dictionary).

REFERENCES

IALA Recommendation R0106(E – 106), Use of Retro-reflective Materials on Aids to Navigation Marks within the IALA Maritime Buoyage System

IALA Recommendation E – 108, Surface Colours used as Visual Signals on Aids to Navigation

IALA Guideline 1094, Daymarks for Aids to Navigation

CIE 54.2-2001 Retroreflection: Definition and Measurement, ISBN 978 3 900734 99 2

Handbook of Applied Photometry, Casmir DeCusitio

Test methods for the coefficient of retroreflection of microprismatic sheeting materials, Kai Sørensen, DELTA, April 2004

IALA E-200-2(or new guideline on calculation)